| CABLE No. | FNL-1-I-00646 ,646A,B,C |
| --- | --- |
| MFG. | 9/22/98 |
| OPERATOR: | H. Higley |

CABLE LOG SHEET

LBNL  SUPERCONDUCTING MAGNET CABLES

BLD 52

Objective:  Preliminary cabling trials.

- Make majority of cable to nominal size.

- Balance of cable in two samples varying mid thickness by +/- .030mm

Note:  Wire dia.  inspected as oversized by  .012mm

- STRAND INFORMATION -

| MANUFACTURER : | IGC |
| --- | --- |
| BILLET #: | FR2044 |
| SPOOL #: | 1,2,3,4-1 |
| COMPOSITION : | Nb3Sn |
| STRAND Dia.. NOMINAL : | 1.000mm | INSP. DIA..: | 1.012mm avg. |
| Cu/SC RATIO NOMINAL : |  | INSP. RATIO : |  |
| FILAMENT TWIST/LENGTH : | 11mm | DIRECTION : | Right |
| SHARP BEND TEST : |  |
| LENGTH PER SPOOL : | 94m |

- CABLING SPECIFICATIONS -

| TYPE or SPEC.: | FNAL Prototype Nb3Sn 28 strand x 1.000mm for Alexander Zlobin. |
| --- | --- |
| No. of STRANDS: | 28 |
| PITCH DIRECTION: | LEFT | PITCH LENGTH: | 109.8mm |
| PLANETARY RATIO: | 0 : 1 |
| ROLLER ID #: | P-1 & 2 | WIDTH: | 14.165mm | ANGLE:: | 1.021 deg. |
| MANDREL ID #: | 39 | WIDTH: | 15.49mm | THICKNESS:: | 0.70mm |
| LUBRICATION : | 100% 4-BR |
| STRAND TENSION: | 5.5 lb | TURKS HEAD LOAD "SGM": | -130 lb. |
| Nom. THICKNESS: | 1.785 mm +/- 0.006mm |
| Nom. WIDTH: | 14.240mm +/- 0.025mm |
| Nom. ANGLE: | 1.0 deg +/- 0.1 deg. |

- FINISHED CABLE -

|  | At Hub of Spool |  |  |  | At Top of Spool |
| --- | --- | --- | --- | --- | --- |
|  | Cable Start-up : | NOMINAL Thick. | -0.030mm | +0.012mm | +0.031mm |
|  | “Variable size” | FNL-1-I-00646 | 646-A | 646-B | 646-C |
| FINISHED LENGTH: | 15.7m | 39.6m | 16m | 6m | 7.6m |
| Avg. THICKNESS: | oversized. | 1.7852mm | 1.7579mm | 1.7965mm | 1.8161mm |
| Avg. WIDTH: | undersized | 14.232mm | 14.233mm | 14.233mm | 14.240mm |
| Avg. ANGLE: | ~0.93 deg. | 0.910 deg. | 0.889 deg. | 0.924 deg. | 0.933 deg. |

| RESIDUAL TWIST/Mtr.: | 60 deg under twist OK. |
| --- | --- |
| ETCH for FILAMENT DAMAGE: | Only sample from tail end of run etched OK H.H. |

See Notes Pg. 2

| CABLE No. | FNL-1-I-00646 ,646A,B,C |
| --- | --- |
| MFG. | 9/22/98 |
| OPERATOR: | H. Higley |

NOTES:

Nominally dimensioned cable has sharp minor edges and the -0.030mm cable is bordering on sharp with flashing.

As this cable was not cut between  samples Nominal ,A,B and C  , a 25mm long sample of each cable  should be soldered , cut and sent to Ron Scanlan at LBNL for metallography.

The Keystone angle was low for all samples.  Note the angle change as a function of  mid thickness.  Future cables can have the rolls ground to an optimum angle for a particular mid thickness.

Start of run oversized. At hub of spool

Start of run oversized. At hub of spool

Nominal Thickness. FNL-1-I-00646

Nominal Thickness. FNL-1-I-00646

-0.030mm thickness  646-A

-0.030mm thickness  646-A

+0.012mm  646-B

+0.012mm  646-B

+0.031mm  646-C.  Top of spool

+0.031mm  646-C.  Top of spool