| CABLE No. | FNL-1-I-731…733 |
| --- | --- |
| MFG. | 11/8/99 |
| OPERATOR: | H. Higley |

CABLE LOG SHEET

LBNL  SUPERCONDUCTING MAGNET CABLES

Objective:  Preliminary cabling trials.

- Make cables as proposed by A. Zlobin and E. Barzi.

- STRAND INFORMATION -

| MANUFACTURER : | IGC |
| --- | --- |
| BILLET #: | B7419 | B7420 | B7421 | B7429 | B7490 |
| No of strands: | 3 | 6 | 7 | 6 | 6 |
| COMPOSITION : | Nb3Sn 19 subelements. |
| STRAND Dia.. NOMINAL : | 1.000mm | INSP. DIA..: | 1.000mm avg. |
| Cu/SC RATIO NOMINAL : | 58.7% | INSP. RATIO : |  |
| FILAMENT TWIST/LENGTH : | 11mm | DIRECTION : | Right |
| SHARP BEND TEST : | Pass 3/3 |
| LENGTH PER SPOOL : | 470m |

- CABLING SPECIFICATIONS -

| TYPE or SPEC.: | FNAL Prototype Nb3Sn 28 strand x 1.000mm with and without SS core. SS Core material is 12.7mm x .025mm 316-L annealed. Core tension = .5 kg. |
| --- | --- |
| No. of STRANDS: | 28 |
| PITCH DIRECTION: | LEFT | PITCH LENGTH: | 109.8mm |
| PLANETARY RATIO: | 0 : 1 |
| ROLLER ID #: | P-1 & 2 | WIDTH: | 14.165mm | ANGLE:: | 1.021 deg. and 0.00 |
| MANDREL ID #: | 37 | WIDTH: | 13.58mm | THICKNESS:: | 0.90mm |
| LUBRICATION : | 100% 4-BR |
| STRAND TENSION: | 2.7 kg. | TURKS HEAD LOAD "SGM": | 59 kg. |
| Nom. THICKNESS: | 1.800 mm +/- 0.006mm |
| Nom. WIDTH: | 14.240mm +/- 0.025mm |
| Nom. ANGLE: | .910 deg +/- 0.1 deg. |

Notes:

The mandrel used was of the earlier design and should be replaced before any long runs of cored cable.  There were

Some instances where the core poked between the strands.  This may have been due to the mandrel design or core tension.

The rolls were reground flat for the last two samples run # 733A and B.

In retrospect I should have done the short samples first to insure we had enough strand.  As it turned out

I made the long lengths longer than the minimum required and ran a little short of wire for the last two samples.

Special Procedures:

- Three strands were marked with red, green and blue ink at approximately 1m intervals.  The spacing of these marked strands makes it possible to identify from which billet all the strands originated.  The strand map has the strand color identification and placement information.

- Strands were marked just ahead of the turkshead roll to determine process elongation.

The strands were knicked with wire cutters at ~4x the pitch length or exactly 440mm +/- .1mm.

These marks were then measured just after the turkshead and compared to the expected contraction.

The sections of cable with knicked strands should be removed from the cables as they may be damaged.

August 24, 1999

A. Zlobin

# Nb3Sn cable and short sample parameters

1. ITER strand:

- Strand diameter (nominal) – 1.000 mm	0.998 mm (measured)

- Total length – 14270 m

2. Nominal cable parameters:

- Number of strands –    	28

- Strand diameter –        	1.000 mm

- Cable width –              	14.24 mm

- Cable mid-thickness – 	1.800 mm

- Minor edge –               	1.687 mm

- Major edge –               	1.913 mm

- Keystone angle –         	0.91 degree

- Transposition angle –  	14.5 degree

- Transposition pitch –   	110 mm

- Cable packing factor – 	0.89

3. Cables to be fabricated:

| # | Cable | Length, m | Width, mm | Min. edge, mm | Max. edge, mm | Mean thickness, mm | Packing factor, % | Special requirements |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | A (nominal) | ~180 | 14.240 | 1.687 | 1.913 | 1.800 | 88 | Lmin=65 m |
| 2 | B (nominal with SS core) | ~150 | 14.240 | 1.687 | 1.913 | 1.800 | 88 | 25 mm SS core, Lmin=65 m |
| 3 | AA (short samples): - AA85 - AA87 - AA89 - AA91 - AA93 - AA93a | 15 15 15 15 15 15 | 14.240 14.240 14.500 14.240 14.240 14.240 | - 1.702 1.650 1.622 1.584 1.584 | - 1.951 1.915 1.870 1.833 1.833 | 1.869 1.827 1.782 1.746 1.709 1.709 | 85 87 89 91 93 93 | Rect. x-section Larger width Two steps: 1st-AA87, 2nd-AA93 in opposite direction |
| 4 | BB (short samples with SS core): - BB86 - BB90 - BB92 | 15 15 15 | 14.240 14.240 14.240 | - 1.642 1.603 | - 1.890 1.851 | 1.848 1.766 1.727 | 86 90 92 | Rect. x-section |

Special requirements:

- during fabrication of short samples AA and BB make marks on 2-3 strands separated by 1 m along the strand before cabling. The marks should allow one to find them in the cable after fabrication

Process Elongation

Note: Cable Packing Factor  does not include strand elongation.

| F1I00731-733 as Manufactured LBNL H. Higley 11/12/1999 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| UNCOMPACTED | 731-A | 731-Bc | 732-Ac | 732-Bc | 732-Cc | 732-Dc | 732-E | 732-F | 732-G | 732-H | 732-I-1 | 732-I-2 | 733-A | 733-Bc |
| No. of Strands = | 28 | 28 | 28 | 28 | 28 | 28 | 28 | 28 | 28 | 28 | 28 | 28 | 28 | 28 |
| Strand DIA. = | 1.0002 | 1.0002 | 1.0002 | 1.0002 | 1.0002 | 1.0002 | 1.0002 | 1.0002 | 1.0002 | 1.0002 | 1.0002 | 1.0002 | 1.0002 | 1.0002 |
| Pitch Angle = | 14.7771 | 14.77715 | 14.7771 | 14.7771 | 14.7771 | 14.7771 | 14.7771 | 14.7771 | 14.7771 | 14.7771 | 14.7771 | 14.7771 | 14.7771 | 14.7771 |
| Cable Width = | 15.2039 | 15.2039 | 15.2039 | 15.2039 | 15.2039 | 15.2039 | 15.2039 | 15.2039 | 15.2039 | 15.2039 | 15.2039 | 15.2039 | 15.2039 | 15.2039 |
| Cable MID Thk. = | 2.0004 | 2.0258 | 2.0258 | 2.0258 | 2.0258 | 2.0258 | 2.0004 | 2.0004 | 2.0004 | 2.0004 | 2.0004 | 2.0004 | 2.0004 | 2.0258 |
| Pitch length = | 109.8 | 109.8 | 109.8 | 109.8 | 109.8 | 109.8 | 109.8 | 109.8 | 109.8 | 109.8 | 109.8 | 109.8 | 109.8 | 109.8 |
| PF = | 0.74809 | 0.74809 | 0.74809 | 0.74809 | 0.74809 | 0.74809 | 0.74809 | 0.74809 | 0.74809 | 0.74809 | 0.74809 | 0.74809 | 0.74809 | 0.74809 |
| COMPACTED | 731-A | 731-Bc | 732-Ac | 732-Bc | 732-Cc | 732-Dc | 732-E | 732-F | 732-G | 732-H | 732-I-1 | 732-I-2 | 733-A | 733-Bc |
| Cable Width = | 14.2364 | 14.2277 | 14.2544 | 14.2256 | 14.2143 | 14.213 | 14.2637 | 14.2268 | 14.2201 | 14.2155 | 14.2728 | 14.2142 | 14.2697 | 14.2082 |
| Cable Mid Thk. = | 1.7989 | 1.8 | 1.9093 | 1.835 | 1.7796 | 1.756 | 1.8496 | 1.7952 | 1.7614 | 1.715 | 1.885 | 1.7064 | 1.8759 | 1.8224 |
| Keystone angle. = | 0.925 | 0.898 | 0.908 | 0.904 | 0.886 | 0.872 | 0.918 | 0.906 | 0.902 | 0.881 | 0.913 | 0.928 | -0.066 | 0.047 |
| Pitch length = | 109.8 | 109.8 | 109.8 | 109.8 | 109.8 | 109.8 | 109.8 | 109.8 | 109.8 | 109.8 | 109.8 | 109.8 | 109.8 | 109.8 |
| Pitch Angle = | 14.4389 | 14.4185 | 14.4981 | 14.4336 | 14.3910 | 14.3825 | 14.4904 | 14.4277 | 14.4046 | 14.3774 | 14.5166 | 14.3719 | 14.5091 | 14.4228 |
| Cable Thickness |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| MINOR EDGE = | 1.6840 | 1.6631 | 1.7709 | 1.6974 | 1.6353 | 1.6224 | 1.7353 | 1.6827 | 1.6495 | 1.6057 | 1.7713 | 1.5913 | 1.8841 | 1.8166 |
| MID = | 1.7989 | 1.7746 | 1.8839 | 1.8096 | 1.7452 | 1.7306 | 1.8496 | 1.7952 | 1.7614 | 1.7150 | 1.8850 | 1.7064 | 1.8759 | 1.8224 |
| MAJOR EDGE = | 1.9138 | 1.8861 | 1.9969 | 1.9218 | 1.8551 | 1.8388 | 1.9639 | 1.9077 | 1.8733 | 1.8243 | 1.9987 | 1.8215 | 1.8677 | 1.8282 |
| Packing Factor |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| MINOR EDGE = | 94.76% | 96.00% | 90.02% | 94.08% | 97.71% | 98.49% | 91.80% | 94.89% | 96.84% | 99.50% | 89.89% | 100.41% | 84.52% | 88.01% |
| MID = | 88.71% | 89.97% | 84.62% | 88.25% | 91.56% | 92.34% | 86.13% | 88.94% | 90.68% | 93.16% | 84.47% | 93.63% | 84.89% | 87.73% |
| MAJOR EDGE = | 83.38% | 84.65% | 79.83% | 83.09% | 86.13% | 86.90% | 81.12% | 83.70% | 85.27% | 87.58% | 79.66% | 87.72% | 85.27% | 87.45% |
|  | 731-A | 731-Bc | 732-Ac | 732-Bc | 732-Cc | 732-Dc | 732-E | 732-F | 732-G | 732-H | 732-I-1 | 732-I-2 | 733-A | 733-Bc |
| Finished Length m = | 134.0 | 136.0 | 14.7 | 17.0 | 16.4 | 17.7 | 16.7 | 15.3 | 15.0 | 12.7 | 11.7 | 11.7 | 8.7 | 7.0 |
| Process Elongation of strands: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Using Compacted Cable Pitch Angle and 440mm reference marks on strands. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | 731-A | 731-Bc | 732-Ac | 732-Bc | 732-Cc | 732-Dc | 732-E | 732-F | 732-G | 732-H | 732-I-1 | 732-I-2 | 733-A | 733-Bc |
| Calc. Length at Pitch = mm | 426.10 | 426.14 | 425.99 | 426.11 | 426.19 | 426.21 | 426.00 | 426.12 | 426.17 | 426.22 | 425.95 | 426.23 | 425.97 | 426.13 |
| Calc. Contraction % | 3.16% | 3.15% | 3.18% | 3.16% | 3.14% | 3.13% | 3.18% | 3.15% | 3.14% | 3.13% | 3.19% | 3.13% | 3.19% | 3.15% |
| Post Process--- |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Mark Length +/-0.5mm | 431.0 | 433.0 | 429.0 | 432.5 | 433.5 | 436.0 | 430.0 | 432.5 | 434.5 | 441.0 | 430.0 | 437.5 | NA | NA |
| Estimated Process Elongation | 1.15% | 1.61% | 0.71% | 1.50% | 1.71% | 2.30% | 0.94% | 1.50% | 1.96% | 3.47% | 0.95% | 2.64% | NA | NA |

### Strand Map for Cable Runs # F1I00731…733

| Mfg. ID # | LBNL Spool # | Insp. Dia. mm | Length m | Notes: |
| --- | --- | --- | --- | --- |
| IGC B7419 | 1 | 1.0012 | 470 |  |
| IGC B7419 | 2 | 1.0015 | 470 |  |
| IGC B7419 | 3 | 1.0010 | 470 |  |
| IGC B7440 | 4 | 1.0005 | 470 | Marked every ~ 1 m BLUE |
| IGC B7440 | 5 | 1.0000 | 470 |  |
| IGC B7440 | 6 | 1.0005 | 470 |  |
| IGC B7440 | 7 | .9905 | 470 |  |
| IGC B7440 | 8 | 1.0001 | 470 |  |
| IGC B7440 | 9 | 1.0006 | 470 |  |
| IGC 7420 | 10 | 1.0008 | 470 | Marked every ~1 m GREEN |
| IGC 7420 | 11 | 1.0005 | 470 |  |
| IGC 7420 | 12 | 1.0007 | 470 |  |
| IGC 7420 | 13 | 1.0010 | 470 |  |
| IGC 7420 | 14 | 1.0006 | 470 |  |
| IGC 7420 | 15 | 1.0011 | 470 |  |
| IGC 7429 | 16 | 1.0010 | 470 | Marked every ~1 m RED |
| IGC 7429 | 17 | 1.0008 | 470 |  |
| IGC 7429 | 18 | 1.0000 | 470 |  |
| IGC 7429 | 19 | 1.0010 | 470 |  |
| IGC 7429 | 20 | 1.0006 | 470 |  |
| IGC 7429 | 21 | 1.0002 | 470 |  |
| IGC 7421 | 22 | 1.0001 | 470 |  |
| IGC 7421 | 23 | 1.0000 | 470 |  |
| IGC 7421 | 24 | 1.0004 | 470 |  |
| IGC 7421 | 25 | 1.0004 | 470 |  |
| IGC 7421 | 26 | 1.0008 | 470 |  |
| IGC 7421 | 27 | 1.0003 | 470 |  |
| IGC 7421 | 28 | .9997 | 470 |  |
|  | Avg. Dia. = | 1.0002mm |  |  |

Example as seen from the start end of the cable:

1       2        3       4       5       6       7       8       9       10     11     12     13      14

Minor edge.

28     27     26      25    24      23     22      21     20     19     18     17      16     15

731-A  Nominal No Core.

731-A  Nominal No Core.

731-Bc  Nominal With Core.

731-B Nominal With Core.

732-Ac With Core.

732-Ac With Core.

732-Bc With Core.

732-Bc With Core

732-Cc With Core.

732-Cc With Core.

732-Dc  With Core.

732-Dc With Core.

732-E    No Core.

732-E   No Core.

732-F   No Core.

732-F   No Core.

732-G   No Core.

732-G   No Core.

732-H   No Core.

732-H   No Core.

732-I No Core First of Two Passes.

732-I No Core First of Two Passes.

732-I No Core Second Pass.

732-I No Core Second Pass.

733-A No Core Rectangular.

733-A No Core Rectangular.

733-Bc With Core  Rectangular.

733-Bc With Core  Rectangular.