MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A09682 | In-Flight Anomaly Number -- | Contractor Report Number T-050 | JSC# -- | KSC# -- |  |
| --- | --- | --- | --- | --- | --- |
| Problem Title PRIMER LIFT-OFF DURING WET TAPE TESTING |  |  |  |  |  |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 3 |  |
| HCRIT -- | Sys_Lvl N | Misc Codes A (2) B C D (X) E F G H I J K L M N O |  |  |  |
| HARDWARE EIM | NOMENCLATURE ET COMPLETE | PART# 80971068420 | SER/LOT# LWT-26 | MANUFACTURER MMC |  |
| HARDWARE LRU | NOMENCLATURE N/A | PART# N/A | SER/LOT# N/A | MANUFACTURER N/A |  |
| HARDWARE NCA | NOMENCLATURE ET COMPLETE | PART# 80971068420 | SER/LOT# LWT-26 | MANUFACTURER MMC |  |
| Test/Operation L - FLD | Prevailing Condtion F - FUNCTIONAL | F / U F | Fail Mode MSI - INSULATION | Cause MAW - MFG-ASY-WORK |  |
| System TPS | Defect DD - DETACH | Material F - INSUL | Work Contact F. RAMSEY | Fail Date 09/25/1985 |  |
| Received at MSFC 11/19/1985 | Date Isolated -- | FMEA Reference 1.2.1 | IFA: Mission Phase -- | Mission Elapsed Time -- |  |
| Location MAF |  | Symptom UC - UNSAT |  | Time Cycle -- |  |
| Effectivity Text LWT-37 |  |  |  |  |  |
| Vehicle Effectivity Codes |  |  |  |  |  |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |  |
| Mission Effectivity Codes |  |  |  |  |  |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |  |
| Estimated Completion Dates |  |  |  |  |  |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |  |  |
| Investigation / Resolution Summary |  |  |  |  |  |
| Last MSFC Update 01/03/1992 | CN RSLV SBMT 09/15/1986 | Defer Date -- | Add Date -- | R/C Codes 2 - MFG -- -- |  |
| Assignee |  |  |  |  |  |
| Design B. DAVIS | Chief Engineer -- | S & MA R. JACKSON | Project J. CAVALARIS | Project MGR -- |  |
| Approval |  |  |  |  |  |
| Design B. DAVIS | Chief Engineer -- | S & MA R. JACKSON | Project J. CAVALARIS | Project MGR -- |  |
| PAC Assignee G. MILLER | PAC Review Complete GM | MSFC Closure Date 10/24/1986 | Status C - CLOSED | F/A Completion -- |  |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |  |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- |  | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |  |  |  |  |
| Related Document Type -- | Related Document ID -- |  |  |  |  |
| Related Document Title -- |  |  |  |  |  |
| Related Document Type -- | Related Document ID -- |  |  |  |  |
| Related Document Title -- |  |  |  |  |  |
| Related Document Type -- | Related Document ID -- |  |  |  |  |
| Related Document Title -- |  |  |  |  |  |
| Contractor Status Summary |  |  |  |  |  |
| Reliability/Quality Assurance Concerns, Recommendations: |  |  |  |  |  |
| Problem Description REF: MARS T-79000 DURING A WET TAPE TESTING OPERATION IN A SCHEDULED CLOSEOUT AREA, PRIMER LIFT-OFF WAS NOTICED. THE ANOMALY EXTENDED INTO AN AREA WHICH WAS PREVIOUSLY PRIMED IN CELL "P." |  |  |  |  |  |
| Contractor Investigation/Resolution 11/19/85 GENERAL - THE LH2 TANK IS CLEANED AND EPOXY PRIMED IN CELL "P," BUILDING 131. AFTER THE CLEANING OPERATION, THE ENTIRE TANK IS INSPECTED FOR VISUAL CLEANLINESS AND OBVIOUS STAINS AND DISCOLORATIONS STAINS MAY BE CLEANED IMMEDIATELY PRIOR TO EPOXY PRIMER APPLICATION, OR MASKED WITH J-414 TAPE AND TOUCHED UP AFTER PRIMER APPLICATION. HISTORY OF CELL "P" SHOWS THAT MOST TANKS HAVE HAD A STAIN ANOMALY WHICH IS CAUSED BY DRIPS FROM THE CEILING AND ENTRAPMENT AREAS AROUND THE 2058 ROLL RINGS. ANOTHER PROBLEM AREA HAS BEEN AROUND THE LH2 FEEDLINE FLANGE DUE TO MASKING ENTRAPMENT OF THE FEEDLINE. IN BUILDING 420, THE AREA AROUND THE FEEDLINE FLANGE IS CLOSED OUT WITH PRIMER AND FOAM PER MPP. AFTER PRIMER APPLICATION, THE AREA IS WET TAPE TESTED PER STP/PI 3004. DURING THIS OPERATION ON LWT-26, PRIMER LIFT-OFF WAS NOTED ON AN AREA ADJACENT TO THE SCHEDULED CLOSEOUT. THE FAILED AREA WAS CHASED OUT UNTIL INDICATION OF GOOD ADHESION WAS NOTED. THE CAUSE OF LOW PRIMER TO SUBSTRATE ADHESION IS DUE TO IMPROPER TOUCH-UP OF STAIN AREAS IN CELL "P." INVESTIGATION - THIS CAPS WILL ADDRESS THE CORRECTIVE ACTION TO PRECLUDE LATENT DEFECTS CAUSED BY STAINS IN CELL "P." INVESTIGATIVE TASKS HAVE BEEN IDENTIFIED AS FOLLOWS: TASK I QUALITY ENGINEERING AND QUALITY CONTROL TO REVIEW PRESENT MAPPING REQUIREMENTS OF STAINS IN THE MPP'S. ADDRESS ANY ALTERNATE METHOD(S) OF RECORDING STAIN LOCATIONS OCCURRING ON THE LH2 TANK. TASK II MATERIALS ENGINEERING, QUALITY ENGINEERING, AND AMT TO REVIEW PRESENT CLEANING METHOD FOR TOUCH-UP AREAS USED IN CELL "P." ADDRESS ANY ALTERNATE METHOD(S) WHICH WOULD INCREASE THE RELIABILITY OF THE REWORKED AREA. TASK III MANUFACTURING ENGINEERING AND AMT TO REVIEW CELL "P" AREA (ENVIRONMENT AND TOOLING) TO IDENTIFY ENTRAPMENT AREAS WHICH COULD CAUSE STRAINS ON A CLEAN TANK CAUSE OF PROBLEM IS AS FOLLOWS: 1. DEOXIDIZER RESIDUE ON TANK SUBSTRATE. 2. IMPROPERLY CLEANED STAINS ON AFT DOME. 4/17/86 PRB STATUS - PROBLEM WAS CAUSED BY DEOXIDIZER RESIDUE ON TANK SUBSTRATE AND IMPROPERLY CLEANED STAINS ON AFT DOME. CORRECTIVE ACTION IS INCREASED INSPECTION POINTS AND UPDATED MAPPING PROCEDURE. CAPS IS IN CLOSURE LOOP AT MMC. 5/15/86 PRB STATUS - NO CHANGE. 6/9/86 FAILURE INVESTIGATION - THE LH2 TANK IS CLEANED AND EPOXY PRIMED IN CELL "P," BUILDING 131. AFTER THE CLEANING OPERATION, THE ENTIRE TANK IS INSPECTED FOR VISUAL CLEANLINESS, OBVIOUS STAINS, AND DISCOLORATIONS STAINS MAY BE CLEANED IMMEDIATELY PRIOR TO EPOXY PRIMER APPLICATION, OR MASKED WITH J-414 TAPE AND TOUCHED UP AFTER PRIMER APPLICATION. HISTORY OF CELL "P" SHOWS THAT MOST TANKS HAVE HAD A STAIN ANOMALY WHICH IS CAUSED BY DRIPS FROM THE CEILING, ENTRAPMENT AREAS AROUND THE 2058 ROLL RINGS, AND FLUID ENTRAPMENT IN THE MASKING MATERIAL OF THE LH2 FEEDLINE. IN BUILDING 420, THE AREA AROUND THE FEEDLINE FLANGE IS CLOSED OUT WITH PRIMER AND FOAM PER MPP. AFTER PRIMER APPLICATION, THE AREA IS WET TAPE TESTED PER STP/PI 3004. DURING THIS OPERATION ON LWT-26, PRIMER LIFT-OFF WAS NOTED ON AN AREA ADJACENT TO THE SCHEDULED CLOSEOUT. THE FAILED AREA WAS CHASED OUT UNTIL INDICATION OF GOOD ADHESION WAS NOTED. SAMPLES OF THE FAILED PRIMER WERE FORWARDED TO THE QE LAB FOR ANALYSIS. RESULTS SHOWED THAT A DEOXIDIZER RESIDUE WAS PRESENT ON THE TANK SUBSTRATE. THIS WOULD INDICATE THAT THE CAUSE OF LOW PRIMER ADHESION WAS DUE TO IMPROPER CLEANING OF STAINED AREAS ON THE TANK PRIOR TO REWORK IN BUILDING 131, CELL "P." A REVIEW OF THE BUILD LOGS FOR LWT'S 28, 29, 30, AND 31 WAS COMPLETED TO ASSURE THAT THE REPAIRS AROUND THE 2058 RING FRAME WAS INSPECTED AND TESTED RESULTS INDICATE THAT EACH VEHICLE HAD MINOR PRIMER LIFT-OFF IN THESE AREAS, AND WERE REWORKED TO DRAWING CONFIGURATION. REFERENCE DR'S D-108749, D-114563, D-114150 AND D-129442. CLEARANCE OF EFFECTIVITIES - NO CONSTRAINTS WERE PLACED ON ANY EFFECTIVITY BASED ON THE FOLLOWING RATIONALE: WET TAPE ADHESION TESTS WERE PERFORMED ON LWT'S 28, 29, 30 AND 31 IN THE SAME LOCATION WITH ONLY MINOR PRIMER FAILURE REPORTED ALL EFFECTIVITIES ARE WET TAPE TESTED PER MPP. 6/9/86 RESOLUTION - FAILURE ANALYSIS REVEALED THAT THE AREA OF LOW PRIMER ADHESION WAS ISOLATED TO THE LWT-26 LH2 FEEDLINE FLANGE, AND AN AREA CLOSE TO THE 2058 RING FRAME AT THE +Z AXIS. CORRECTIVEACTIONS IMPLEMENTED WERE IN TWO CATEGORIES: 1) FACILITY IMPROVEMENTS; AND 2) DOCUMENTATION 23 FACILITY IMPROVEMENTS INCLUDED: - REPLACING MASKING TAPE WITH BLANK OFF PLATES - ADCOATING BLIND HOLES IN THE ROLL RING - ACTIVATING NEW AUTOMATIC CEILING RINSE SYSTEM - INSTALLATION OF AUTOMATIC DRAIN SYSTEM TO REMOVE RESIDUAL WATER ON SPRAY BOOM. DOCUMENTATION CHANGES INCLUDED UPDATING THE MPP'S TO INCLUDE: - A MAPPING OF ALL STAINS ON THE TANK - INCREMENTAL BUY-OFF STEP DURING CLEANING AND REWORKING OF STAINED AREAS. ADDITIONALLY, MATERIALS ENGINEERING, AMT, AND QUALITY ENGINEERING REVIEWED THE PRESENT CLEANING METHOD FOR TOUCH UP OF STAINS AND FOUND THEM TO BE ADEQUATE. NO FURTHER RECURRENCE CONTROL ACTION IS CONSIDERED NECESSARY. RECOMMEND THIS PROBLEM REPORT BE CLOSED. 7/23/86 RESOLUTION (ADDENDUM) - THE CORRECTIVE ACTIONS IMPLEMENTED DO NOT CONSTITUTE A PROCESS CHANGE, BUT RATHER A DOCUMENTATION ENHANCEMENT MPP'S 80914005940-XXX FOR LWT-37 AND SUBS HAVE BEEN UPDATED TO INCLUDE A DETAILED MAP OF ALL STAINS AND INCREMENTAL BUY-OFFS FOR CLEANING THE STAINS. THESE CORRECTIVE ACTIONS WERE VERIFIED BY THE CAPS TEAM, INCLUDING DCAS, IN CELL "P" ON LH2 TANK, LWT-37, (REF MEMO 3741-86-076 FROM F. RAMSEY, SUPERVISOR, RELIABILITY ASSURANCE/MMC TO GEORGE MILLER/MSFC-PAS). 7/31/86 - CLOSURE CONSIDERED INADEQUATE BY ET PROJECT CHIEF ENGINEER, J. J. NICHOLS, AND WAS REJECTED PER NONCONCURRENCE LETTER EG21-PAS(NC)-86-08. 9/15/86 RESOLUTION (ADDENDUM) - RESPONSE TO NONCONFORMANCE LETTER EG21-PAS(NC)-86-08 REAFFIRMS THE CAUSE OF LOW PRIMER ADHESION AS BEING IMPROPERLY CLEANED STAINS. SOURCE OF THE STAINS WAS DRIPS FROM ENTRAPPED CLEANING SOLUTION. A REVIEW OF CELL "P" CLEANING OPERATION WAS CONDUCTED (REF MEMO 3614-86-012) TO IDENTIFY ENTRAPMENT AREAS WHICH COULD CAUSE STAINS ON THE LH2 TANK AFTER FINAL RISE AND DRY CLEANING OPERATIONS. THOSE AREAS IDENTIFIED AS STAIN CONTRIBUTORS, AND THE CORRECTIVE ACTION TAKEN, ARE LISTED BELOW ENTRAPMENT PROBLEM AREAS CORRECTIVE ACTION 1. UNUSED BLIND, THRU AND THREADED FASTNER ALL HOLES TO BE PLUGGED WITH EPOXY FILLER HOLES IN ROLL RINGS. MATERIAL. 2. BLANK-OFF PLATE 17", AND LH2 OUTLET (T26K2038). TOOLING BLANK-OFF PLATE REDESIGNED TO ADCOAT MASKING MATERIAL USED TO PROTECT ELIMINATE ALL MASKING. FIRST USE LWT-34 FASTENERS AND SEALS MATING SURFACE, SEPARATES FROM SUBSTRATE AND CREATES ENTRAPMENT AREA AROUND THE PLATE ALLOWING CLEANING SOLUTION TO ACCUMULATE INSIDE MASKANT THEN RELEASING ONTO TANK DURING DRY CYCLE. 3 ROLL RING, AND LH2 TANK INTERFACE (TEFLON SEAL). NEW STAINLESS STEEL ROLL RINGS ARE BEI CLEANING SOLUTIONS BECOME ENTRAPPED BETWEEN DESIGNED. THE INTERFACE AREA IS BEING TANK AND TOOL TEFLON SEAL INTERFACE. ADDRESSED TO REDUCE OR ELIMINATE ENTRAP- MENT AREAS. ROLL RINGS NOW HAVE INDIVIDUAL RINSE NOZZLE DIRECTED TO RINSE ENTRAPMENT AREAS, BUT ARE NOT 100% EFFECTIVE. 4. STAINLESS STEEL CEILING SEAM AREAS. INSPECTION OF SEAM AREAS IS CONDUCTED BY RESIDUAL CHEMICALS ENTRAP IN CEILING PANEL FACILITIES EVERY (6) MONTHS OR MORE OFTEN SEAM AREAS DURING CLEAN CYCLE WHICH CREATE IF A SPECIFIC FAILURE OCCURS REPAIRS ARE CONTAMINATED WATER DRIPS ON TANK DURING MADE AS REQUIRED DRY CYCLE. ALL SEAMS ARE CAULKED BUT FAILURES OCCUR WHEN CAULKING IS DISTURBED BY HIGH PRESSURE HOSE RISE ON CEILING. SEE ITEM (5). 5. DRIPS FROM ACCUMULATED CHEMICAL CONTAMINATED NEW AUTOMATIC CEILING RINSE SYSTEM TO BE WATER DROPLETS ON SURFACE OF STAINLESS STEEL INSTALLED TO PROVIDE COMPLETE CEILING CEILING, CREATED DURING CLEAN CYCLE. CEILING RINSE COVERAGE OVER THE TANK. SCHEDULED IS MANUALLY RINSED WITH HIGH PRESSURE HOSE START DATE IS 2/15/86. LESS HARSH TO REMOVE SURFACE CONTAMINATION. CLEANING PRESSURES DURING CEILING RINSE WILL REDUCE OCCURRENCE OF CAULKING REMOVAL IN CEILING SEAM AREAS IDENTIFIED IN ITEM (4). 6. ADCOAT MASKING ON MANHOLE COVER PLATES, FLEXIBLE PLASTIC COVERS WERE DESIGNED TO ELECTRICAL FEED-THROUGH COVER PLATES, AND PROTECT FASTENERS. GASKET MATERIALS ON BLANK-OFF PLATES, AND LH2 VENT TO PROTECT COVER PLATES WAS CHANGED TO VITON. FASTENERS AND SEALING SURFACES. LEAKS OCCUR FROM ADCOAT FAILURE DURING CLEAN CYCLE. 7. DRIPS FROM CLEANING SPRAY BOOM HIT TOOLING AUTOMATIC DRAIN SYSTEM INSTALLED TO REMOVE PLATFORM CREATING SPLASH ON CLEAN TANK RESIDUAL WATER LEFT IN SPRAY BOOM AFTER SURFACE. CLEANING CYCLE. TANK II OF CAPS T-050 DIRECTED ENGINEERING (MATERIAL, MANUFACTURING, QUALITY, AND AMT) TO REVIEW THE PRESENT CLEANING METHOD, WHICH WAS DONE, AND THE CLEANING METHOD WAS DETERMINED TO BE ADEQUATE IF PERFORMED CORRECTLY. IT WAS, THEREFORE, CONCLUDED THAT THE CAUSE FOR LOW PRIMER ADHESION WAS A RESULT OF EMPLOYEE ERROR, AND NOT A SUBSTANDARD CLEANING METHOD HOWEVER, TO HELP PRECLUDE THESE EMPLOYEE ERRORS, INCREMENTAL QC BUY-OFF STEPS WERE ADDED TO ENHANCE THE MPP'S, ALONG WITH MAPS FOR TRACKING THE REMAINING STAINS. RECOMMEND THIS PROBLEM REPORT BE CLOSED |  |  |  |  |  |
| MSFC Response/Concurrence |  |  |  |  |  |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A09682 | IFA# -- | Contractor RPT# T-050 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# 80974018409 | Asmnt Part Name LH2 TANK BARREL SOFI | Asmnt Serial/Lot# L2T-26 |  |  |  |
| HCRIT CD -- | FCRIT CD 1 | CAUSE CD MAW - MFG-ASY-WORK | FAIL MODE MI - INSULATION |  |  |
| Asmnt FMEA 5.2.2.1 | Asmnt FM 1 | FMEA CSE B | FMEA SCSE 8 |  |  |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |  |  |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |  |  |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |  |  |  |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |  |  |  |
| MAJOR DESIGN CHANGES |  |  |  |  |  |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |  |  |  |  |
| ASSESSMENT TEXT |  |  |  |  |  |