96M03/29/06

S403-96M.doc

Use on projects as appropriate. Include the standard 401 SCR, subsections 401.09 and 401.12.

Section 403. - HOT RECYCLED ASPHALT CONCRETE PAVEMENT

Construction Requirements

  - Composition of Mix (Job-Mix Formula).  Delete the first sentence and substitute the following:

Prepare hot recycled asphalt concrete mixes using reclaimed aggregate material, reclaimed asphalt pavement material, new aggregate, asphalt cement, recycling agent, and additives that meet the applicable aggregate gradation requirements in Table 703-4 and design parameters (a), (c), and (d) in Table 401-1 for the mix class shown in the bid schedule.

Add the following:

When antistrip additive is used, use lime.

Include only when the government does the laboratory testing.

403.06  Acceptance.  Add the following:

Provide the solvent used for determining the gradation of paving aggregate according to the Sampling and Testing Table at the end of this Section.  Use of approved maximum strength biodegradable solvents is required.  Information on the source of supply of approved solvents may be obtained by contacting the CFLHD Central Materials Laboratory at (303) 716-2176.  Approximately 7 liters of solvent will be required for each acceptance test of asphalt mixtures.  Additional quantities will be required for equipment calibration and clean up.  Do not begin paving operations until an adequate quantity of the solvent is available.  Provide a copy of the current Material Safety Data Sheet for the solvent.  Remove and dispose of the solvent after use.