MSFC PRACA : 2003-02-12 08:41

MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A17583 | In-Flight Anomaly Number -- | Contractor Report Number S-085 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title SANDED/SHAVED SLWT 2195 WELDS |
| EICN# -- | ELEMENT ET | Contractor LMMSS | FSCM# -- | FCRIT 3 |
| HCRIT 1 | Sys_Lvl -- | Misc Codes A B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE LRU | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE NCA | NOMENCLATURE 2195 WELDING | PART# STP-5507;5508;5509 | SER/LOT# N/A | MANUFACTURER MAF |
| Test/Operation MI - MFI | Prevailing Condtion N - INSPECTION | F / U UC | Fail Mode MU - MECH TOLRNCE | Cause MPP - MFG-PRC-INST |
| System STRUCTURAL | Defect MU - STRESS | Material H - WELD | Work Contact WM. MATTHEES | Fail Date 06/09/2000 |
| Received at MSFC 06/15/2000 | Date Isolated 06/09/2000 | FMEA Reference NONE | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location MAF | Symptom MU - MECH TOLRNCE | Time Cycle -- |
| Effectivity Text ET 103 AND SUBSEQUENT |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 08/15/2001 | CN RSLV SBMT -- | Defer Date -- | Add Date 06/15/2000 | R/C Codes 2 - MFG -- -- |
| Assignee |
| Design S. AVANS | Chief Engineer N. OTTE | S & MA K. LAYNE | Project -- | Project MGR J. SMELSER |
| Approval |
| Design J. KRESS | Chief Engineer N. OTTE | S & MA K. LAYNE | Project . | Project MGR J. SMELSER |
| PAC Assignee T. WHITE | PAC Review Complete TLW | MSFC Closure Date 08/14/2001 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID N046920; N046922; N046925 |
| Related Document Title -- |
| Related Document Type -- | Related Document ID N046968; N046999;N051137 |
| Related Document Title -- |
| Related Document Type -- | Related Document ID N051166; N051183; N051201 |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description THE WELD REINFORCEMENT BEAD ON SLWT WELDS USING 4043 FILLER METAL MAY CURRENTLY BE SHAVED/SANDED DOWN TO THE 0.040" MINIMUM HEIGHT REQUIREMENT WITHOUT MAINTAINING THE INTENDED WELD BEAD PROFILE. CRITICALITY: ------------ THIS IS A DISCRETIONARY CAPS.THIS CONDITION DID NOT RESULT IN A FAILURE. REVISION F: REFER TO ASTERISK (*) FOR CHANGES; CLOSED TASKS I.G, .III, & IV |
| Contractor Investigation/Resolution GENERAL: -------- THE INVESTIGATION OF THIS PROBLEM WAS INITIATED FROM A NEQA CATEGORY-1 FINDING. DURING NORMAL PRODUCTION OPERATIONS, WELD SURFACE DEFECTS WERE NOTED AT THE BASE OF THE ROOT/CROWN REINFORCEMENT AT VARIOUS AREAS ALONG THE WELD BEAD. THE WELD REINFORCEMENT BEAD WAS DRESSED TO REMOVE THE SURFACE INDICATIONS BY GRINDING THE WELD BEAD. THE DEFECTS WERE SUCCESSFULLY REMOVED, AND THE MINIMUM BEAD HEIGHT WAS MAINTAINED. HOWEVER, THE REMOVAL OF THE TOE EXPOSED THE FUSION LINES WHICH MAY HAVE VIOLATED THE INTENT OF THE POST-WELD DIMENSIONAL REQUIREMENTS OF STP-5507/5508/5509 PARAGRAPH 3.3.2. AS A TEMPORARY MEASURE, OD #000396 AND PRODUCTION TIP #151 WERE ISSUED STATING THAT ALL DRESSING OF WELD BEADS SHALL BE RECORDED ON AN NCD UNTIL A LONG TERM CRITERIA HAS BEEN DEVELOPED. THIS PROBLEM DOES NOT EFFECT LIGHTWEIGHT VEHICLES SINCE THE ALLOWABLES DO NOT DECREASE ON SHAVING WELD BEADS FOR 2219 ALUMINUM WELDS. TASK I FAILURE/PROBLEM INVESTIGATION: A. GENERATE SUSPECT NCDS FOR VIOLATING THE INTENT OF ENGINEERING REQUIREMENTS FOR ET-112 LO2, AND ET-103 THRU ET-111. PRIORITY SHALL BE ET-104, ET-110, ET-103, ET-105. RESPONSIBILITY: J. SPRAY - 3724 / D. OWENS - 3720 ECD: 6/23/00 COMPLETE: 6/21/00 CLOSURE STATEMENT REVIEW OF ET-103 THRU ET-112 LO2 WELD DATA HAS BEEN COMPLETED, AND SUSPECT NCDS WERE GENERATED FOR EACH TANK. (SEE APPENDIX 1) B. PROVIDE DISPOSITION/DEVELOP FLEET CLEARANCE RATIONALE FOR ALL AFFECTED TANKS. RESPONSIBILITY: G. WADGE - 4420 / E. SWEET - 4400 - DISPOSITION NCDS ECD: 6/23/00 EXTENSION: 8/4/00 EXTENSION: 11/30/00 COMPLETE: 12/6/00 CLOSURE STATEMENT ET-103 THRU ET-112 CLEARANCE HAS BEEN COMPLETED AND DOCUMENTED ON NCDS ("USE-AS-IS"). (SEE APPENDIX 1 FOR NCD NUMBERS) REF. DISCREPANT WELD BEAD PROFILE 12/5/00 D. BOLSTAD ET-113 AND SUBSEQUENT, STPS REVISED TO NOT ALLOW BEAD SHAVING WITHOUT MRB AUTHORITY. REF. DISCREPANT WELD BEAD PROFILE 12/5/00 D. BOLSTAD C. PERFORM INSPECTION OF SUSPECT AREAS AND DOCUMENT RESULTS ON NCDS FOR ET-112 LH2, ET-113 LO2, AND ET-114 LO2. RESPONSIBILITY: J. SPRAY - 3724 / D. OWENS - 3720 ECD: 6/23/00 COMPLETE: 6/30/00 CLOSURE STATEMENT INSPECTION OF ET-112 LH2, ET-113 LO2, AND ET-114 LO2 HAS BEEN COMPLETED AND DOCUMENTED ON NCDS. (REFERENCE APPENDIX 1) D. GENERATE A LIAISON CALL AGAINST STP-5507/5508/5509. RESPONSIBILITY: H. MCPEEK - 3614 / R. WEAVER - 3614 ECD: 6/23/00 COMPLETE: 6/9/00 CLOSURE STATEMENT THE FOLLOWING LI-CALLS HAVE BEEN ANSWERED REMOVING SAND/GRIND CAPABILITY FROM THE STPS: M340-1271 AGAINST STP-5507 M340-1272 AGAINST STP-5508 M340-1273 AGAINST STP-5509 E. PROVIDE RESPONSE TO CLARIFY/ELIMINATE THE MISINTERPRETATION OF DRESSING THE WELDS. (REFERENCE LIAISON CALL IN ITEM D.) RESPONSIBILITY: F. OGDEN - 4630 / P. HINKELDEY - 4600 E. SWEET - 4400 ECD: 6/23/00 COMPLETE: 6/13/00 CLOSURE STATEMENT STP-5507/5508/5509 PARAGRAPH 3.4.8.1.1 IS REVISED SO THAT ALL SANDING, SHAVING, AND/OR GRINDING OF WELD BEADS TO REMOVE DEFECTS SHALL REQUIRE PRIOR MRB APPROVAL. (REFERENCE LI-CALLS M340-1271, M340-1272, AND M340-1273) F. INSPECT TWO ET EQUIVALENCIES FOR THIS SHAVING PROBLEM, AND DOCUMENT SUSPECT CONDITIONS ON NCDS. PROVIDE A MATRIX OF INSPECTED HARDWARE TO RELIABILITY ASSURANCE. RESPONSIBILITY: J. SPRAY - 3724 / D. OWENS - 3720 ECD: 6/23/00 CANCELLED: 7/13/00 CANCELLATION STATEMENT REVIEW OF THE INITIAL DATA SHOWS THAT THIS REWORK WAS FAIRLY EXTENSIVE AND WAS NOT WELL DOCUMENTED ON THE QE WELD SHEETS; THEREFORE, THIS TASK IS CANCELLED AND A COMPLETE INSPECTION OF ALL HARDWARE BUILT PRIOR TO THE IMPLEMENTATION OF OD #000396 IS REQUIRED. THE INSPECTION IS BEING TRACKED IN ITEM "K". (REFERENCE E-MAIL FROM D. OWENS 6/20/00.) * G. DEVELOP A LONG TERM WELD BEAD SHAVING CRITERIA WHICH INCLUDES AN SRI. RESPONSIBILITY: F. OGDEN - 4630 / P. HINKELDEY - 4600 ECD: 7/23/00 EXTENSION: 12/22/00 EXTENSION: 2/9/01 EXTENSION: 4/06/01 THIS TASK IS OPEN STATUS A LONG TERM PLAN HAS BEEN DEVELOPED TO ADDRESS THE WELD BEAD SHAVING PROBLEM. THE PLAN WILL DETERMINE POST SANDING NDE REQUIREMENTS AND THEN UPDATE STP-5507, STP-5508, STP-5509 AND DRAWING #80900000069. (REFERENCE 'RESOLUTION OF WELD BEAD DRESSING' BY D. BOLSTAD 8/14/00.) H. MANUFACTURING ENGINEERING TO REDLINE MPPS RELEASED TO THE PRODUCTION FLOOR TO DELETE THE PERMISSION OF WELD DRESSING, AND LOCKOUT (FREEZE) THE FUTURE RELEASE OF MPPS THAT PERMITS WELD DRESSING. RESPONSIBILITY: H. MCPEEK - 3614 / R. WEAVER - 3614 ECD: 6/14/00 COMPLETE: 6/23/00 CLOSURE STATEMENT FUTURE MPPS HAVE BEEN LOCKED OUT FROM BEING RELEASED. THEY WILL BE RELEASE UPON REVISION TO CURRENT DRESSING REQUREMENTS. (REFERENCE E-MAIL FROM R. WEAVER 6/23/00) I. FOR ET-103 AND ET-104, PROVIDE PEAKING AND MISMATCH DATA OF THE FOLLOWING WELDS TO TECHNICAL OPERATIONS: H2, H3, H6, H7, H8, HADC, HAF, HAG, HB, HFDC, HFF, HFG, OADC, OAO, OB. RESPONSIBILITY: J. SPRAY - 3724 / D. OWENS - 3720 ECD: 6/23/00 COMPLETE: 6/12/00 CLOSURE STATEMENT DATA WAS OBTAINED AND PROVIDED TO PTS. (G. WADGE - 4420, REFERENCE E-MAIL FROM P. POWELL 6/12/00.) J. IDENTIFY WHICH WELDS REQUIRE VISUAL INSPECTION. RESPONSIBILITY: D. BOLSTAD - 4600 / P. HINKELDEY - 4600 ECD: 6/23/00 COMPLETE: 7/12/00 CLOSURE STATEMENT SEE APPENDIX 2. K INSPECT ALL HARDWARE BUILT PRIOR TO IMPLEMENTATION OF OD #000396, AND DOCUMENT SUSPECT CONDITIONS ON NCDS. PROVIDE A MATRIX OF INSPECTED HARDWARE TO RELIABILITY ASSURANCE. RESPONSIBILITY: J. SPRAY - 3724 / D. OWENS - 3720 ECD: 8/4/00 EXTENSION: 9/4/00 COMPLETE: 9/1/00 CLOSURE STATEMENT ALL HARDWARE HAS BEEN INSPECTED & NCDS WERE GENERATED AS NEEDED (REFERENCE APPENDIX 1), REF: EMAIL J. SPRAY 9/27/00 CAUSE: ENGINEERING'S INTENT (FOR WELD BEAD PROFILE) WAS NOT ADEQUATELY INSTITUTIONALIZED IN MANUFACTURING WORK DOCUMENTS, NOR PROPERLY IMPLEMENTED BY WELDING PRACTITIONER. TASK II CORRECTIVE ACTIONS: UNDER INVESTIGATION THIS TASK IS OPEN TASK III CLEARANCE OF EFFECTIVITIES: * ET-103 THRU ET-112 CLEARANCE HAS BEEN COMPLETED AND DOCUMENTED ON NCDS. ("USE-AS-IS"). (SEE APPENDIX 1 FOR NCD NUMBERS.) & REF. DISCREPANT WELD BEAD PROFILE 12/5/00 D. BOLSTAD * ET-113 AND SUBSEQUENT, STPS REVISED TO NOT ALLOW BEAD SHAVING WITHOUT MRB AUTHORITY. REF. DISCREPANT WELD BEAD PROFILE 12/5/00 D. BOLSTAD THIS TASK IS CLOSED TASK IV CAPS CLOSURE SUMMARY: THIS TASK IS OPEN THIS IS AN OPEN CAPS. SEE TASKS I THRU IV APPENDIX 1 EFF REMARKS/PLAN/STATUS NCD ET-103 QE WELD/P&MM DATA COMPILED N051137-CLOSED ET-104 QE WELD/P&MM DATA COMPILED N051201-CLOSED ET-105 QE WELD/P&MM DATA COMPILED N051204-CLOSED ET-106 QE WELD/P&MM DATA COMPILED N051203-CLOSED ET-107 QE WELD/P&MM DATA COMPILED N051230-CLOSED ET-108 QE WELD/P&MM DATA COMPILED N051215-CLOSED ET-109 QE WELD/P&MM DATA COMPILED N051231-CLOSED ET-110 QE WELD/P&MM DATA COMPILED N051214-CLOSED ET-111 QE WELD/P&MM DATA COMPILED N051232-CLOSED ET-112 LO QE WELD/P&MM DATA COMPILED N051224-CLOSED ET-112 LH AFT DOME @ 5019 INSPECTION COMPLETE N051240-CLOSED BARREL 1 @ 5019 INSPECTION COMPLETE N051240-CLOSED BARREL 2 @ 5019 INSPECTION COMPLETE N051240-CLOSED BARREL 3 @ 5019 INSPECTION COMPLETE N051240-CLOSED BARREL 4 INSPECTION COMPLETE/ N051216-CLOSED DATA COMPILED FWD DOME AS BUILT ET-105R N051208-CLOSED ET-113 LO @ 7419 INSPECTION COMPLETE N051202-CLOSED DATA COMPILED ET-113 LH AFT DOME- @ 5128 INSPECTION COMPLETE/ N046920-CLOSED DATA COMPILED BARREL 1 AS BUILT ET-112 (NEQA FINDING) N051207-CLOSED DATA COMPILED BARREL 2 AS BUILT ET-112 INSPECTION N051210-CLOSED COMPLETE/DATA COMPILED BARREL 3 INSPECTION COMPLETE/ N051212-CLOSED DATA COMPILED N/A BARREL 4 INSPECTION COMPLETE (NO DRESSING PERFORMED) FWD DOME (GORES & FRAME) INSPECTION N046925-CLOSED COMPLETE/DATA COMPILED HFDC WORK/INSP. PER O.D. N/A ET-114 LO @ 7023 01-04 & SUBASSY @ 5018 INSPECTION N051218-CLOSED COMPLETE/DATA COMPILED 05 WORK/INSP. PER O.D. N/A ET-114 LH AFT DOME-MECH ASSY INSPECTION COMPLETE N051222-CLOSED BARREL 1 INSPECTION COMPLETE/ N051209-CLOSED DATA COMPILED BARREL 2 INSPECTION COMPLETE/ N051211-CLOSED DATA COMPILED BARREL 3 INSPECTION COMPLETE/ N051213-CLOSED DATA COMPLIED BARREL 4 @ 5016 WORK/INSP. PER O.D. N/A FWD DOME (GORES & FRAME) N046999-CLOSED HFDC WORK/INSP. PER O.D. N/A ET-115 LO @ 5347 01-04, FWD, AFT & BARREL INSPECTION N051217-CLOSED COMPLETE/DATA COMPILED DOME INSPECTION COMPLETE/DATA COMPILED N051226-CLOSED 05 WORK/INSP. PER O.D. N/A ET-115 LH AFT DOME GORES & FRAME INSPECTION COMPLETE/ N046922-CLOSED DATA COMPILING I/W HADC WORK/INSP. PER O.D. N/A BARREL 1 FABRICATION NOT STARTED-WORK/O.D. N/A BARREL 2 FABRICATION NOT STARTED-WORK/O.D. N/A BARREL 3 FABRICATION NOT STARTED-WORK/O.D. N/A BARREL 4 FABRICATION NOT STARTED-WORK/O.D. N/A FWD DOME (GORES & FRAME) INSPECTION N051879-CLOSED COMPLETE DATA COMPILED HFDC WORK/INSP. PER O.D. N/A ET-116 LO FWD OGIVE @ 5186 INSPECTION COMPLETE/ N051219-CLOSED DATA COMPILED AFT OGIVE @ COL G2 INSPECTION COMPLETE N051183-CLOSED BARREL WORK/INSP. PER O.D. N/A DOME (GORES & FRAME) INSPECTION N051880-CLOSED COMPLETE/DATA COMPILED OADC WORK/INSP. PER O.D. N/A ET-116 LH AFT DOME (GORES & FRAME) INSPECTION COMPLETE N046968-CLOSED HADC WORK/INSP. PER O.D. N/A FWD DOME (GORES) INSPECTION COMPLETE N/A (NO DRESSING PERFORMED) HFF WORK/INSP. PER O.D. N/A HFDC WORK/INSP. PER O.D. N/A BARRELS 1-4 FABRICATION NOT STARTED- N/A WORK/O.D. ET-117 LO FWD OGIVE @ 5012 WORK/INSP. PER O.D. N051166-CLOSED LESS OFO-4 (REBUILD) AFT OGIVE @ 5024 WORK/INSP. PER O.D. N/A BARREL FABRICATION NOT STARTED-WORK/O.D. N/A DOME (GORES & FRAME) INSPECTION COMPLETE N/A (NO DRESSING PERFORMED) OADC WORK/INSP. PER O.D. N/A ET-117 LH AFT DOME (GORES & FRAME) INSPECTION N054151-CLOSED COMPLETE HADC WORK/INSP. PER O.D. N/A BARRELS 1-4 FABRICATION NOT STARTED- N/A WORK/O.D. FWD DOME WORK/INSP. PER O.D. N/A ET-118 LO FWD OGIVE FABRICATION NOT STARTED- N/A WORK/O.D. AFT OGIVE FABRICATION NOT STARTED- N/A WORK/O.D. BARREL FABRICATION NOT STARTED-WORK/O.D. N/A DOME FABRICATION NOT STARTED-WORK/O.D. N/A ET-118 LH AFT DOME (GORES & FRAME) HADC WORK/INSP. PER O.D. N/A BARRELS 1-4 FABRICATION NOT STARTED- N/A WORK/O.D. FWD DOME FABRICATION NOT STARTED- N/A WORK/O.D. ET-119 & SUBSEQUENT BUILDS WORK/INSP. PER O.D. N/A * APPENDIX 2 WELD LOCATION CLEARANCE RATIONALE O1 DESIGN LOAD ASSESSMENT OFO PROOF TEST DEMONSTRATION O2 PROOF TEST DEMONSTRATION OAO REQUIRES VISUAL INSPECTION O3 DESIGN LOAD ASSESSMENT OT 2219 WELD O4 DESIGN LOAD ASSESSMENT OB REQUIRES VISUAL INSPECTION O5 DESIGN LOAD ASSESSMENT OAF DESIGN LOAD ASSESSMENT ODG DESIGN LOAD ASSESSMENT OADC REQUIRES VISUAL INSPECTION OAL 2219 WELD OMH 2219 WELD HFM 2219 WELD HFE 2219 WELD HFV 2219 WELD HFDC REQUIRES VISUAL INSPECTION HFF REQUIRES VISUAL INSPECTION HFG REQUIRES VISUAL INSPECTION H8 REQUIRES VISUAL INSPECTION HB -ALL REQUIRES VISUAL INSPECTION HT -ALL 2219 WELD H7 REQUIRES VISUAL INSPECTION H6 REQUIRES VISUAL INSPECTION H5 REQUIRES VISUAL INSPECTION H4 REQUIRES VISUAL INSPECTION H3 REQUIRES VISUAL INSPECTION H2 REQUIRES VISUAL INSPECTION H1 REQUIRES VISUAL INSPECTION HAF REQUIRES VISUAL INSPECTION HAG REQUIRES VISUAL INSPECTION HADC PROOF TEST DEMONSTRATION HAM 2219 WELD HSP 2219 WELD 07/19/2001 - CONTRACTOR SUBMITTED PROBLEM CLOSURE REQUEST AS FOLLOWS: GENERAL: THE INVESTIGATION OF THIS PROBLEM WAS INITIATED FROM A NEQA MARGIN CATEGORY-1 FINDING. DURING NORMAL PRODUCTION OPERATIONS, WELD SURFACE DEFECTS WERE NOTED AT THE BASE OF THE ROOT/CROWN REINFORCEMENT AT VARIOUS AREAS ALONG THE WELD BEAD. THE WELD REINFORCEMENT BEAD WAS DRESSED TO REMOVE THE SURFACE INDICATIONS BY GRINDING THE WELD BEAD. THE DEFECTS WERE SUCCESSFULLY REMOVED, AND THE MINIMUM BEAD HEIGHT WAS MAINTAINED. HOWEVER, THE REMOVAL OF THE TOE EXPOSED THE FUSION LINES WHICH MAY HAVE VIOLATED THE INTENT OF THE POST-WELD DIMENSIONAL REQUIREMENTS OF STP-5507/5508/5509 PARAGRAPH 3.3.2. GENERAL: -------- THE INVESTIGATION OF THIS PROBLEM WAS INITIATED FROM A NEQA MARGIN CATEGORY-1 FINDING. DURING NORMAL PRODUCTION OPERATIONS, WELD SURFACE DEFECTS WERE NOTED AT THE BASE OF THE ROOT/CROWN REINFORCEMENT AT VARIOUS AREAS ALONG THE WELD BEAD. THE WELD REINFORCEMENT BEAD WAS DRESSED TO REMOVE THE SURFACE INDICATIONS BY GRINDING THE WELD BEAD. THE DEFECTS WERE SUCCESSFULLY REMOVED, AND THE MINIMUM BEAD HEIGHT WAS MAINTAINED. HOWEVER, THE REMOVAL OF THE TOE EXPOSED THE FUSION LINES WHICH MAY HAVE VIOLATED THE INTENT OF THE POST-WELD DIMENSIONAL REQUIREMENTS OF STP-5507/5508/5509 PARAGRAPH 3.3.2. AS A TEMPORARY MEASURE, OD #000396 AND PRODUCTION TIP #151 WERE ISSUED STATING THAT ALL DRESSING OF WELD BEADS SHALL BE RECORDED ON AN NCD UNTIL A LONG TERM CRITERIA HAS BEEN DEVELOPED. THIS PROBLEM DOES NOT EFFECT LIGHTWEIGHT VEHICLES SINCE THE ALLOWABLES DO NOT DECREASE ON SHAVING WELD BEADS FOR 2219 ALUMINUM WELDS. TASK I FAILURE/PROBLEM INVESTIGATION: ----------------------------- A. GENERATE SUSPECT NCDS FOR VIOLATING THE INTENT OF ENGINEERING REQUIREMENTS FOR ET-112 LO2, AND ET-103 THRU ET-111. PRIORITY SHALL BE ET-104, ET-110, ET-103, ET-105. RESPONSIBILITY: J. SPRAY - 3724/D. OWENS - 3720 ECD: 6/23/00 COMPLETE: 6/21/00 CLOSURE STATEMENT ----------------- REVIEW OF ET-103 THRU ET-111 & THE LO2 TANK FOR ET-112 WELD DATA HAS BEEN COMPLETED, AND SUSPECT NCDS WERE GENERATED FOR EACH TANK. (SEE APPENDIX 1) B. PROVIDE DISPOSITION/DEVELOP FLEET CLEARANCE RATIONALE FOR ALL AFFECTED TANKS. RESPONSIBILITY: G. WADGE - 4420/E. SWEET-4400 - DISPOSITION NCDS ECD: 6/23/00 EXTENSION: 8/4/00 EXTENSION: 11/30/00 COMPLETE: 12/6/00 CLOSURE STATEMENT ----------------- ET-103 THRU ET-112 CLEARANCE HAS BEEN COMPLETED AND DOCUMENTED ON NCDS ("USE-AS-IS"). (SEE APPENDIX 1 FOR NCD NUMBERS) REF. DISCREPANT WELD BEAD PROFILE 12/5/00 D. BOLSTAD ET-113 AND SUBSEQUENT, STPS REVISED TO NOT ALLOW BEAD SHAVING WITHOUT MRB AUTHORITY. REF. DISCREPANT WELD BEAD PROFILE 12/5/00 D. BOLSTAD C. PERFORM INSPECTION OF SUSPECT AREAS AND DOCUMENT RESULTS ON NCDS FOR ET-112 LH2, ET-113 LO2, AND ET-114 LO2. RESPONSIBILITY: J. SPRAY - 3724/D. OWENS - 3720 ECD: 6/23/00 COMPLETE: 6/30/00 CLOSURE STATEMENT ----------------- INSPECTION OF ET-112 LH2, ET-113 LO2, AND ET-114 LO2 HAS BEEN COMPLETED AND DOCUMENTED ON NCDS. (REFERENCE APPENDIX 1) D. GENERATE A LIAISON CALL AGAINST STP-5507/5508/5509. RESPONSIBILITY: H. MCPEEK - 3614/R. WEAVER - 3614 ECD: 6/23/00 COMPLETE: 6/9/00 CLOSURE STATEMENT ----------------- THE FOLLOWING LI-CALLS HAVE BEEN ANSWERED REMOVING SAND/GRIND CAPABILITY FROM THE STPS: M340-1271 AGAINST STP-5507 M340-1272 AGAINST STP-5508 M340-1273 AGAINST STP-5509 E. PROVIDE RESPONSE TO CLARIFY/ELIMINATE THE MISINTERPRETATION OF DRESSING THE WELDS. (REFERENCE LIAISON CALL IN ITEM D.) RESPONSIBILITY: F. OGDEN - 4630/P. HINKELDEY - 4600 E. SWEET - 4400 ECD: 6/23/00 COMPLETE: 6/13/00 CLOSURE STATEMENT ----------------- STP-5507/5508/5509 PARAGRAPH 3.4.8.1.1 IS REVISED SO THAT ALL SANDING, SHAVING, AND/OR GRINDING OF WELD BEADS TO REMOVE DEFECTS SHALL REQUIRE PRIOR MRB APPROVAL. (REFERENCE LI-CALLS M340-1271, M340-1272, AND M340-1273) F. INSPECT TWO ET EQUIVALENCIES FOR THIS SHAVING PROBLEM, AND DOCUMENT SUSPECT CONDITIONS ON NCDS. PROVIDE A MATRIX OF INSPECTED HARDWARE TO RELIABILITY ASSURANCE. RESPONSIBILITY: J. SPRAY - 3724/D. OWENS - 3720 ECD: 6/23/00 CANCELLED: 7/13/00 CANCELLATION STATEMENT ---------------------- REVIEW OF THE INITIAL DATA SHOWS THAT THIS REWORK WAS FAIRLY EXTENSIVE AND WAS NOT WELL DOCUMENTED ON THE QE WELD SHEETS; THEREFORE, THIS TASK IS CANCELLED AND A COMPLETE INSPECTION OF ALL HARDWARE BUILT PRIOR TO THE IMPLEMENTATION OF OD #000396 IS REQUIRED. THE INSPECTION IS BEING TRACKED IN ITEM "K". (REFERENCE E-MAIL FROM D. OWENS 6/20/00.) * G. DEVELOP A LONG TERM WELD BEAD SHAVING CRITERIA WHICH INCLUDES AN SRI. RESPONSIBILITY: F. OGDEN - 4630/P. HINKELDEY - 4600 ECD: 7/23/00 EXTENSION: 12/22/00 EXTENSION: 2/9/01 EXTENSION: 4/06/01 EXTENSION: 5/11/01 - PACKAGE RELEASE #J31219 FROM N. BUTE EXTENSION: 8/10/01 COMPLETE: 7/17/01 CLOSURE STATEMENT: ------------------ A LONG TERM PLAN HAS BEEN DEVELOPED & IMPLEMENTED TO ADDRESS THE WELD BEAD SHAVING PROBLEM. WELD BEAD SHAVING REQUIREMENTS BASED ON LOCATION AND WELD GEOMETRY HAVE BEEN GENERATED. STP- 5507, STP-5508, STP-5509 AND DRAWING #80900000069 ARE BEING REVISED TO INCORPORATE THESE CHANGES (#J31219). REFERENCE # J31219 H. MANUFACTURING ENGINEERING TO REDLINE MPPS RELEASED TO THE PRODUCTION FLOOR TO DELETE THE PERMISSION OF WELD DRESSING, AND LOCKOUT (FREEZE) THE FUTURE RELEASE OF MPPS THAT PERMITS WELD DRESSING. RESPONSIBILITY: H. MCPEEK - 3614/R. WEAVER - 3614 ECD: 6/14/00 COMPLETE: 6/23/00 CLOSURE STATEMENT ----------------- FUTURE MPPS HAVE BEEN LOCKED OUT FROM BEING RELEASED. THEY WILL BE RELEASE UPON REVISION TO CURRENT DRESSING REQUIREMENTS. (REFERENCE E-MAIL FROM R. WEAVER 6/23/00) I. FOR ET-103 AND ET-104, PROVIDE PEAKING AND MISMATCH DATA OF THE FOLLOWING WELDS TO TECHNICAL OPERATIONS: H2, H3, H6, H7, H8, HADC, HAF, HAG, HB, HFDC, HFF, HFG, OADC, OAO, OB. RESPONSIBILITY: J. SPRAY - 3724/D. OWENS - 3720 ECD: 6/23/00 COMPLETE: 6/12/00 CLOSURE STATEMENT ----------------- DATA WAS OBTAINED AND PROVIDED TO PTS. (G. WADGE - 4420, REFERENCE E-MAIL FROM P. POWELL 6/12/00.) J. IDENTIFY WHICH WELDS REQUIRE VISUAL INSPECTION. RESPONSIBILITY: D. BOLSTAD - 4600/P. HINKELDEY - 4600 ECD: 6/23/00 COMPLETE: 7/12/00 CLOSURE STATEMENT ----------------- SEE APPENDIX 2. K INSPECT ALL HARDWARE BUILT PRIOR TO IMPLEMENTATION OF OD #000396,AND DOCUMENT SUSPECT CONDITIONS ON NCDS. PROVIDE A MATRIX OF INSPECTED HARDWARE TO RELIABILITY ASSURANCE. RESPONSIBILITY: J. SPRAY - 3724/D. OWENS - 3720 ECD: 8/4/00 EXTENSION: 9/4/00 COMPLETE: 9/1/00 CLOSURE STATEMENT ----------------- ALL HARDWARE HAS BEEN INSPECTED & NCDS WERE GENERATED AS NEEDED (REFERENCE APPENDIX 1), REF: EMAIL J. SPRAY 9/27/00 CAUSE: ENGINEERING'S INTENT (FOR WELD BEAD PROFILE) WAS NOT ADEQUATELY INSTITUTIONALIZED IN MANUFACTURING WORK DOCUMENTS, NOR PROPERLY IMPLEMENTED BY WELDING PRACTITIONER. * TASK II CORRECTIVE ACTIONS: ------------------ O STP-5507, STP-5508, & STP-5509 REVISED TO DELETE AND/GRIND CAPABILITY WITHOUT MRB AUTHORITY. (IMMEDIATE) O STP-5507, STP-5508, STP-5509, & 80900000069 REVISED TO ALLOW FOR LIMITED SAND/GRIND CAPABILITY WITHOUT MRB AUTHORITY. (LONG TERM) THIS TASK IS CLOSED ------------------- TASK III CLEARANCE OF EFFECTIVITIES: --------------------------- O ET-103 THRU ET-112 CLEARANCE HAS BEEN COMPLETED AND DOCUMENTED ON NCDS. ("USE-AS-IS"). (SEE APPENDIX 1 FOR NCD NUMBERS.) & REF. DISCREPANT WELD BEAD PROFILE 12/5/00 D. BOLSTAD O ET-113 AND SUBSEQUENT, STPS REVISED TO NOT ALLOW BEAD SHAVING WITHOUT MRB AUTHORITY. REF. DISCREPANT WELD BEAD PROFILE 12/5/00 D. BOLSTAD THIS TASK IS CLOSED ------------------- * TASK IV CAPS CLOSURE SUMMARY: --------------------- DURING A NEQA AUDIT, A CATEGORY-1 FINDING WAS GENERATED FOR SLWT 2195 WELDS THAT UTILIZE 4043 WELD MATERIAL. THE PROPER WELD BEAD GEOMETRY WAS NOT BEING MAINTAINED AFTER THE WELD HAD BEEN SHAVED/SANDED TO REMOVE DEFECTS. THE REQUIREMENT WAS TO HAVE A UNIFORM 0.040" MINIMUM HEIGHT OVER THE BASE METAL. THIS REQUIREMENT WAS BASED ON THE FACT THAT WELDS WITH LESS REINFORCEMENT HAD LOWER MECHANICAL PROPERTY ALLOWABLES THAN "UNSHAVED WELDS". LIGHTWEIGHT VEHICLES ARE NOT AFFECTED SINCE THIS EFFECT DOES NOT OCCUR ON 2219 MATERIAL. A REVIEW WAS CONDUCTED WHICH DETERMINED THAT THIS WAS AN EXTENSIVE NON-DOCUMENTED PRACTICE. ALL AFFECTED TANKS WERE CLEARED BY WAY OF NCDS AND ENGINEERING ANALYSIS. THE MPPS AND STPS WERE REVISED TO REMOVE THE SAND/GRIND CAPABILITY WITHOUT MRB AUTHORITY. ENGINEERING THEN EVALUATED AND DETERMINED THAT WITH CERTAIN WELD LOCATIONS AND WELD BEAD GEOMETRY, A LIMITED AND RESTRICTED AMOUNT OF SAND/GRINDING COULD BE ALLOWED WITHOUT MRB AUTHORITY. THIS TASK IS CLOSED ------------------- APPENDIX 1 EFF REMARKS/PLAN/STATUS NCD ET-103 QE WELD/P&MM DATA COMPILED N051137-CLOSED ET-104 QE WELD/P&MM DATA COMPILED N051201-CLOSED ET-105 QE WELD/P&MM DATA COMPILED N051204-CLOSED ET-106 QE WELD/P&MM DATA COMPILED N051203-CLOSED ET-107 QE WELD/P&MM DATA COMPILED N051230-CLOSED ET-108 QE WELD/P&MM DATA COMPILED N051215-CLOSED ET-109 QE WELD/P&MM DATA COMPILED N051231-CLOSED ET-110 QE WELD/P&MM DATA COMPILED N051214-CLOSED ET-111 QE WELD/P&MM DATA COMPILED N051232-CLOSED ET-112 LO QE WELD/P&MM DATA COMPILED N051224-CLOSED ET-112 LH AFT DOME @ 5019 INSPECTION COMPLETE N051240-CLOSED BARREL 1 @ 5019 INSPECTION COMPLETE N051240-CLOSED BARREL 2 @ 5019 INSPECTION COMPLETE N051240-CLOSED BARREL 3 @ 5019 INSPECTION COMPLETE N051240-CLOSED BARREL 4 INSPECTION COMPLETE/ N051216-CLOSED DATA COMPILED FWD DOME AS BUILT ET-105R N051208-CLOSED ET-113 LO @ 7419 INSPECTION COMPLETE N051202-CLOSED DATA COMPILED ET-113 LH AFT DOME- @ 5128 INSPECTION COMPLETE/ N046920-CLOSED DATA COMPILED BARREL 1 AS BUILT ET-112 (NEQA FINDING) N051207-CLOSED DATA COMPILED BARREL 2 AS BUILT ET-112 INSPECTION N051210-CLOSED COMPLETE/DATA COMPILED BARREL 3 INSPECTION COMPLETE/ N051212-CLOSED DATA COMPILED N/A BARREL 4 INSPECTION COMPLETE (NO DRESSING PERFORMED) FWD DOME (GORES & FRAME) INSPECTION N046925-CLOSED COMPLETE/DATA COMPILED HFDC WORK/INSP. PER O.D. N/A ET-114 LO @ 7023 01-04 & SUBASSY @ 5018 INSPECTION N051218-CLOSED COMPLETE/DATA COMPILED 05 WORK/INSP. PER O.D. N/A ET-114 LH AFT DOME-MECH ASSY INSPECTION COMPLETE N051222-CLOSED BARREL 1 INSPECTION COMPLETE/ N051209-CLOSED DATA COMPILED BARREL 2 INSPECTION COMPLETE/ N051211-CLOSED DATA COMPILED BARREL 3 INSPECTION COMPLETE/ N051213-CLOSED DATA COMPLIED BARREL 4 @ 5016 WORK/INSP. PER O.D. N/A FWD DOME (GORES & FRAME) N046999-CLOSED HFDC WORK/INSP. PER O.D. N/A ET-115 LO @ 5347 01-04, FWD, AFT & BARREL INSPECTION N051217-CLOSED COMPLETE/DATA COMPILED DOME INSPECTION COMPLETE/DATA COMPILED N051226-CLOSED 05 WORK/INSP. PER O.D. N/A ET-115 LH AFT DOME GORES & FRAME INSPECTION COMPLETE/ N046922-CLOSED DATA COMPILING I/W HADC WORK/INSP. PER O.D. N/A BARREL 1 FABRICATION NOT STARTED-WORK/O.D. N/A BARREL 2 FABRICATION NOT STARTED-WORK/O.D. N/A BARREL 3 FABRICATION NOT STARTED-WORK/O.D. N/A BARREL 4 FABRICATION NOT STARTED-WORK/O.D. N/A FWD DOME (GORES & FRAME) INSPECTION N051879-CLOSED COMPLETE DATA COMPILED HFDC WORK/INSP. PER O.D. N/A ET-116 LO FWD OGIVE @ 5186 INSPECTION COMPLETE/ N051219-CLOSED DATA COMPILED AFT OGIVE @ COL G2 INSPECTION COMPLETE N051183-CLOSED BARREL WORK/INSP. PER O.D. N/A DOME (GORES & FRAME) INSPECTION N051880-CLOSED COMPLETE/DATA COMPILED OADC WORK/INSP. PER O.D. N/A ET-116 LH AFT DOME (GORES & FRAME) INSPECTION COMPLETE N046968-CLOSED HADC WORK/INSP. PER O.D. N/A FWD DOME (GORES) INSPECTION COMPLETE N/A (NO DRESSING PERFORMED) HFF WORK/INSP. PER O.D. N/A HFDC WORK/INSP. PER O.D. N/A BARRELS 1-4 FABRICATION NOT STARTED- N/A WORK/O.D. ET-117 LO FWD OGIVE @ 5012 WORK/INSP. PER O.D. N051166-CLOSED LESS OFO-4 (REBUILD) AFT OGIVE @ 5024 WORK/INSP. PER O.D. N/A BARREL FABRICATION NOT STARTED-WORK/O.D. N/A DOME (GORES & FRAME) INSPECTION COMPLETE N/A (NO DRESSING PERFORMED) OADC WORK/INSP. PER O.D. N/A ET-117 LH AFT DOME (GORES & FRAME) INSPECTION N054151-CLOSED COMPLETE HADC WORK/INSP. PER O.D. N/A BARRELS 1-4 FABRICATION NOT STARTED- N/A WORK/O.D. FWD DOME WORK/INSP. PER O.D. N/A ET-118 LO FWD OGIVE FABRICATION NOT STARTED- N/A WORK/O.D. AFT OGIVE FABRICATION NOT STARTED- N/A WORK/O.D. BARREL FABRICATION NOT STARTED-WORK/O.D. N/A DOME FABRICATION NOT STARTED-WORK/O.D. N/A ET-118 LH AFT DOME (GORES & FRAME) HADC WORK/INSP. PER O.D. N/A BARRELS 1-4 FABRICATION NOT STARTED- N/A WORK/O.D. FWD DOME FABRICATION NOT STARTED- N/A WORK/O.D. ET-119 & SUBSEQUENT BUILDS WORK/INSP. PER O.D. N/A APPENDIX 2 WELD LOCATION CLEARANCE RATIONALE O1 DESIGN LOAD ASSESSMENT OFO PROOF TEST DEMONSTRATION O2 PROOF TEST DEMONSTRATION OAO REQUIRES VISUAL INSPECTION O3 DESIGN LOAD ASSESSMENT OT 2219 WELD O4 DESIGN LOAD ASSESSMENT OB REQUIRES VISUAL INSPECTION O5 DESIGN LOAD ASSESSMENT OAF DESIGN LOAD ASSESSMENT ODG DESIGN LOAD ASSESSMENT OADC REQUIRES VISUAL INSPECTION OAL 2219 WELD OMH 2219 WELD HFM 2219 WELD HFE 2219 WELD HFV 2219 WELD HFDC REQUIRES VISUAL INSPECTION HFF REQUIRES VISUAL INSPECTION HFG REQUIRES VISUAL INSPECTION H8 REQUIRES VISUAL INSPECTION HB -ALL REQUIRES VISUAL INSPECTION HT -ALL 2219 WELD H7 REQUIRES VISUAL INSPECTION H6 REQUIRES VISUAL INSPECTION H5 REQUIRES VISUAL INSPECTION H4 REQUIRES VISUAL INSPECTION H3 REQUIRES VISUAL INSPECTION H2 REQUIRES VISUAL INSPECTION H1 REQUIRES VISUAL INSPECTION HAF REQUIRES VISUAL INSPECTION HAG REQUIRES VISUAL INSPECTION HADC PROOF TEST DEMONSTRATION HAM 2219 WELD HSP 2219 WELD (REFERENCE 'DISCREPANT WELD BEAD PROFILE' PRESENTATION ON 6/26/00 FROM W. SIGUR) |
| MSFC Response/Concurrence 10/31/2000 - BOARD ACCEPTS POA UNTIL 12/22/2000 PER RATIONALE B: WORST CASE MANIFESTATION OF THE PROBLEM IS NOT A FMEA CRITICALITY 1 EFFECT. CRIT 3 NO SIGN-OFFS REQUIRED. 01/30/2001 - BOARD ACCEPTS POA UNTIL 3/26/2001 PER RATIONALE (B): WORST CASE MANIFESTATION OF THE PROBLEM IS NOT A FMEA CRITICALITY 1 EFFECT. 03/22/2001 - BOARD ACCEPTED PLAN OF ACTION UNTIL 4/30/2001 PER RATIONALE (B): THE PROBLEM CONDITION IS CLEARLY SCREENED DURING PREFLIGHT CHECKOUT OR SPECIAL TESTS. 05/25/2001 - BOARD ACCEPTED PLAN OF ACTION UNTIL 6/30/2001 PER RATIONALE B: THE PROBLEM CONDITION IS CLEARLY SCREENED DURING PREFLIGHT CHECKOUT OR SPECIAL TESTS. 07/09/2001 - BOARD ACCEPTED PLAN OF ACTION UNTI 8/30/2001 PER RATIONALE (B): THE PROBLEM CONDITION IS CLEARLY SCREENED DURING PREFLIGHT CHECKOUT OR SPECIAL TESTS. 08/14/2001 - BOARD ACCEPTED PROBLEM CLOSURE RATIONALE. SIGNATURES ARE ON FILE IN THE PAC. THIS PROBLEM IS OFFICIALLY CLOSED. |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A17583 | IFA# -- | Contractor RPT# S-085 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# STP-5507 | Asmnt Part Name 2195 WELDING | Asmnt Serial/Lot# N/A |
| HCRIT CD 1 | FCRIT CD N/A | CAUSE CD MPP - MFG-PRC-INST | FAIL MODE MU - MECH TOLRNCE |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |