MSFC PRACA : 2003-02-12 08:41

MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A16702 | In-Flight Anomaly Number -- | Contractor Report Number P-080 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title G02 FORWARD PRESSLINE WELD LEAKAGE DURING ATP |
| EICN# -- | ELEMENT ET | Contractor LMMSS | FSCM# -- | FCRIT 1 |
| HCRIT -- | Sys_Lvl -- | Misc Codes A B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE LRU | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE NCA | NOMENCLATURE GO2 FORWARD PRESSLIN | PART# PD4800180-069 | SER/LOT# 0001280 | MANUFACTURER ARROWHEAD |
| Test/Operation A - ATP | Prevailing Condtion F - FUNCTIONAL | F / U F | Fail Mode MV - EXT LEAK | Cause DH - DES-HDW |
| System PROPULSION | Defect PE - VOID | Material H - WELD | Work Contact D. O`NEAL | Fail Date 11/03/1995 |
| Received at MSFC 06/09/1995 | Date Isolated 11/03/1995 | FMEA Reference 2.2.1.1 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location ARROWHEAD | Symptom MV - EXT LEAK | Time Cycle -- |
| Effectivity Text -- |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date 05/10/1996 | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 02/15/2001 | CN RSLV SBMT -- | Defer Date 11/10/1995 | Add Date 11/08/1995 | R/C Codes 0 - EXPL 4 - TEST -- |
| Assignee |
| Design M. MOORE | Chief Engineer M. PESSIN | S & MA M. SMILES | Project -- | Project MGR P. COUNTS |
| Approval |
| Design M. MOORE | Chief Engineer M. PESSIN | S & MA J. GREEN | Project -- | Project MGR P. COUNTS |
| PAC Assignee J. NELSON | PAC Review Complete JMN | MSFC Closure Date 03/05/1996 | Status C - CLOSED | F/A Completion 11/03/1995 |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID N000565 |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description DURING PERFORMANCE OF ATP 14180-309-7 AT ARROWHEAD, A LEAK WAS VISUALLY DETECTED ON WELD #6, THE BUTT WELD JOINING THE MIDDLE BSTRA FROM FORWARD END AND THE CURVED TUBE SECTION. HYDROSTATIC PRESSURE (600 PSIG) HAD BEEN APPLIED TO THE LINE TO PERFORM A PRESSURIZED DEFLECTION TEST WHEN WATER SEEPAGE AT THE WELD WAS NOTED. THE LINE HAD PREVIOUSLY PASSED A 1500 PSIG PROOF TEST AND AN UNPRESSURIZED DEFLECTION TEST CRITICALITY: THE PRESSURIZATION LINE IS CRIT. 1; FMEA ITEM CODE 2.2.1.1; LEAKAGE |
| Contractor Investigation/Resolution GENERAL: DURING ATP TESTING PERFORMED ON THIS LINE ASSEMBLY, THE LINE UNDERGOES A 1510 +/- 10 PSIG HYDROSTATIC PROOF TEST FOLLOWED BY DEFLECTION TESTS, TWO MOTIONS WITH THE LINE NOT PRESSURIZED AND TWO WITH THE LINE HYDROSTATICALLY PRESSURIZED TO 600 +10/-0 PSIG; ACCEPTANCE CRITERIA IS NO DAMAGE. THE LINE IS THEN DRIED AND A LEAK TEST IS PERFORMED AT A PRESSURE OF 300 +10/-0 PSIG GN2 THESE WELDS ARE MANUAL WELDS WITH MULTIPLE START AND STOP POINTS THEY ARE PENETRANT AND X-RAY INSPECTED PRIOR TO ATP. THERE IS NO LEAK OR PROOF TEST PERFORMED PRIOR TO ATP. THE PENETRANT USED WAS P6F4 WITH AN ACREAGE PROBABILITY OF DETECTION (POD) OF 0.086 INCHES AT 90% PROB/95%CL DURING THE INITIAL PROOF TEST, A WATER DROPLET WAS NOTED ON WELD #6, BUT THE SOURCE COULD NOT BE POSITIVELY DETERMINED AT THAT TIME. IT WAS NOT UNTIL THE LINE WAS PRESSURIZED FOR THE DEFLECTION TEST THAT THE LEAK WAS CONFIRMED. THE CRITICAL FLAW SIZE FOR THIS WELD IS 1.76 INCHES TASK I. FAILURE /PROBLEM INVESTIGATION PERFORM FAILURE ANALYSIS AT THE DIRECTION OF DESIGN ENGINEERING AND RELIABILITY ASSURANCE ON NCD N000565 RESPONSIBILITY: S. PARIKH/3760 J. SEIFERT/4120 - Z. KIRKLAND/4100 D. O'NEAL/3741 - D. WESTPHAL/3740 COMPLETE: 11/7/95 CLOSURE STATEMENT: THE TEST SETUP WAS DETERMINED TO BE CORRECT AND THE LINE WAS REMOVED FOR FURTHER ANALYSIS A REVIEW OF PRE-TEST X-RAYS BY AHP AND LMMSS CERTIFIED TECHNICIANS DID NOT REVEAL ANY INDICATIONS AFTER BAKING THE LINE DRY AND PERFORMING AN ATP TYPICAL GN2 LEAK TEST, THE LEAK PATH LOCATION WAS IDENTIFIED BY THE PRESENCE OF A MINUTE BUBBLE FORMING AT THE WELD BEAD TO TUBING INTERFACE WHEN A LEAK DETECTION SOLUTION WAS APPLIED. THE FORMATION OF THE BUBBLE WAS DESCRIBED AS EXTREMELY SLOW. THE LENGTH OF THE TEST WAS 5 TO 7 MINUTES AT 300 PSIG MAX. THE ACTUAL LEAK AREA WAS MARKED FOR REFERENCE VISUAL INSPECTION AT 10X DID NOT REVEAL EVIDENCE OF A CRACK OR ANY OTHER DEFECT POST ATP PENETRANT INSPECTION OF THE LEAK LOCATION DID NOT REVEAL ANY DEFECT (WOULD NOT HOLD PENETRANT). NO DEFECT SIZE COULD BE DETERMINED THE WELDER PERFORMING THIS WELD AND THE INSPECTORS PERFORMING THE X-RAY REVIEW AND PENETRANT INSPECTION WERE APPROPRIATELY CERTIFIED A REVIEW OF THE BUILD PAPER AND INSPECTION PROCESS FOUND NO ANOMALIES AND NO PRIOR REWORK AFFECTING WELD #6 THE RESULTS OF THESE INVESTIGATION ACTION ITEMS SUPPORT A CONCLUSION THAT THIS FAILURE IS IDENTICAL IN CAUSE AND EFFECT AS THE FAILURES ADDRESSED PER CAPS P-078. NO FURTHER ANALYSIS WILL BE PERFORMED CAUSE: THIS DEFECT WAS SMALLER THAN THE PROBABILITY OF DETECTION (POD) FOR NON-DESTRUCTIVE TESTING (I.E., X-RAY OR PENETRANT INSPECTION) ROOT CAUSE: WHEN WELDING THIN SECTIONS OF METAL, THE RAPID COOLING AT THE COMPLETION OF THE WELD CAN CAUSE CRACKING. THE FAILURES OCCURRED AT MANUAL WELDS THAT ARE INHERENTLY DIFFICULT TO PERFORM DUE TO THE JOINING OF THIN-WALL ICONEL 718 TUBE TO THE THICKER 21-6-9 CRES BALL-STRUT ASSEMBLY (BSTRA) USING HASTELLOY W TASK II. CORRECTIVE ACTION NONE REQUIRED AT THIS TIME. THESE DEFECTS ARE INHERENT TO THIS TYPE WELD, I.E. MANUAL WELD, THESE PARTICULAR MATERIALS, ETC (REFERENCE CAPS P-078) RELATIVE TO THIS LINE, A LEAK TEST WILL BE PERFORMED AS AN ADDITIONAL NON-DESTRUCTIVE INSPECTION PRIOR TO THE LINE REPEATING ATP PROBLEMS OF THIS TYPE WILL ALWAYS BE DETECTED DURING ATP, EITHER DURING PRESSURIZATION TESTS OR AS POSITIVELY ESTABLISHED, DURING THE LATER GN2 LEAK TEST PERFORMED. THESE LEAKS HAVE NOT AND SHOULD NOT RECUR AFTER ATP. GIVEN THAT ENHANCEMENTS TO THE MANUFACTURING PROCESS AS CITED IN CAPS P-078, AHP'S COMMITMENT TO FURTHER STUDY THIS WELD FOR POSSIBLE PROCESS IMPROVEMENT AND LMMSS/AHP NEGOTIATING EXTENDING PRE-ATP LEAK TESTING TO FUTURE UNITS, HAVE NOT YET TAKEN EFFECT OR BEEN IMPLEMENTED, NO FURTHER CORRECTIVE ACTIONS NEED BE TAKEN. (REFERENCE MMC-ET-RA06, SPACE SHUTTLE EXTERNAL TANK CRITICALITY 1, 1R, 2, 2R PROBLEM REPORTING PLAN FOR CAPS CLOSURE REQUIREMENTS) III. CLEARANCE OF EFFECTIVITIES ET-74 AND UP: ALL UNITS SUCCESSFULLY PASSED ATP. ATP IS DESIGNED TO CATCH THIS TYPE OF FAILURE NOTE: THIS IS ALSO DEFERRAL RATIONALE * TASK IV. CAPS CLOSURE SUMMARY THE PRESSLINE LEAK DISCOVERED DURING ATP TESTING WHILE THE LINE WAS HYDROSTATICALLY PRESSURIZED, RESULTED FROM APPARENT MINUTE CRACKS CREATED DURING THE WELDING PROCESS THAT WENT UNDETECTED DURING PRE-ATP NON-DESTRUCTIVE TESTING. THE CREATION OF THESE CRACKS OCCUR AS A RESULT OF DIFFERENTIAL COOLING THAT TAKES PLACE ALONG THE WELD, LEADING TO LOCALIZED HIGH STRESS AREAS AND LOCALIZED MICRO CRACKING. THIS CRACKING IS INHERENT TO THIS PARTICULAR PROCESS AND IS NORMALLY DETECTED DURING PENETRANT INSPECTION OR X-RAY PRIOR TO ATP, BUT IN THIS INCIDENT WENT UNDETECTED. EXAMINATION OF THE DEFECT AREA FAILED TO VISUALLY IDENTIFY THE LEAK PATH, IT WAS BELOW THE POD FOR PENETRANT INSPECTION AND IT WAS NOT DETECTABLE BY X-RAY. AS THIS TYPE DEFECT IS INHERENT TO THIS PROCESS, BUT IS DETECTABLE DURING ATP LEAK TEST, NO CONCERN EXISTS FOR PAST BUILDS THE RESULTS OF THIS INVESTIGATION FOUND THE CAUSE AND EFFECT TO BE IDENTICAL TO THE TWO FAILURES OCCURRING ON THIS SAME TYPE PRESSLINES ADDRESSED PER CAPS P-078. NO FURTHER ANALYSIS OR CORRECTIVE ACTION WAS NECESSARY THIS CAPS IS CLOSED. NO FURTHER ACTION IS REQUIRED RATIONALE FOR NON-CLOSURE OF CAPS P-080 MICHAEL B. MOORE/EP43 PROPULSION LABORATORY, PROPULSION & MECHANICAL SYSTEM DIVISION, MECHANICAL SYSTEMS DESIGN BRANCH 205-544-7176 |
| MSFC Response/Concurrence |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A16702 | IFA# -- | Contractor RPT# P-080 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# PD4800180-069 | Asmnt Part Name G02 FORWARD PRESSURE | Asmnt Serial/Lot# 0001280 |
| HCRIT CD -- | FCRIT CD 1 | CAUSE CD DH - DES-HDW | FAIL MODE MV - EXT LEAK |
| Asmnt FMEA 2.2.1.1 | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |