WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A12208 | In-Flight Anomaly Number -- | Contractor Report Number E-124 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title LOX PRESSURE TRANSDUCER FAILED DURING ATP |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 1R |
| HCRIT 1R | Sys_Lvl N | Misc Codes A (X) B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE LOX PRESSURE TRN | PART# PD7400098-079 | SER/LOT# 2235 | MANUFACTURER GULTON |
| HARDWARE LRU | NOMENCLATURE N/A | PART# N/A | SER/LOT# N/A | MANUFACTURER N/A |
| HARDWARE NCA | NOMENCLATURE LOX PRESSURE TRN | PART# PD7400098-079 | SER/LOT# 2235 | MANUFACTURER GULTON |
| Test/Operation A - ATP | Prevailing Condtion F - FUNCTIONAL | F / U F | Fail Mode EV - NOT-TO-SPEC | Cause MAW - MFG-ASY-WORK |
| System ELECTRICAL | Defect XN - NA | Material H - WELD | Work Contact J. ADAMS | Fail Date 04/27/1989 |
| Received at MSFC 04/28/1989 | Date Isolated -- | FMEA Reference 3.2.1.2 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location GULTON | Symptom ET - MEAS ANOMALY | Time Cycle N/A |
| Effectivity Text DEFERRED FOR STS-28, STS-34, STS-33 |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary CAUSE: IMPROPERLY PERFORMED WELD DURING TRANSDUCER ASSEMBLY R/C: THE MANUFACTURER RETRAINED ITS PERSONNEL IN PROPER WELD PROCEDURE AND ADDED AN IN-PROCESS 1R TEST FOLLOWING WELDING TO THE SHOP TRAVELERS |
| Last MSFC Update 02/13/1995 | CN RSLV SBMT 08/03/1989 | Defer Date -- | Add Date 04/28/1989 | R/C Codes 2 - MFG -- -- |
| Assignee |
| Design A. JACKMAN | Chief Engineer M. PESSIN | S & MA R. JACKSON | Project -- | Project MGR G. BRIDWELL |
| Approval |
| Design A. JACKMAN | Chief Engineer M. PESSIN | S & MA R. JACKSON | Project -- | Project MGR G. BRIDWLL |
| PAC Assignee C. MEYER | PAC Review Complete CM | MSFC Closure Date 08/17/1989 | Status C - CLOSED | F/A Completion 07/17/1989 |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description THE PRESSURE TRANSDUCER FAILED THE INSULATION RESISTANCE TEST SEGMENT DURING ATP PREVIOUS CAPS: E-082, E-091, E-101, E-106, E-110, E-111, E-112, E-115, E-119, E-120, E-121, E-122, E-123 |
| Contractor Investigation/Resolution 4/28/89 - THIS PROBLEM REPORT HAS BEEN DEFERRED FOR STS-30 BASED ON THE FOLLOWING RATIONALE: THE LOX PRESSURE TRANSDUCER IS CRIT 1R. THERE ARE FOUR UNITS INSTALLED WHILE THREE ARE REQUIRED TO BE FUNCTIONAL. IF ONE UNIT FAILS TO OPERATE THE BACK-UP UNIT COULD BE SWITCHED TO UNTIL T-10 SECONDS ALL EFFECTIVITIES CLEARED, THE FAILURE OCCURRED DURING VENDOR ACCEPTANCE TESTING. ALL INSTALLED COMPONENTS HAVE SUCCESSFULLY PASSED ACCEPTANCE TESTING THE ABOVE DEFERRAL MEETS THE DEFERRAL REQUIREMENTS OF NSTS 07700 VOLUME XI, ITEM C, WHICH STATES "THE PROBLEM CONDITION DOES NOT EXIST IN THE FLIGHT HARDWARE AND IS CLEARLY SCREENED BY ACCEPTANCE TEST, PREFLIGHT CHECKOUT, OR SPECIAL TEST" THE ABOVE DEFERRAL RATIONALE HAS BEEN APPROVED BY THE ET PROJECT MANAGER, MR. J. SMELSER ________JERRY W. SMELSER (SIGNED 5/1/89)_____________ THIS PRBLEM REPORT HAS BEEN DEFERRED FOR STS-28, STS-34 AND STS-33 BASED ON THE ABOVE RATIONALE THE ABOVE DEFERRAL HAS BEEN APPROVED BY THE ET ACTING PROJECT MANAGER, MR. G.P. BRIDWELL __________________G.P. BRIDWELL (SIGNED)__________________________ 5/2/89 GENERAL PRESSURE TRANSDUCER, S/N 2235, FAILED DURING VENDOR ACCEPTANCE TESTING AND WAS DOCUMENTED ON MARS T-34395. THE TEST, ATP-3061-0000-81, PARA 5.1., REQUIRES A MINIMUM RESISTANCE OF 50 MEGOHMS AT 50 VDC BETWEEN THE TRANSDUCER WIRING AND THE CASE. THE ACTUAL RESISTANCE WAS LOWER IN VALUE THAN THE MEASUREMENT CAPABILITIES OF THE METER USED, I.E. A NEAR ZERO READING TASK I FAILURE INVESTIGATION THE LOW INSULATION RESISTANCE WAS TRACED TO A SOLDER JOINT WHICH HAD BEEN REMELTED DURING AN IMPROPERLY PERFORMED TRANSDUCER CABLE RETAINER WELD. THE SOLDER BRIDGED ACROSS AN INSULATOR. REFERENCE: FAILURE ANALYSIS T-34395 TASK CLOSED TASK II CORRECTIVE ACTION A. GULTON-SERVONIC REEMPHASIZED THE IMPORTANCE OF ADHERING TO THE WELDING PROCEDURES TO THEIR WORKERS. REFERENCE: MRAS T-34395 B. GULTON-SERVONIC'S PERSONNEL, WHICH PERFORM INSULATION RESISTANCE TESTING DURING TRANSDUCER MANUFACTURE, WERE RETRAINED TO ASSURE PROPER USE OF THE EQUIPMENT DURING IN-PROCESS CONFIDENCE TESTS PRIOR TO ACCEPTANCE TESTING. REFERENCE: MARS T-34395 C. GULTON-SERVONIC REVISED THE SHOP TRAVELERS FOR BOTH THE -079 AND THE -089 TRANSDUCERS TO INCLUDE AN INSULATION RESISTANCE TEST IMMEDIATELY FOLLOWING THE CABLE RETAINER WELD. REFERENCE: MARS T-34395 D. GULTON-SERVONIC PERFORMED A SEARCH OF THE PRODUCTION RECORDS FOR ALL -089 TRANSDUCERS AND ALL CURRENT USAGE -079 TRANSDUCERS FOR CABLE RETAINER WELD PROBLEMS. NO -089 PART HAD BEEN DELIVERED TO MMC THAT HAD ANY CABLE RETAINER WELD DIFFICULTIES. ONE -079 PART HAD BEEN REWORKED FOR A CABLE RETAINER WELD PROBLEM. THE -079 SUBSEQUENTLY PASSED BOTH THE IN-PROCESS AND ACCEPTANCE INSULATION RESISTANCE TESTS. REFERENCE: GULTON MEMOS MS: 89-010 AND PEM89-089 TASK CLOSED TASK III CLEARANCE OF EFFECTIVITIES ALL ETS CLEARED. THE FAILURE OCCURRED DURING VENDOR ACCEPTANCE TESTING AND ALL INSTALLED TRANSDUCERS HAVE SUCCESSFULLY PASSED THE ACCEPTANCE TEST TASK CLOSED TASK IV CAPS CLOSURE SUMMARY ONE TRANSDUCER FAILED THE ACCEPTANCE TEST REQUIREMENT FOR INSULATION RESISTANCE. THE FAILURE WAS TRACED TO AN IMPROPERLY PERFORMED WELD WHICH REMELTED A SOLDER JOINT. THE MANUFACTURER RESTRAINED ITS PERSONNEL IN PROPER WELD PROCEDURES AND ADDED AN IN-PROCESS IR TEST FOLLOWING WELDING TO THE SHOP TRAVELERS TASK CLOSED THIS PROBLEM REPORT CLOSURE IS SUBMITTED TO MSFC FOR CLOSURE REVIEW AND APPROVAL |
| MSFC Response/Concurrence |

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A12208 | IFA# -- | Contractor RPT# E-124 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# PD7400098-079 | Asmnt Part Name LOX PRES TRANSDUCER | Asmnt Serial/Lot# 2235 |
| HCRIT CD -- | FCRIT CD 1R | CAUSE CD MAW - MFG-ASY-WORK | FAIL MODE EG - SIG HI OR LO |
| Asmnt FMEA 3.2.1.1 | Asmnt FM 1 | FMEA CSE E | FMEA SCSE 4 |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |