96M03/29/06

S717-96M.doc

Include the following when using relatively small amount of structural steel. AASHTO M270M steel is not readily available for rolled shapes and small quantities.

Section 717. - STRUCTURAL METAL

717.01  Structural Steel.  Delete the text and substitute the following:

(a) Structural carbon steel.  Structural carbon steel for riveted, bolted, or welded construction shall conform to ASTM A36M.  In addition, steel for primary bridge members and fracture critical bridge members shall meet the supplementary requirements for Charpy V-notch test.

(b) High-strength low-alloy structural (HSLA) steel.  High-strength, low-alloy structural steel, or steel acquiring enhanced atmospheric corrosion resistance for riveted, bolted, or welded construction, use steel conforming to ASTM A588M.  In addition, steel for primary bridge members and fracture critical bridge members shall meet the supplementary requirements for Charpy V-notch test.

(c) Bolts and nuts.  Conform to ASTM A 307.

(d) High-strength bolts, nuts, and washers.  Conform to either AASHTO M 164M or AASHTO M 253M, as specified.  Use Type 3 bolts in combination with unpainted weathering structural steel.

Include the following whenever steel castings may be required or permitted.

717.04  Castings.

(a) Steel castings.  Delete the text and substitute the following:

Conform to AASHTO M 103M, grade 485-250.

When steel pipe is specified, include the following:

717.06  Steel Pipe.  Delete the text and substitute the following:

Furnish galvanized steel pipe conforming to ASTM A 53, type F, standard weight class, and plain ends for the designation specified in the contract.

When steel grid floors are specified, include the following:

717.09  Steel Grid Floors.  Delete the text and substitute the following:

Conform to ASTM D5484 type I.  Furnish galvanized steel grid floors unless painting is specified.

717.10  Elastomeric Bearing Pads.  Delete the title and text and substitute the following:

717.10  Bearings.

(a) Elastomeric bearings, plain or laminated.  Conform the AASHTO M 251.

(b) Elastomeric bearings, high load rotational confined.  Conform to ASTM D 5212.

(c) High lead rotational spherical bearings.  Conform to ASTM D 5977.

When tetrafluoroethylene surfaces for bearings are specified, include the following:

717.11  Tetrafluoroethylene (TFE) Surfaces for Bearings.  Delete the title and text and substitute the following:

717.11  Polytetrafluoroethylene (PTFE) Surfaces for Bearings.  When PTFE surfaces are

specified for bearings which are not listed in subsection 717.10, conform to the following:

(a) PTFE resin.  Furnish virgin PTFE resin material conforming to ASTM D 4895 and the following:

(1) Specific gravity	2.13 to 2.19

(2) Melting point	328º C ± 1ºC

(b) Filler material.  Furnish milled glass fibers, carbon, or other approved inert material.

(c) Adhesive material.  Furnish epoxy resin adhesive conforming to FSS MMM-A-134, FEP film, or an approved equal.

(d) Unfilled PTFE sheet.  Furnish unfilled PTFE sheet made from PTFE resin.  Conform to the following:

(1) Tensile strength, ASTM D 638	19 MPa min.

(2) Elongation, ASTM D 638	200% min.

(e) Filled PTFE sheet.  Furnish filled PTFE sheet made from PTFE resin uniformly blended with filler material.  For filled PTFE sheets containing glass fibers or carbon, conform to Table 717-1.

(f) Fabric containing PTFE fibers.  Furnish fabric made from oriental multi filament PTFE fluorocarbon and other fibers.  Use PTFE fibers conforming to the following:

(1) Tensile strength, ASTM D 2256	165 MPa min.

(2) Elongation, ASTM D 2256	75% min.

Table 717-1

Filled Polytetrafluoroethylene Sheeting

| Property | ASTM Method | 15% Glass Fibers | 25% Carbon |
| --- | --- | --- | --- |
| Mechanical: Min. Tensile strength Min. Elongation | D 638 D 638 | 14 MPa 150% | 9 MPa 75% |
| Physical: Min. Specific gravity Melting point | D 792 D 638 | 2.20 327 ± 10ºC | 2.10 327 ± 10ºC |

(g) Interlocked bronze and filled PTFE components.  Furnish a phosphor bronze plate conforming to AASHTO M 108 with an 0.25 millimeter thick porous bronze surface layer conforming to ASTM B 103M into which is impregnated a PTFE compound.  Overlay the surface with compounded PTFE not less than 25 micrometers thick.

(h) PTFE metal composite.  Furnish virgin PTFE molded on each side and completely through a 33 millimeter perforated stainless steel sheet conforming to ASTM A 240M type 304.

(i) Surface treatment.  For epoxy bonding, factory treat one side of the PTFE sheet with a sodium naphthalene or sodium ammonia process.

(j) Stainless steel mating surface.  Conform to ASTM A 240M type 304 and the following:

(1) Thickness	0.91 mm min.

(2) Surface finish	0.5µm root mean square max.

Polish or roll stainless steel mating surfaces as necessary to meet the specified friction properties.

When aluminum alloy for bridge rail is specified, include the following:

717.13  Aluminum Alloy for Bridge Rail.  Delete the text and Table 717-3 and substitute the following:

Conform to AASHTO-AGC-ARTBA “A Guide to Standardized Highway Barrier Hardware.”

When elastomeric compression joint seals are specified, include the following:

717.16  Elastomeric Compression Joint Seals.  Delete the text and substitute the following:

Conform to AASHTO M 297.