MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A15427 | In-Flight Anomaly Number -- | Contractor Report Number S-077 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title ET WEB SUSPECTED OF LOW MATERIAL PROPERTIES |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 3 |
| HCRIT -- | Sys_Lvl N | Misc Codes A B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE LRU | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE NCA | NOMENCLATURE EXTERNAL TANK | PART# 80914801982-XXX | SER/LOT# NA | MANUFACTURER MCI |
| Test/Operation M - MFG | Prevailing Condtion N - INSPECTION | F / U UC | Fail Mode MS - STRUCT | Cause MAW - MFG-ASY-WORK |
| System STRUCTURAL | Defect MT - TYPE W | Material S - STRUCT | Work Contact M. BANKESTER | Fail Date 03/19/1993 |
| Received at MSFC 05/25/1993 | Date Isolated 03/19/1993 | FMEA Reference N/A | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location MAF | Symptom UC - UNSAT | Time Cycle -- |
| Effectivity Text -- |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 02/22/1995 | CN RSLV SBMT 07/28/1993 | Defer Date -- | Add Date 05/25/1993 | R/C Codes 0 - EXPL -- -- |
| Assignee |
| Design O. MOON | Chief Engineer M. PESSIN | S & MA R. JACKSON | Project -- | Project MGR P. COUNTS |
| Approval |
| Design O. MOON | Chief Engineer M. PESSIN | S & MA R. JACKSON | Project -- | Project MGR P. COUNTS |
| PAC Assignee B. HURST | PAC Review Complete BH | MSFC Closure Date 08/03/1993 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description ET-60 AND UP 80914801982-XXX WEB DETAILS ARE SUSPECT OF HAVING LOW MATERIAL PROPERTIES. (REQUIREMENT: YIELD = MIN 50 KSI; ULTIMATE = 64 KSI) NOTE 1: THIS IS A DISCRETIONARY CAPS (REFERENCE PARAGRAPH 1.6.2.3C OF MMC-ET-RAO3) REQUESTED BY THE ET PROJECT OFFICE AND DOES NOT SPECIFICALLY RELATE TO ANY CIL ITEM NOTE 2: SPECIAL INVESTIGATION SI-93-S011 HAS BEEN OPENED AND PROVIDES DETAILED INVESTIGATIVE INFORMATION PERTAINING TO ALL WEB DISCREPANCIES REPORTED. COPIES OF SI-93-S011 ARE AVAILABLE UPON REQUEST NOTE 3: THIS CAPS DOCUMENTS THE MATERIAL PROPERTIES PROBLEM THAT WAS PREVIOUSLY REPORTED ON CAPS S-076 (REV. "B": REVISED TO INCLUDE RESPONSE TO SCAR 93-049 (TASK II) AND CLOSED CAPS---SEE ASTERISKS |
| Contractor Investigation/Resolution GENERAL: MAY 1993 AS A PART OF THE MATERIAL THICKNESS INVESTIGATION, A PANEL WAS SELECTED FROM INVENTORY STORES AND TESTED TO DETERMINE ACTUAL TENSILE STRENGTH VALUES. THIS PANEL FAILED WITH WORST CASE RECORDED VALUES OF YIELD = 48.6 KSI AND ULTIMATE = 60.6 KSI (REQUIREMENT: YIELD = 50.0 KSI; ULTIMATE = MIN 64 KSI) - AN ADDITIONAL PANEL WAS TESTED AND BOTH YIELD AND ULTIMATE VALUES PASSED - MCI DELIVERED AN ETCHED AND UNETCHED PANEL FOR MECHANICAL PROPERTIES TESTING, BOTH PASSED TASK I. PROBLEM/FAILURE INVESTIGATION 1) ENGINEERING TO DEVELOP WORST CASE MECHANICAL PROPERTIES SCENARIO RESPONSIBILITY: L. JOHNSTON/P. HINKELDEY COMPLETE: 5/14/93 CLOSURE STATEMENT BASED ON TESTS FOR MECHANICAL PROPERTIES PERFORMED AT MAF, MATERIALS ENGINEERING'S BEST ESTIMATE FOR LOWER BOUND YIELD AND ULTIMATE VALUES IS FTY = 47 KSI; FTU = 59 KSI 2) ENGINEERING TO EVALUATE WORST CASE PREDICTED CONDITIONS FOR MATERIAL PROPERTIES AND PROVIDE RATIONALE FOR FLEET CLEARANCE RESPONSIBILITY: J. DYE/G. COPELAND COMPLETE: 5/14/93 CLOSURE STATEMENT ENGINEERING DETERMINED BY ANALYTICAL METHODOLOGY (REVISED TO REFLECT SEMI-TENSION FIELD CAPABILITY), VERIFIED BY TEST, THAT WEBS WITH LOW MECHANICAL PROPERTIES (FTY = 47.0 KSI AND FTU = 59.0 KSI) ARE ACCEPTABLE FOR FLIGHT * TASK II. ENHANCEMENTS MCI HAS RESPONDED TO SCAR 93-049 BY STATING THAT THEY INSTRUCTED ASTRO ALUMINUM HEAT TREATING (SUBCONTRACTOR) TO MONITOR QUENCH OPERATIONS MORE CLOSELY TO ENSURE THE CORRECT TIME REQUIREMENT IS MAINTAINED AND TO ASSURE PROPER AGITATION IS PERFORMED TO ELIMINATE STEAM POCKETS THESE PARTS WERE PROCESSED FIVE YEARS AGO. ASTRO ALUMINUM HAS MADE SIGNIFICANT IMPROVEMENTS DURING THAT TIME. THESE IMPROVEMENTS INCLUDE: - MECHANIZATION AND TYPING OF ALL JOB FOLDERS - COMPUTERIZED TYPING OF ALL JOBS - CERTIFICATION PROGRAM FOR BOTH HEAT TREAT SHOP PERSONNEL AND INSPECTORS WHO DO HARDNESS TESTING - RECORDING OF ACTUAL QUENCH TIMES (FURNACE TO SUBMERSION) - IMPLEMENTATION OF IMPROVEMENT TEAMS RELIABILITY ASSURANCE FEELS THAT NO FURTHER ACTION IS NECESSARY TASK III. FLEET CLEARANCE ETS THROUGH ET-59 HAVE BEEN CLEARED SINCE THEY WERE ISSUED 80914801980-XXX PARTS FROM A PREVIOUS VENDOR (TELEDYNE AERO-CAL) BEFORE RECEIPT OF MCI PARTS IN JANUARY 1989 ETS 60 THROUGH 75 HAVE BEEN CLEARED BY USE AS IS DISPOSITION FROM ENGINEERING ON MULTI-EFFECTIVITY MARS T-125467 ETS 76 AND UP HAVE BEEN CLEARED BY USE AS IS DISPOSITION FROM ENGINEERING ON MARS T-123598 (ADDRESSING ALL WEB FRAMES IN INVENTORY STORES) AND MARS T-119710 (ADDRESSING 160 FORMED BUT NOT ETCHED PARTS AT MCI) NOTE: THE INFORMATION IN THIS SECTION IS ALSO THE DEFERRAL RATIONALE PROBABLE CAUSE: 1) SLACK QUENCH - TIME FROM FURNACE TO QUENCH WATER > 15 SECONDS, OR STEAM POCKETS FORMED DECREASING COOLING RATE 2) OVER AGED - APPROXIMATELY 18 HOURS COULD GIVE SIMILAR PROPERTIES (DOUBLE NORMAL AGE TIME) TASK IV. CAPS CLOSURE SUMMARY AS A RESULT OF THE WEB MATERIAL THICKNESS INVESTIGATION, A PANEL WAS TESTED FOR TENSILE STRENGTH AND WORST CASE RECORDED VALUES OF YIELD= 48.6 KSI AND ULTIMATE =60.6 KSI WAS OBTAINED (REQUIREMENT: YIELD=MIN 50 KSI; ULTIMATE=MIN 64 KSI). THREE ADDITIONAL PANELS WERE TESTED AND ALL PASSED BOTH ULTIMATE AND YIELD. ENGINEERING THEN DETERMINED BY ANALYTICAL METHODOLOGY THAT WEBS WITH LOW MECHANICAL PROPERTIES (FTY= 47.0 KSI AND FTU=59.0 KSI) ARE ACCEPTABLE FOR FLIGHT. PROBABLE CAUSE WAS ATTRIBUTED TO SLACK QUENCH OR OVER AGING OF THE PART. MCI INSTRUCTED ASTRO ALUMINUM HEAT TREATING TO MONITOR THEIR QUENCH OPERATIONS MORE CLOSELY TO ENSURE THE CORRECT TIME REQUIREMENT IS MAINTAINED AND TO ASSURE PROPER AGITATION IS PERFORMED TO ELIMINATE STEAM POCKETS. THESE PARTS WERE PROCESSED FIVE YEARS AGO AND ASTRO ALUMINUM HAS MADE SIGNIFICANT IMPROVEMENTS DURING THAT TIME. NO FURTHER ACTION IS REQUIRED THIS CAPS IS CLOSED |
| MSFC Response/Concurrence |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A15427 | IFA# -- | Contractor RPT# S-077 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# 8091401982-XXX | Asmnt Part Name EXTERNAL TANK | Asmnt Serial/Lot# N/A |
| HCRIT CD -- | FCRIT CD 1 | CAUSE CD MAW - MFG-ASY-WORK | FAIL MODE MS - STRUCT |
| Asmnt FMEA N/A | Asmnt FM N/A | FMEA CSE N/A | FMEA SCSE N/A |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |