WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A11705 | In-Flight Anomaly Number -- | Contractor Report Number E-115-2 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title LO2 ULLAGE PRESSURE TRANSDUCER FAILED DURING ATP |
| EICN# -- | ELEMENT ET | Contractor MMMSS | FSCM# -- | FCRIT 1R |
| HCRIT 1 | Sys_Lvl N | Misc Codes A B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE L02 ULL PRES TRNSDCR | PART# PD7400098-079 | SER/LOT# 2286 | MANUFACTURER GULTON |
| HARDWARE LRU | NOMENCLATURE N/A | PART# N/A | SER/LOT# N/A | MANUFACTURER N/A |
| HARDWARE NCA | NOMENCLATURE L02 ULL PRES TRNSDCR | PART# PD7400098-079 | SER/LOT# 2286 | MANUFACTURER GULTON |
| Test/Operation A - ATP | Prevailing Condtion -- | F / U F | Fail Mode EV - NOT-TO-SPEC | Cause MAE - MFG-ASY-ENVR |
| System ELECTRICAL | Defect CN - CONTAM | Material C - EEE | Work Contact J. ADAMS | Fail Date 09/07/1988 |
| Received at MSFC 09/07/1988 | Date Isolated -- | FMEA Reference 3.2.1.2 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location SUPPLIER | Symptom EE - RANDOM | Time Cycle N/A |
| Effectivity Text NONE |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 02/13/1995 | CN RSLV SBMT 11/10/1988 | Defer Date -- | Add Date 09/08/1988 | R/C Codes 0 - EXPL -- -- |
| Assignee |
| Design A. JACKMAN | Chief Engineer J. NICHOLS | S & MA R. JACKSON | Project M. PESSIN | Project MGR G. SMELSER |
| Approval |
| Design A. JACKMAN | Chief Engineer J. NICHOLS | S & MA R. JACKSON | Project M. PESSIN | Project MGR G. SMELSER |
| PAC Assignee J.EL-IBRAHIM | PAC Review Complete JE | MSFC Closure Date 12/22/1988 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description L02 ULLAGE PRESSURE TRANSDUCER FAILED DURING VENDOR ACCEPTANCE TESTING THE TRANSDUCER LOST SIGNAL (DROPOUT) AT 23 PSI ON PRESSURE RISE DURING HIGH RESOLUTIONS CALIBRATION TEST. NO DROPOUT ALLOWED. REF MARS T 34378 |
| Contractor Investigation/Resolution 9/7/88 - THIS PROBLEM HAS BEEN DEFERRED FOR STS-26 PER NSTS 07700, VOLUME XI AND NSTS 08126 PARAGRAPH 3.4.1, ITEM C WHICH STATES "PROBLEM CONDITION DOES NOT EXIST IN THE FLIGHT HARDWARE AND IS CLEARLY SCREENED BY ACCEPTANCE TEST, PREFLIGHT CHECKOUT, OR SPECIAL TEST." THIS DEFERRAL HAS BEEN APPROVED BY THE ET PROJECT MANAGER, MR. G.P. BRIDWELL _______G.P. BRIDWELL (SIGNED 9/15/88)____________ 10/3/88 - THIS PROBLEM HAS BEEN DEFERRED FOR STS-27 PER NSTS 07700, VOLUME XI AND NSTS 08126 PARAGRAPH 3.4.1, ITEM C WHICH STATES "PROBLEM CONDITION DOES NOT EXIST IN THE FLIGHT HARDWARE AND IS CLEARLY SCREENED BY ACCEPTANCE TEST, PREFLIGHT CHECKOUT, OR SPECIAL TEST." THIS DEFERRAL HAS BEEN APPROVED BY THE ET PROJECT MANAGER, MR. G.P. BRIDWELL _____G.P. BRIDWELL (SIGNED 10/7/88)______________ CAUSE: THE PROBABLE CAUSE WAS CONTAMINATION OF THE INTERNAL POTENTIOMETER R/C: NONE 11/10/88 GENERAL THE TRANSDUCER FAILED THE SIGNAL DROPOUT CRITERIA DURING VENDOR ACCEPTANCE TESTING (ATP). OCCASIONAL ATP FAILURES OF THIS TYPE ARE EXPECTED AS PART OF NORMAL PRODUCTION FALLOUT. INVESTIGATION OF PREVIOUS SIMILAR FAILURES HAS FOUND THAT MICROSCOPIC PARTICULATE CONTAMINATION OF THE INTERNAL RESISTIVE ELEMENT AND WIPER IS THE MOST PROBABLE CAUSE. REFERENCE: CAPS E-082 TASK I FAILURE INVESTIGATION FAILURE ANALYSES WILL BE PERFORMED ON THE TRANSDUCERS AT MAF FAILURE ANALYSIS OF THE TRANSDUCERS WAS PERFORMED AT MAF. THE TRANSDUCER WAS IN GOOD CONDITION EXTERNALLY. DISASSEMBLY AND EXAMINATION OF THE INTERNAL MECHANISM FOUND BUT A SINGLE PROBLEM THE RESISTIVE ELEMENT OF THE TRANSDUCERS AD CONTAMINATION ON THE PATH OF CONTACT WITH THE WIPER. OPTICALLY IT APPEARED AS A STREAK OF DARK MATERIAL. UNDER SEM EXAMINATION WAS ONLY VISIBLE USING THE BACKSCATTER IMAGE. ATTEMPTS AT CHEMICAL ANALYSIS WERE NOT SUCCESSFUL CONTAMINATION OF THE RESISTIVE ELEMENT HAS BEEN SHOWN TO RESULT IN HIGH CONTACT RESISTANCE AND, ON OCCASION, DROPOUTS TASK CLOSED TASK II CORRECTIVE ACTION NO CORRECTIVE ACTION IS REQUIRED TASK CLOSED TASK III CLEARANCE EFFECTIVITIES ALL ETS CLEARED. THE FAILURE OCCURRED DURING VENDOR ACCEPTANCE TESTING AND ALL INSTALLED TRANSDUCERS HAVE SUCCESSFULLY PASSED THE ACCEPTANCE TEST TASK CLOSED TASK IV CAPS CLOSURE SUMMARY THE TRANSDUCER FAILED DURING VENDOR ACCEPTANCE TEST. THE FAILURE WAS OF A TYPE THAT IS CONSIDERED NORMAL PRODUCTION FALLOUT. NO CORRECTIVE ACTION IS REQUIRED TASK CLOSED THIS PROBLEM REPORT CLOSURE IS SUBMITTED TO MSFC FOR REVIEW AND APPROVAL |
| MSFC Response/Concurrence |

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A11705 | IFA# -- | Contractor RPT# E-115-2 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# PD7400098-079 | Asmnt Part Name LOX PRES TRANSDUCER | Asmnt Serial/Lot# 2286 |
| HCRIT CD -- | FCRIT CD 1R | CAUSE CD MAE - MFG-ASY-ENVR | FAIL MODE EV - NOT-TO-SPEC |
| Asmnt FMEA 3.2.1.1 | Asmnt FM 1 | FMEA CSE E | FMEA SCSE 1 |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |