Wet Lay-Up Shear vs. Compression

C Neumeyer

9/26/3

The following figure shows the wet lay-up shear data including the latest results from G6. A fit was made to the minimum of the data, and then a peak equivalent to that fit based on the 1.65 peak to average applied to the zero compression value. This result is shown superimposed, along with the prior assumption. The equation for the peak fit is…

For compression <= 3000 psi….

Shear Stress = 1.65*2300+0.625*Compression

For compression > 3000 psi….

Shear Stress = 1.65*2300+0.625*3000

…where shear and compression are in psi.

It is proposed to use this curve in the wet lay-up safety factor calculation.