| CABLE No. | FNL-2-I-00744 |
| --- | --- |
| MFG. | 3/10/00 |
| OPERATOR: | H. Higley |

CABLE LOG SHEET

LBNL SUPERCONDUCTING MAGNET CABLES

Objective: Make NbTi cable as proposed by E. Barzi for FNAL Cos. ( splices.

- STRAND INFORMATION -

| MANUFACTURER : | IGC |
| --- | --- |
| BILLET #: | B1672 |
| No of strands: | 34 |
| COMPOSITION : | NbTi From SSC Inner cable inventory. |
| STRAND Dia.. NOMINAL : | .808mm | INSP. DIA..: | .8095mm avg. |
| Cu/SC RATIO NOMINAL : | 1.3:1 | INSP. RATIO : |  |
| FILAMENT TWIST/LENGTH : | 11mm | DIRECTION : | Right |
| SHARP BEND TEST : |  |
| LENGTH PER SPOOL : | 75m |

- CABLING SPECIFICATIONS -

| TYPE or SPEC.: | As per E. Barzi HIGH FIELD MAGNET FIRST DIPOLE MODEL NbTi SPLICE |
| --- | --- |
| No. of STRANDS: | 28 |
| PITCH DIRECTION: | LEFT | PITCH LENGTH: | 109.8mm |
| PLANETARY RATIO: | -1:1 |
| ROLLER ID #: | P-1 & 2 | WIDTH: | 14.165mm | ANGLE:: | Ground to 0.475 deg. |
| MANDREL ID #: | 37 | WIDTH: | 13.58mm | THICKNESS:: | 0.90mm |
| LUBRICATION : | 100% 4-BR |
| STRAND TENSION: | 2.7 kg. | TURKS HEAD LOAD "SGM": | 59 kg. |
| Nom. THICKNESS: | 1.535 mm |
| Nom. WIDTH: | 14.232mm |
| Nom. ANGLE: | .455 deg. |

Notes:  The cable as defined was mechanically unstable.  The major edge of the cable being at nearly two strand diameters needed more compaction.  The simplest solution with regard to the cables intended purpose was to decrease the mid-thickness of the cable.  I decided to settle with the largest mid-thickness that yields some measure of stability.

Note that this cable is still relatively unstable, but that it can be handled and strands that do pop out can be realigned.

- FINISHED CABLE

| FINISHED LENGTH: | 65m |
| --- | --- |
| Avg. THICKNESS: | 1.4928 mm |
| Avg. WIDTH: | 14.2281 |
| Avg. ANGLE: | .375 deg. |
| RESIDUAL TWIST/Mtr.: | 0 deg. Excellent residual twist. |
| ETCH for FILAMENT DAMAGE: | OK |

See data display: