5/4/07

TD-07-007

LARP TQS01c Test Summary

G. Ambrosio, R. Carcagno, S. Caspi, G. Chlachidze, F. Lewis, A. Lietzke, D. Orris, Y. Pischalnikov, G.L. Sabbi, D. Shpakov, C. Sylvester, M. Tartaglia, J.C. Tompkins, G. Velev, A.V. Zlobin

Content:

1. Introduction				  2

2. Quench history			  2

3. Temperature dependence		15

4. Ramp rate dependence		16

5. Protection heater study		17

6. MIITs study				18

7. Magnetic measurement 		19

8. Strain gauge results			24

9. Quench antenna data		34

10. RRR measurement		35

11. Voltage spikes			38

1. Introduction

TQS01 is a 1m long quadrupole model assembled at LBNL as part of the LARP program. TQS01c stands for the third test of this magnet. In these tests different coil sets have been used (coils 5,6,7, and 8 in the first test; coils 7, 8, 14, and 15 in TQS01b; coils 5,7,8, and 15 in TQS01c).  This report documents the tests of TQS01c which were conducted at Fermilab in the Vertical Magnet Test Facility (VMTF) in order to study quench performance at superfluid helium temperature, and perform magnetic field measurements.  According to a request by LBNL a slow cool down (maintaining T<50 K across the magnet) was executed, starting on the morning of February 28 to March 2, during which strain gauges and coil segment resistances were continuously monitored. Magnet performance tests started in the afternoon of March 5 and lasted until the morning of March 16.

2. Quench History

The magnet test program started with quench training at 20 A/s ramp rate at 4.5 K. At the beginning the quench detection threshold was set to 350 mV. A series of trips induced by voltage spikes (flux jumps) caused the increase of the detection threshold to 400 and 500 mV. The first magnet quench occurred at 8526 A with 500 mV threshold. After two more spike induced trips the threshold was set to 600 mV. During the following six current ramps two more trips occurred and the threshold was set to 700 mV. This threshold was used for all the rest of the test except for the MIITs studies.

At the eighth quench a plateau was reach at about 9560 A confirmed by the following 5 quenches. The magnet was then cooled down to 1.9 K and the training started from 9596 A followed by a step back to 9416 A. The rest of the training at 1.9 K showed a small but constant current increase up to 10490 A (quench 35) with a small step back at quench 32 (from 10340 A to 10100 A).  Quenches 35 to 40 showed a plateau with current between 10475 and 10501 A. In the two subsequent quenches the ramp rate was 20 A/s up to 10 kA, and then 5 A/s after two minutes hold (quench current: 10526 A, and 10489 A). The magnet was then warmed up to 4.5 K holding the temperature at some intermediate steps in order to measure the quench current at 20 A/s.

Ramp rate studies were subsequently performed at 4.5 K, followed by quench protection studies and MIITs effect studies.

The quench history is presented in Figure 2.1 and in the following tables.  These tables have been generated by processing the quench files. Comments in blue have been added subsequently based on notes taken during the test.

During magnet training all coils had at least two quenches. Coil 15 had most of the quenches during training and all quenches at the plateau and during temperature studies (Fig. 2.2)

Quench current temperature dependence and ramp rate dependence are shown in Figs. 3.1 and Fig 4.1 respectively. Protection heater and MIITs studies are presented in section 5 and 6.

Figure 2.1. TQS01c quench history. Quench 43 is not shown because occurred during magnetic measurement. Quench protection heater studies were performed between quench 51 and 52.

| TQS01c Quench History table with comments |
| --- |
| File | Q No. | Current | dI/dt | tquench | MIITs | Mag Temp Bot Left | Mag Temp Top Left | Comments |
| tqs01.Quench.070227164332.150 |  | 3 | 0 | 1.0000 | 0.00 | 0.000 | 0.000 |  |
| tqs01.Quench.070302162331.717 |  | 967 | 72 | -0.0057 | 0.12 | 4.455 | 4.452 | DQD_COIL trip at about 900 A... investigating. |
| tqs01.Quench.070302173255.243 |  | 1470 | 100 | -0.0001 | 0.16 | 4.455 | 4.450 | all of the AQDs went off at the same time ?? at about 1350 A. |
| tqs01.Quench.070302180720.696 |  | 1574 | 19 | -0.0070 | 0.21 | 4.453 | 4.451 | perhaps another flux jump trip. |
| tqs01.Quench.070302182651.634 |  | 3002 | 0 | -0.0748 | 1.32 | 4.457 | 4.456 | Heater induced quench at 3000 A with 200 V |
| tqs01.Quench.070305130113.865 |  | 1265 | -50 | -0.0218 | 0.19 | 4.443 | 4.442 | The PS trip at the ramp down at 1.5 kA at 50 A/s ramp down. |
| tqs01.Quench.070305145226.937 | 1 | 8526 | 20 | -0.0091 | 4.06 | 4.438 | 4.435 | Quench 01 at 8526 A, ramp = 20 A/s, T = 4.5 K - Threshold 500 mV |
| tqs01.Quench.070305152334.542 |  | 967 | 0 | -0.6028 | 0.67 | 4.441 | 4.440 | Quench 02 (trip?) I = 983A, ramp=20A/s, T=4.5K Spike |
| tqs01.Quench.070305153611.382 |  | 1649 | 19 | -0.0070 | 0.24 | 4.441 | 4.440 | Quench 03 I = 1650A, ramp = 20 A/s, T = 4.5K Spike ==> new threshold 600 mV |
| tqs01.Quench.070305160411.523 | 2 | 8973 | 20 | -0.0085 | 4.16 | 4.441 | 4.439 | quench 04 I = 8970 A, ramp = 20 A/s, T = 4.5K |
| tqs01.Quench.070305163721.108 | 3 | 9160 | 20 | -0.0073 | 4.15 | 4.447 | 4.445 | quench 05, I = 9163 A, ramp = 20 A/s, T = 4.45K |
| tqs01.Quench.070305170415.947 | 4 | 9302 | 20 | -0.0118 | 4.61 | 4.445 | 4.443 | quench 06 I = 9299 A, ramp = 20 A/s, T = 4.5K |
| tqs01.Quench.070305172159.668 |  | 1477 | 20 | -0.0346 | 0.26 | 4.445 | 4.442 | quench 07 I = 1480 A, ramp = 20 A/s, T = 4.5K Spike |
| tqs01.Quench.070305174414.221 | 5 | 9286 | 20 | -0.0115 | 4.57 | 4.451 | 4.446 | quench 08, I = 9280 A, ramp = 20 A/s, T = 4.5 K |
| tqs01.Quench.070305180959.938 | 6 | 9431 | 20 | -0.0069 | 4.24 | 4.445 | 4.444 | Quench 09, I = 9433 A, ramp = 20 A/s, T = 4.5K |
| tqs01.Quench.070305182226.273 |  | 1010 | 20 | -0.0839 | 0.19 | 4.444 | 4.443 | quench 10, I = 1015A, ramp = 20 A/s, T = 4.5K Spike ==> new threshold 700 mV |
| tqs01.Quench.070305190700.267 | 7 | 9479 | 20 | -0.0095 | 4.51 | 4.447 | 4.445 | Quench 11, I = 9479 A, ramp = 20 A/s, T = 4.5K |
| tqs01.Quench.070305193141.398 | 8 | 9551 | 20 | -0.0111 | 4.66 | 4.447 | 4.446 | quench 12, I = 9548 A, ramp = 20 A/s, T = 4.5k |
| tqs01.Quench.070305195537.447 | 9 | 9562 | 19 | -0.0077 | 4.37 | 4.455 | 4.451 | quench 13, I = 9562 A, ramp = 20 A/s, T = 4.5 K |
| tqs01.Quench.070305203017.539 | 10 | 9571 | 20 | -0.0059 | 4.20 | 4.457 | 4.453 | quench 14, I = 9569 A, ramp = 20 A/s, T = 4.5Kx |
| tqs01.Quench.070305205903.158 | 11 | 9556 | 19 | -0.0066 | 4.25 | 4.466 | 4.461 | quench 15, I = 9556 A, ramp = 20 A/s, T = 4.5 K |
| tqs01.Quench.070306094115.736 | 12 | 9574 | 20 | -0.0069 | 4.35 | 4.451 | 4.453 | 20 A/s ramp to quench, at Iq=9570A |
| tqs01.Quench.070306103252.831 | 13 | 9557 | 20 | -0.0220 | 4.3 | 4.452 | 4.451 | Quench 17, I= 9577 A, Rate 20A/sec, T=4.5K |
| tqs01.Quench.070306155027.170 | 14 | 9596 | 20 | -0.0034 | 4.09 | 1.870 | 1.870 | Quench 18, I = 9592 A, ramp = 20 A/s, T = 1.9K |
| tqs01.Quench.070306161411.908 | 15 | 9416 | 20 | -0.0123 | 4.80 | 1.875 | 1.874 | quench 19, I = 9412 A, ramp = 20 A/s, T = 1.9K |
| tqs01.Quench.070306164441.720 | 16 | 9622 | 20 | -0.0116 | 4.86 | 1.855 | 1.855 | quench 20, I = 9618 A, ramp = 20 A/s, T = 1.87 K |
| tqs01.Quench.070306171458.775 | 17 | 9665 | 20 | -0.0109 | 4.81 | 1.845 | 1.846 | quench 21, I = 9665 A, ramp = 20 A/s, T = 1.85 K |
| tqs01.Quench.070306174825.503 | 18 | 9640 | 20 | -0.0116 | 4.87 | 1.888 | 1.888 | quench 22, I = 9636 A, ramp = 20 A/s, T = 1.85 K |
| tqs01.Quench.070306181517.269 | 19 | 9735 | 20 | -0.0062 | 4.40 | 1.872 | 1.884 | quench 23, I = 9731 A, ramp = 20 A/s, T = 1.9 K |
| tqs01.Quench.070306184224.483 | 20 | 9791 | 19 | -0.0111 | 4.89 | 1.882 | 1.882 | quench 24, I = 9787 A, ramp = 20 A/s, T = 1.9 K |
| tqs01.Quench.070306191115.374 | 21 | 9871 | 20 | -0.0158 | 5.39 | 1.881 | 1.890 | quench 25, I = 9850 A, ramp = 20 A/s, T = 1.9 K |
| tqs01.Quench.070306193953.193 | 22 | 9942 | 20 | -0.0039 | 4.27 | 1.887 | 1.888 | quench 26, I = 9938 A, ramp = 20 A/s, T = 1.9 K |
| tqs01.Quench.070306200723.408 | 23 | 9964 | 20 | -0.0067 | 4.55 | 1.908 | 1.900 | quench 27, I = 9962 A, ramp = 20 A/s, T = 1.9 K |
| tqs01.Quench.070306203509.877 | 24 | 10021 | 20 | -0.0105 | 4.97 | 1.903 | 1.910 | quench 28, I = ???, ramp = 20 A/s, T = 1.9 K |
| tqs01.Quench.070306205957.757 | 25 | 10065 | 20 | -0.0105 | 4.97 | 1.906 | 1.900 | quench 29, I = 10061 A, ramp = 20 A/s, T = 1.9 K |
| tqs01.Quench.070307122242.539 | 26 | 10092 | 20 | -0.0032 | 4.33 | 1.889 | 1.876 | Quench 30, I=10091A, ramp=20A/s, Te=1.88K |
| tqs01.Quench.070307125355.444 | 27 | 10144 | 20 | -0.0064 | 4.59 | 1.867 | 1.868 | quench 31, I = 10142 A, ramp = 20 A/s, T = 1.9 K |
| tqs01.Quench.070307132153.951 | 28 | 10214 | 20 | -0.0041 | 4.38 | 1.866 | 1.855 | quench 32, I ???, ramp = 20 A/s, T = 1.9 K |
| tqs01.Quench.070307134902.477 | 29 | 10224 | 20 | -0.0036 | 4.35 | 1.861 | 1.862 | quench 33, I = 10224 A, ramp = 20 A/s, T = 1.9K |
| tqs01.Quench.070307141553.052 | 30 | 10314 | 20 | -0.0038 | 4.38 | 1.866 | 1.871 | quench 34, I = 10310 A, ramp = 20 A/s, T = 1.9K |
| tqs01.Quench.070307144317.298 | 31 | 10340 | 20 | -0.0031 | 4.33 | 1.850 | 1.852 | quench 35, I = 10337 A, ramp = 20 A/s, T = 1.9 K |
| tqs01.Quench.070307150619.194 | 32 | 10100 | 20 | -0.0032 | 4.26 | 1.877 | 1.878 | quench 36, I = 10095, ramp = 20 A/s, T = 1.9 K |
| tqs01.Quench.070307153312.160 | 33 | 10403 | 20 | -0.0088 | 5.00 | 1.847 | 1.847 | quench 37, I = 10397 A, ramp = 20 A/s, T = 1.9 K |
| tqs01.Quench.070307160632.489 |  | 10167 | 20 | -0.0001 | 3.50 | 1.857 | 1.861 | Quench 38, I=10127A, rate=20A/sec, T=1.9K, trip on leads |
| tqs01.Quench.070307164633.855 |  | 10427 | 20 | 0.0000 | 3.53 | 1.883 | 1.884 | Quench 30, trip on leads, I=10324A, rate =20A/s. |
| tqs01.Quench.070307171026.323 | 34 | 10463 | 21 | -0.0036 | 4.43 | 1.891 | 1.892 | quench 40, I = 10458 A, ramp = 20 A/s, T = 1.9 K |
| tqs01.Quench.070307174230.151 | 35 | 10492 | 20 | -0.0028 | 4.35 | 1.875 | 1.879 | Quench 41, AQD_Coil trip, I=10488A, rate=20A/s, Te=1.89K |
| tqs01.Quench.070307180946.997 | 36 | 10475 | 20 | -0.0031 | 4.37 | 1.904 | 1.906 | quench 42, I = 10469 A, ramp = 20 A/s T = 1.95 K |
| tqs01.Quench.070307184423.091 | 37 | 10484 | 20 | -0.0029 | 4.37 | 1.899 | 1.900 | Quench 43, I=10481A. Rate=20A/sec. Te=1.9K |
| tqs01.Quench.070307191706.650 | 38 | 10479 | 20 | -0.0031 | 4.38 | 1.846 | 1.846 | Quench 44 on coil, I=10478A, Rate=20A/s. Te=1.88K. |
| tqs01.Quench.070307195232.095 | 39 | 10499 | 19 | -0.0029 | 4.38 | 1.868 | 1.869 | Quench 45 on coil, I=10497A, Rate=20A/s. Te=1.88K. |
| tqs01.Quench.070307202125.595 | 40 | 10501 | 19 | -0.0032 | 4.40 | 1.885 | 1.886 | Quench 46 on coil, I=10499A., Rate=20A/s, Te=1.89K. |
| tqs01.Quench.070308100050.836 | 41 | 10526 | 4 | -0.0088 | 5.08 | 1.902 | 1.903 | Quench 47, I=10521A, Rate=20A/s (up to 10kA) and 5A/s (after 10kA). Te=1.9K |
| tqs01.Quench.070308103901.200 | 42 | 10489 | 4 | -0.0081 | 4.93 | 1.868 | 1.869 | Quench 48, I=10488A. Rate=20A/s(upto 10kA) and 5A/s(after 10kA). Te=1.89K. |
|  | 43 | 10350 | 50 |  |  |  |  | Quench during magnetic measurement - Lost data |
| tqs01.Quench.070308201410.017 |  | 0 | 0 | 0.0000 | 0.00 | 0.000 | 0.000 |  |
| tqs01.Quench.070309105948.717 |  | 0 | 0 | 0.0000 | 0.00 | 0.000 | 0.000 |  |
|  | 44 | 10477 | 20 |  |  | 1.900 | 1.900 | Lost data |
| tqs01.Quench.070309113209.493 | 45 | 10135 | 19 | -0.0046 | 4.39 | 2.605 | 2.615 | quench 50, I = 10134 A, ramp = 20 A/s, T = 2.6K |
| tqs01.Quench.070309121142.921 | 46 | 9966 | 20 | -0.0053 | 4.38 | 3.219 | 3.236 | quench 51, I = 9964 A, ramp = 20 A/s, T = 3.25 K |
| tqs01.Quench.070309123515.618 | 47 | 9858 | 19 | -0.0055 | 4.33 | 3.583 | 3.594 | quench 52, I = 9854 A, ramp 20 A/s, T = 3.58 K |
| tqs01.Quench.070309140937.832 | 48 | 9701 | 20 | -0.0067 | 4.40 | 3.992 | 4.003 | quench 53, Te=4.0K, I=~9800A (will put the exact numbers in comment), rate=20A/s. |
| tqs01.Quench.070309144928.641 | 49 | 9602 | 19 | -0.0060 | 4.22 | 4.416 | 4.414 | quench 54 at I=9601A. T=4.4K, Rate=20A/s. |
| tqs01.Quench.070309152808.566 |  | 3001 | 0 | -0.0813 | 1.38 | 4.430 | 4.427 | quench 55, protection heater studies, I=3000A, T=4.4K, Rate=20A/s. hfu_02 at 200V fired the quench. |
| tqs01.Quench.070309154324.746 |  | 1118 | -20 | -0.0435 | 0.18 | 4.430 | 4.430 | Quench 56 when ramping down - Shlomo requested 2 more quenches at 4.5K to see the magnet performance - Spike |
| tqs01.Quench.070309162018.346 | 50 | 9601 | 20 | -0.0063 | 4.26 | 4.441 | 4.438 | quench 56, I=9598A at 4.44K, rate=20A/s. |
| tqs01.Quench.070309164511.289 | 51 | 9603 | 20 | -0.0060 | 4.22 | 4.451 | 4.446 | Quench 58 at I=9601A, rate=20A/s and Te=4.4K. |
| tqs01.Quench.070309171106.013 |  | 3003 | 0 | -0.0456 | 1.05 | 4.442 | 4.438 | Quench 59, heater studies going on. I=3000A, Te=4.4K, Fired HFU_02 at 300V. |
| tqs01.Quench.070309172722.734 |  | 3001 | 0 | -0.0392 | 0.99 | 4.442 | 4.437 | Quench 60, I=3000A, Te=4.4K, hfu_02 fired at 400V. |
| tqs01.Quench.070309175051.493 |  | 5001 | 0 | -0.0211 | 2.07 | 4.445 | 4.440 | Quench 61, I=5000A. Te=4.4K, fired hfu_02 at 400V. |
| tqs01.Quench.070309180721.594 |  | 5004 | 0 | -0.0272 | 2.23 | 4.443 | 4.439 | Quench 62, I=5000A, Rate=20A/s, Te=4.4K, fired hfu_02. |
| tqs01.Quench.070309182905.477 |  | 5003 | 0 | -0.0423 | 2.62 | 4.437 | 4.435 | Quench 63, I=5000A, Te=4.4K, fired hfu_02 at 200V |
| tqs01.Quench.070309185336.279 |  | 8006 | 0 | -0.0202 | 4.30 | 4.443 | 4.439 | Quench 64, I=8000A, Rate=20A/s, Te=4.4K, fired hfu_02 at 200V. |
| tqs01.Quench.070309191753.369 |  | 8006 | 0 | -0.0130 | 3.80 | 4.446 | 4.438 | Quench 65, I=8000A, Te=4.4K, fired hfu_02 at 300V. |
| tqs01.Quench.070309194032.957 |  | 8004 | 0 | -0.0105 | 3.63 | 4.454 | 4.453 | Quench 66, I=8000A, Te=4.4K, fired hfu_02 at 400V |
| tqs01.Quench.070309200939.358 |  | 9411 | 0 | -0.0076 | 4.12 | 4.438 | 4.438 | Quench 67, I=9400A, Rate=20A/s, Te=4.4K. Fired hfu_02 at 400V. |
| tqs01.Quench.070309203322.207 |  | 9405 | 0 | -0.0091 | 4.28 | 4.446 | 4.442 | Quench 68, I=9400A, 20A/s, Te=4.4K, fired hfu_02 at 300V. |
| tqs01.Quench.070309205458.892 |  | 9406 | 0 | -0.0143 | 4.75 | 4.449 | 4.445 | Quench 69, I=9400A., Te=4.4K, fired hfu_02 at 200V. |
| tqs01.Quench.070312164435.878 | 52 | 9603 | 20 | -0.0060 | 4.26 | 4.427 | 4.426 | Quench 70, we started ramp rate study at 4.4K. I=9607A at 20A/s. |
| tqs01.Quench.070312170656.263 | 53 | 9359 | 100 | -0.0134 | 4.76 | 4.446 | 4.445 | quench 71, I = 9359 A, ramp = 100 A/s, T = 4.44K |
| tqs01.Quench.070312172903.316 | 54 | 9291 | 122 | -0.0118 | 4.57 | 4.445 | 4.446 | quench 72, I = 9292 A, ramp 200 A/s, T = 4.45 K |
| tqs01.Quench.070312175026.599 | 55 | 9101 | 200 | -0.0125 | 4.51 | 4.429 | 4.431 | quench 73, I = 9099 A, ramp = 200 A/s, T = 4.4 K |
| tqs01.Quench.070312181453.187 | 56 | 8411 | 300 | -0.0048 | 3.47 | 4.439 | 4.436 | Quench 74 at I=8411A, Rate=300A, T=4.4K. |
| tqs01.Quench.070312184626.003 | 57 | 3170 | 352 | -0.1616 | 2.39 | 4.435 | 4.430 | Quench 75 at I=3227A, Rate=400A/s. T=4.4K |
| tqs01.Quench.070312190734.194 | 58 | 8966 | 250 | -0.0147 | 4.60 | 4.437 | 4.433 | Quench 76 at I=8967A, rate=250A/s. T=4.4K. |
| tqs01.Quench.070312192553.589 | 59 | 3225 | 350 | -0.0143 | 0.89 | 4.433 | 4.431 | quernch 77, I = 3231 A, ramp = 350 A/s, T = 4.4 K |
| tqs01.Quench.070312195617.882 | 60 | 8966 | 250 | -0.0134 | 5.47 | 4.441 | 4.433 | quench 78, I = 8968 A, ramp = 250 A/s, T = 4.43 K, dump delay = 25 ms |
| tqs01.Quench.070312202058.433 | 61 | 8978 | 250 | -0.0129 | 6.05 | 4.437 | 4.434 | quench 79, I = 8978 A, ramp = 250 A/s, T = 4.45K dump delay = 45 ms |
| tqs01.Quench.070313094326.023 |  | 4 | 0 | -0.0035 | 0.00 | 4.437 | 4.434 |  |
| tqs01.Quench.070313121853.733 | 62 | 9614 | 20 | -0.0063 | 4.27 | 0.000 | 0.000 | ramp = 20 A/s, Dump 5 ms |
| tqs01.Quench.070313123808.269 |  | 0 | 0 | -0.0020 | 0.00 | 0.000 | 0.000 |  |
| tqs01.Quench.070313130308.171 | 63 | 9097 | 198 | -0.0123 | 6.39 | 0.000 | 0.000 | ramp = 250 A/s, Dump 65 ms |
| tqs01.Quench.070313134409.170 | 64 | 9611 | 20 | -0.0066 | 4.23 | 0.000 | 0.000 | ramp = 20 A/s, Dump 5 ms |
| tqs01.Quench.070313140831.009 | 65 | 8981 | 250 | -0.0127 | 6.51 | 4.453 | 4.444 | ramp = 250 A/s, Dump 90 ms |
| tqs01.Quench.070313152204.724 | 66 | 9615 | 20 | -0.0070 | 4.28 | 4.433 | 4.427 | ramp = 20 A/s, Dump 5 ms |
| tqs01.Quench.070313154137.591 | 67 | 8981 | 250 | -0.0160 | 6.87 | 4.437 | 4.432 | ramp = 250 A/s, Dump 200 ms |
| tqs01.Quench.070313161252.035 | 68 | 9617 | 19 | -0.0071 | 4.29 | 4.441 | 4.436 | quench 86, I = 9617 A, ramp = 20 A/s, T = 4.45K |
| tqs01.Quench.070313164459.088 | 69 | 9616 | 20 | -0.0066 | 5.97 | 4.445 | 4.439 | quench 87, I = 9618 A, ramp = 20 A/s, T = 4.43K, Dump delay 50 ms |
| tqs01.Quench.070313171540.528 | 70 | 9616 | 20 | -0.0064 | 6.27 | 4.443 | 4.437 | quench 88, I = 9614 A, ramp = 20 A/s, T = 4.44 K, Dump dealy 100 ms |
| tqs01.Quench.070313174803.661 | 71 | 9632 | 20 | -0.0069 | 6.34 | 4.443 | 4.438 | quench 89, I = 9629 A, ramp = 20 A/s, T = 4.44K, Dump delay 250 ms |
| tqs01.Quench.070313182743.141 | 72 | 9630 | 19 | -0.0064 | 6.83 | 4.440 | 4.439 | Quench 90, I=9628A, Dump delay 257ms, Heater delay 7.6ms, rate=20A/s, T=4.4K. |
| tqs01.Quench.070313190544.467 | 73 | 9641 | 20 | -0.0073 | 7.50 | 4.437 | 4.431 | quench 91, I = 9640 A, ramp = 20 A/s, T = 4.4K, Dump delay 265 ms, PHeater delay 15.6 ms�Rate |
| tqs01.Quench.070313194543.628 | 74 | 9612 | 20 | -0.0084 | 7.95 | 4.435 | 4.431 | quench 92, I = 9611, ramp = 20 A/s, T = 4.4K, Dump delay 270 ms, PHeater delay 21.2 ms |
| tqs01.Quench.070313202919.217 | 75 | 9926 | 20 | -0.0071 | 8.16 | 4.434 | 4.432 | quench 93, I = 9924 A, ramp = 20 A/s, T = 4.43K, Dump 276 ms PHeater 27.3 ms |
| tqs01.Quench.070313205845.334 | 76 | 9211 | 19 | -0.0101 | 4.39 | 4.438 | 4.430 | quench 94, I = 9212 A, ramp = 20 A/s, T = 4.44 K, Dump 5 ms, PHeater 0 ms |
| tqs01.Quench.070313212139.437 | 77 | 9927 | 20 | -0.0063 | 4.33 | 4.434 | 4.435 | quench 95, I = 9928 A, ramp = 20 A/s, T = 4.4 K, Dump 5 ms, PHeater 0 ms |
| tqs01.Quench.070313214428.697 | 78 | 9924 | 20 | -0.0057 | 4.28 | 4.439 | 4.432 | quench 96, I = 9922 A, ramp = 20 A/s, T = 4.4 K, dump 5 ms, PHeater 0 ms |
| tqs01.Quench.070314143026.727 |  | 1 | 0 | -0.1945 | 0.04 | 4.428 | 4.428 | don't know why - no welding. save data to look at the cause. |
| tqs01.Quench.070314144411.388 | 79 | 9918 | 19 | -0.0060 | 4.36 | 4.436 | 4.431 | quench 97, I = 9912 A, ramp = 20 A/s, T = 4.45 K, dump 5 ms |
| tqs01.Quench.070314172755.661 | 80 | 9923 | 20 | -0.0062 | 8.07 | 4.431 | 4.429 | quench 98, I = 9922 A, ramp = 20 A/s, T = 4.45 K Dump 280 ms, PHeater 30.7 ms |
| tqs01.Quench.070314181635.332 | 81 | 9703 | 20 | -0.0041 | 4.06 | 4.449 | 4.444 | quench 99, I = 9699 A, ramp = 20 A/s, T = 4.45 K, standard dump and heater delay |
| tqs01.Quench.070314184853.444 | 82 | 9989 | 20 | -0.2071 | 4.40 | 4.441 | 4.432 | quench 100, I = 9990 A, ramp = 20 A/s, T = 4.45 K, standard delays |
| tqs01.Quench.070314194009.492 | 83 | 9983 | 20 | -0.0035 | 7.82 | 4.450 | 4.440 | quench 101, I = 9980 A, ramp = 20 A/s, T = 4.44 K, dump 289 ms, Protect heater 40 ms |
| tqs01.Quench.070314202926.124 | 84 | 9792 | 20 | -0.0064 | 4.31 | 4.459 | 4.447 | quench 102, I = 9790 A, ramp = 20 A/s, T = 4.45 K, no delays |
| tqs01.Quench.070314205544.003 | 85 | 9982 | 20 | -0.0046 | 4.18 | 4.448 | 4.442 | quench 103, I = 9977 A, ramp = 20 A/s, T = 4.44 K, NO delays |
| tqs01.Quench.070315115603.030 | 86 | 9977 | 19 | -0.0042 | 4.22 | 4.451 | 4.447 | quench 104, I = 9974 A, ramp = 20 A/s, T = 4.45 K, detect thres 1.25 V, standard delays |
| tqs01.Quench.070315123423.553 | 87 | 9979 | 20 | -0.0064 | 7.51 | 4.455 | 4.453 | Quench 105, I=9975.3A, detect thresh=1.25V, Dump delay 300ms, Heater delay 80ms, rate=20A/s, T=4.44K |
| tqs01.Quench.070315130807.526 | 88 | 9925 | 20 | -0.0091 | 4.59 | 4.458 | 4.451 | quench 106, I = 9922 A, ramp = 20 A/s, T = 4.44K , standard delays |
| tqs01.Quench.070315135406.786 | 89 | 9935 | 20 | -0.0059 | 7.54 | 4.448 | 4.446 | quench 107, I = 9930 A, ramp = 20 A/s, T = 4.4K, Dump 300 ms, Heaters 100 ms |
| tqs01.Quench.070315143047.299 | 90 | 9872 | 20 | -0.0097 | 7.75 | 4.456 | 4.453 | quench 108, ramp = 20 A/s, T = 4.44K Dump 300 ms, NO heaters, detection 3V |
| tqs01.Quench.070315153507.444 | 91 | 9770 | 20 | -0.0134 | 8.08 | 4.453 | 4.449 | quench 109, I = 9765 A, ramp = 20 A/s, T = 4.45 K Dump 300 ms, NO heaters, detect 4V |
| tqs01.Quench.070315183145.732 | 92 | 9487 | 20 | -0.0136 | 8.70 | 4.455 | 4.452 | quench 110, I = 9480 A, ramp = 20 A/s, T = 4.45K, Detection 7V, Dump 300 ms, NO heaters |
| tqs01.Quench.070315191243.471 | 93 | 8785 | 20 | -0.0245 | 5.22 | 4.461 | 4.460 | quench 111, I = 8781 A, ramp = 20 A/s, T = 4.45K, standard delays |
| tqs01.Quench.070315193942.342 | 94 | 8814 | 20 | -0.0238 | 5.18 | 4.450 | 4.443 | quench 112, I = 8811 A, ramp = 20 A/s, T = 4.44K, standard delays |
| tqs01.Quench.070315200356.056 | 95 | 8819 | 20 | -0.0262 | 5.35 | 4.457 | 4.451 | quench 113, I = 8811 A, ramp = 20 A/s, T = 4.45K, Standard delays |
| tqs01.Quench.070315203136.000 | 96 | 8822 | 20 | -0.0241 | 5.20 | 4.459 | 4.449 | quench 114, I = 8818 A, ramp = 20 A/s, T = 4.45K, standard delays |
| tqs01.Quench.070315205716.269 | 97 | 8822 | 20 | -0.0238 | 9.53 | 4.458 | 4.457 | quench 115, I = 8817 A, ramp = 20 A/s, T = 4.45K, dump 300 ms, NO heaters, Detect 7V |
| tqs01.Quench.070315213106.928 | 98 | 7148 | 20 | -0.0489 | 5.09 | 4.459 | 4.456 | quench 116, I = 7145, ramp = 20 A/s, T = 4.45K, standard delays |
| tqs01.Quench.070316100850.826 | 99 | 7184 | 20 | -0.0442 | 4.96 | 4.453 | 4.450 | quench 117, I = 7180 A, ramp = 20 A/s, T = 4.45 K, standard delays |
| tqs01.Quench.070316103450.084 | 100 | 7200 | 20 | -0.0483 | 5.11 | 4.455 | 4.447 | quench 118, I=7196 A. Rate=20A/s, T=4.4K, standard delays. |
| tqs01.Quench.070316110436.334 | 101 | 7207 | 20 | -0.0451 | 4.97 | 4.458 | 4.451 | Quench 119, I=7203A. Rate=20A/s, T=4.4K, standard delays. |

| TQS01c Quench History table with first quenching segments |
| --- |
| File | Q No. | Current | dI/dt | tquench | QDC | 1st VTseg | trise | 2nd VTseg | trise | 3rd VTseg | trise | VSDS run |
| tqs01.Quench.070227164332.150 |  | 3 | 0 | 1.0000 | GndRef | ------------ | ---- | ------------ | ---- | ------------ | ---- |  |
| tqs01.Quench.070302162331.717 |  | 967 | 72 | -0.0057 | WcoilGnd | 08A3_08A2 | -0.0034 | 08A7_08A6 | -0.0034 | 08B2_08B3 | -0.0029 |  |
| tqs01.Quench.070302173255.243 |  | 1470 | 100 | -0.0001 | WcoilGnd | 08A8_08A7 | -0.0094 | 08B5_08A8 | -0.0087 | 08B1_08B2 | -0.0066 |  |
| tqs01.Quench.070302180720.696 |  | 1574 | 19 | -0.0070 | HcoilHcoil | 05B5_05B4 | -0.0049 | 05A2_05A3 | -0.0046 | 05B3_05B2 | -0.0046 |  |
| tqs01.Quench.070302182651.634 |  | 3002 | 0 | -0.0748 | HcoilHcoil | 05B2_05B1 | -0.0109 | 05B3_05B2 | -0.0091 | 08B2_08B3 | -0.0074 |  |
| tqs01.Quench.070305130113.865 |  | 1265 | -50 | -0.0218 | HcoilHcoil | 07B2_07B3 | -0.0214 | 08A3_08A2 | -0.0214 | 08B1_08B2M_2 | -0.0213 |  |
| tqs01.Quench.070305145226.937 | 1 | 8526 | 20 | -0.0091 | HcoilHcoil | 15A6_15A8 | -0.0098 | 15A5_15A6 | -0.0085 | 05A1_05A2M_2 | -0.0056 | 1 |
| tqs01.Quench.070305152334.542 |  | 967 | 0 | -0.6028 | HcoilHcoil | 15A6_15A8 | -0.0067 | 05A2_05A3 | -0.0060 | 05B3_05B2 | -0.006 | 2 |
| tqs01.Quench.070305153611.382 |  | 1649 | 19 | -0.0070 | HcoilHcoil | 15A5_15A6 | -0.0063 | 15A4_15A5 | -0.0060 | 15A6_15A8 | -0.0053 | 3 |
| tqs01.Quench.070305160411.523 | 2 | 8973 | 20 | -0.0085 | HcoilHcoil | 15A6_15A8 | -0.0094 | 05B5_05B4 | -0.0056 | 05A1_05A2M_2 | -0.0056 | 4 |
| tqs01.Quench.070305163721.108 | 3 | 9160 | 20 | -0.0073 | HcoilHcoil | 15A6_15A8 | -0.0077 | 15A5_15A6 | -0.0067 | 15A8_15B6 | -0.0015 | 5 |
| tqs01.Quench.070305170415.947 | 4 | 9302 | 20 | -0.0118 | HcoilHcoil | 07A7_07A6 | -0.0050 | 07B3_07B4 | -0.0031 | V1_TrigCvtB2 | -0.0003 | 6 |
| tqs01.Quench.070305172159.668 |  | 1477 | 20 | -0.0346 | HcoilHcoil | 08B4_08B5 | -0.0193 | 15A6_15A8 | -0.0052 | 15A4_15A5 | -0.005 | 7 |
| tqs01.Quench.070305174414.221 | 5 | 9286 | 20 | -0.0115 | HcoilHcoil | 07A8_07A7 | -0.0119 | 05A2_05A3 | -0.0053 | 08A3_08A2 | -0.0053 | 8 |
| tqs01.Quench.070305180959.938 | 6 | 9431 | 20 | -0.0069 | HcoilHcoil | 15A6_15A8 | -0.0077 | 05A1_05A2M_2 | -0.0042 | 05A2_05A3 | -0.0041 | 9 |
| tqs01.Quench.070305182226.273 |  | 1010 | 20 | -0.0839 | HcoilHcoil | 08A7_08A6 | -0.0035 | 08B2_08B3 | -0.0035 | 08A3_08A2 | -0.0034 | 10 |
| tqs01.Quench.070305190700.267 | 7 | 9479 | 20 | -0.0095 | HcoilHcoil | 15A8_15B6 | -0.0105 | 15A6_15A8 | -0.0062 | 05B5_05B4 | -0.0053 | 11 |
| tqs01.Quench.070305193141.398 | 8 | 9551 | 20 | -0.0111 | HcoilHcoil | 08B5_08A8 | -0.0118 | 08A8_08A7 | -0.0105 | 08A6_08A5 | -0.005 | 12 |
| tqs01.Quench.070305195537.447 | 9 | 9562 | 19 | -0.0077 | HcoilHcoil | 15A6_15A8 | -0.0078 | 15A5_15A6 | -0.0062 | 05A5_05A6 | -0.0031 | 13 |
| tqs01.Quench.070305203017.539 | 10 | 9571 | 20 | -0.0059 | HcoilHcoil | 15A6_15A8 | -0.0071 | 15A5_15A6 | -0.0034 | 05A5_05A6 | -0.002 | 14 |
| tqs01.Quench.070305205903.158 | 11 | 9556 | 19 | -0.0066 | HcoilHcoil | 15A6_15A8 | -0.0071 | 15A5_15A6 | -0.0032 | V1_TrigCvtB2 | -0.0003 | 15 |
| tqs01.Quench.070306094115.736 | 12 | 9574 | 20 | -0.0069 | HcoilHcoil | 15A6_15A8 | -0.0070 | 15A5_15A6 | -0.0041 | 05A2_05A3 | -0.0022 | 16 |
| tqs01.Quench.070306103252.831 | 13 | 9557 | 20 | -0.0220 | HcoilHcoil | 15A6_15A8 | -0.0074 | 05A2_05A3 | -0.0041 | 05B3_05B2 | -0.0039 | 17 |
| tqs01.Quench.070306155027.170 | 14 | 9596 | 20 | -0.0034 | HcoilHcoil | 15A8_15B6 | -0.0042 | 15A6_15A8 | -0.0041 | 15B6_15B5 | -0.0024 | 18 |
| tqs01.Quench.070306161411.908 | 15 | 9416 | 20 | -0.0123 | HcoilHcoil | 07A8_07A7 | -0.0136 | 08B2_08B3 | -0.0088 | 05A5_05A6 | -0.0087 | 19 |
| tqs01.Quench.070306164441.720 | 16 | 9622 | 20 | -0.0116 | HcoilHcoil | 05A6_05A7 | -0.0130 | 05A1_05A2M_2 | -0.0108 | 15A2_15A3 | -0.0073 | 20 |
| tqs01.Quench.070306171458.775 | 17 | 9665 | 20 | -0.0109 | HcoilHcoil | 08A7_08A6 | -0.0123 | 08A5_08A4 | -0.0080 | 07B2_07B3 | -0.0073 | 21 |
| tqs01.Quench.070306174825.503 | 18 | 9640 | 20 | -0.0116 | HcoilHcoil | 08B5_08A8 | -0.0132 | 08A4_08A3 | -0.0105 | 08A5_08A4 | -0.009 | 22 |
| tqs01.Quench.070306181517.269 | 19 | 9735 | 20 | -0.0062 | HcoilHcoil | 15A8_15B6 | -0.0076 | 15A5_15A6 | -0.0045 | 05A2_05A3 | -0.0038 | 23 |
| tqs01.Quench.070306184224.483 | 20 | 9791 | 19 | -0.0111 | HcoilHcoil | 07A8_07A7 | -0.0119 | 08A3_08A2 | -0.0091 | 08B2_08B3 | -0.0091 | 24 |
| tqs01.Quench.070306191115.374 | 21 | 9871 | 20 | -0.0158 | HcoilHcoil | 15A6_15A8 | -0.0066 | 15A5_15A6 | -0.0041 | 05A5_05A6 | -0.0022 | 25 |
| tqs01.Quench.070306193953.193 | 22 | 9942 | 20 | -0.0039 | HcoilHcoil | 15A6_15A8 | -0.0045 | 15A5_15A6 | -0.0034 | 15A8_15B6 | -0.0028 | 26 |
| tqs01.Quench.070306200723.408 | 23 | 9964 | 20 | -0.0067 | WcoilIdot | 15A6_15A8 | -0.0053 | 15A5_15A6 | -0.0041 | 15B6_15B5 | -0.0028 | 27 |
| tqs01.Quench.070306203509.877 | 24 | 10021 | 20 | -0.0105 | HcoilHcoil | 07A7_07A6 | -0.0049 | 07B3_07B4 | -0.0045 | 08A3_08A2 | -0.0015 | 28 |
| tqs01.Quench.070306205957.757 | 25 | 10065 | 20 | -0.0105 | HcoilHcoil | 07A8_07A7 | -0.0108 | 08B2_08B3 | -0.0045 | 05A5_05A6 | -0.0042 | 29 |
| tqs01.Quench.070307122242.539 | 26 | 10092 | 20 | -0.0032 | HcoilHcoil | 15A6_15A8 | -0.0045 | 15A5_15A6 | -0.0041 | 15A8_15B6 | -0.0025 | VSDS failure |
| tqs01.Quench.070307125355.444 | 27 | 10144 | 20 | -0.0064 | HcoilHcoil | 08B5_08A8 | -0.0070 | 08A7_08A6 | -0.0069 | 08A8_08A7 | -0.0067 |  |
| tqs01.Quench.070307132153.951 | 28 | 10214 | 20 | -0.0041 | HcoilHcoil | 15A8_15B6 | -0.0034 | 15A6_15A8 | -0.0028 | 15A5_15A6 | -0.0021 |  |
| tqs01.Quench.070307134902.477 | 29 | 10224 | 20 | -0.0036 | HcoilHcoil | 15A6_15A8 | -0.0038 | 15A5_15A6 | -0.0029 | 15A8_15B6 | -0.0027 |  |
| tqs01.Quench.070307141553.052 | 30 | 10314 | 20 | -0.0038 | HcoilHcoil | 15A6_15A8 | -0.0046 | 15A5_15A6 | -0.0036 | 05A5_05A6 | -0.0017 |  |
| tqs01.Quench.070307144317.298 | 31 | 10340 | 20 | -0.0031 | HcoilHcoil | 15A6_15A8 | -0.0038 | 15A5_15A6 | -0.0029 | 15A8_15B6 | -0.0022 |  |
| tqs01.Quench.070307150619.194 | 32 | 10100 | 20 | -0.0032 | HcoilHcoil | 15A6_15A8 | -0.0042 | 15A5_15A6 | -0.0032 | 15A8_15B6 | -0.0025 |  |
| tqs01.Quench.070307153312.160 | 33 | 10403 | 20 | -0.0088 | HcoilHcoil | 05A7_05B6 | -0.0102 | 05A6_05A7 | -0.0078 | 15B5_15B4 | -0.0032 |  |
| tqs01.Quench.070307160632.489 |  | 10167 | 20 | -0.0001 | WcoilGnd | V1_TrigCvtB2 | -0.0003 | 15A6_15A8 | -0.0001 | 15B4_15B3 | -0.0001 |  |
| tqs01.Quench.070307164633.855 |  | 10427 | 20 | 0.0000 | WcoilGnd | 15A6_15A8 | -0.0001 | 15B4_15B3 | -0.0001 | V1_TrigCvtB2 | -0.0001 |  |
| tqs01.Quench.070307171026.323 | 34 | 10463 | 21 | -0.0036 | HcoilHcoil | 15A6_15A8 | -0.0048 | 15A5_15A6 | -0.0035 | 15B6_15B5 | -0.0024 |  |
| tqs01.Quench.070307174230.151 | 35 | 10492 | 20 | -0.0028 | HcoilHcoil | 15A6_15A8 | -0.0036 | 15A5_15A6 | -0.0028 | 15A8_15B6 | -0.002 |  |
| tqs01.Quench.070307180946.997 | 36 | 10475 | 20 | -0.0031 | HcoilHcoil | 15A6_15A8 | -0.0045 | 15A5_15A6 | -0.0028 | 15B6_15B5 | -0.0014 |  |
| tqs01.Quench.070307184423.091 | 37 | 10484 | 20 | -0.0029 | HcoilHcoil | 15A6_15A8 | -0.0043 | 15A5_15A6 | -0.0028 | 15B6_15B5 | -0.0021 |  |
| tqs01.Quench.070307191706.650 | 38 | 10479 | 20 | -0.0031 | HcoilHcoil | 15A6_15A8 | -0.0045 | 15A5_15A6 | -0.0031 | 15A4_15A5 | -0.0024 |  |
| tqs01.Quench.070307195232.095 | 39 | 10499 | 19 | -0.0029 | HcoilHcoil | 15A6_15A8 | -0.0042 | 05A2_05A3 | -0.0031 | 05A4_05A5 | -0.0031 |  |
| tqs01.Quench.070307202125.595 | 40 | 10501 | 19 | -0.0032 | HcoilHcoil | 15A6_15A8 | -0.0043 | 15A5_15A6 | -0.0027 | 05B3_05B2 | -0.0022 |  |
| tqs01.Quench.070308100050.836 | 41 | 10526 | 4 | -0.0088 | HcoilHcoil | 15B4_15B3 | -0.0097 | 15B5_15B4 | -0.0038 | 08A6_08A5 | -0.0018 |  |
| tqs01.Quench.070308103901.200 | 42 | 10489 | 4 | -0.0081 | HcoilHcoil | 15B4_15B3 | -0.0097 | 15B5_15B4 | -0.0039 | 05A5_05A6 | -0.0032 |  |
|  | 43 | 10350 | 50 |  |  |  |  |  |  |  |  |  |
| tqs01.Quench.070308201410.017 |  | 0 | 0 | 0.0000 |  | ------------ | ---- | ------------ | ---- | ------------ | ---- |  |
| tqs01.Quench.070309105948.717 |  | 0 | 0 | 0.0000 |  | ------------ | ---- | ------------ | ---- | ------------ | ---- |  |
|  | 44 | 10477 | 20 |  |  |  |  |  |  |  |  |  |
| tqs01.Quench.070309113209.493 | 45 | 10135 | 19 | -0.0046 | HcoilHcoil | 15A6_15A8 | -0.0050 | 15A5_15A6 | -0.0029 | 15B6_15B5 | -0.0021 |  |
| tqs01.Quench.070309121142.921 | 46 | 9966 | 20 | -0.0053 | HcoilHcoil | 15A6_15A8 | -0.0062 | 15A5_15A6 | -0.0031 | 15B6_15B5 | -0.0017 |  |
| tqs01.Quench.070309123515.618 | 47 | 9858 | 19 | -0.0055 | HcoilHcoil | 15A6_15A8 | -0.0063 | 15A5_15A6 | -0.0032 | 05A2_05A3 | -0.0024 |  |
| tqs01.Quench.070309140937.832 | 48 | 9701 | 20 | -0.0067 | HcoilHcoil | 15A6_15A8 | -0.0071 | 15A5_15A6 | -0.0050 | 05A1_05A2M_2 | -0.0022 |  |
| tqs01.Quench.070309144928.641 | 49 | 9602 | 19 | -0.0060 | HcoilHcoil | 15A6_15A8 | -0.0070 | 05A4_05A5 | -0.0036 | 05A5_05A6 | -0.0036 |  |
| tqs01.Quench.070309152808.566 |  | 3001 | 0 | -0.0813 | HcoilHcoil | 05B5_05B4 | -0.0808 | 05A2_05A3 | -0.0802 | 05B3_05B2 | -0.0795 |  |
| tqs01.Quench.070309154324.746 |  | 1118 | -20 | -0.0435 | HcoilHcoil | 15A6_15A8 | -0.0045 | 15B3_15B2 | -0.0029 | 15A2_15A3 | -0.0028 |  |
| tqs01.Quench.070309162018.346 | 50 | 9601 | 20 | -0.0063 | HcoilHcoil | 15A6_15A8 | -0.0071 | 15A5_15A6 | -0.0041 | 05A2_05A3 | -0.0029 |  |
| tqs01.Quench.070309164511.289 | 51 | 9603 | 20 | -0.0060 | HcoilHcoil | 15A6_15A8 | -0.0069 | 05B3_05B2 | -0.0057 | 05A5_05A6 | -0.0056 |  |
| tqs01.Quench.070309171106.013 |  | 3003 | 0 | -0.0456 | HcoilHcoil | 05B5_05B4 | -0.0459 | 08B4_08B5 | -0.0456 | 05A2_05A3 | -0.0434 |  |
| tqs01.Quench.070309172722.734 |  | 3001 | 0 | -0.0392 | HcoilHcoil | 08B4_08B5 | -0.0400 | 08A6_08A5 | -0.0398 | 05B3_05B2 | -0.0384 |  |
| tqs01.Quench.070309175051.493 |  | 5001 | 0 | -0.0211 | HcoilHcoil | 08B4_08B5 | -0.0242 | 05B5_05B4 | -0.0203 | 08A3_08A2 | -0.0189 |  |
| tqs01.Quench.070309180721.594 |  | 5004 | 0 | -0.0272 | HcoilHcoil | 08B4_08B5 | -0.0290 | 05B5_05B4 | -0.0262 | 05B3_05B2 | -0.0231 |  |
| tqs01.Quench.070309182905.477 |  | 5003 | 0 | -0.0423 | HcoilHcoil | 08B4_08B5 | -0.0451 | 05B5_05B4 | -0.0413 | 05B3_05B2 | -0.0209 |  |
| tqs01.Quench.070309185336.279 |  | 8006 | 0 | -0.0202 | HcoilHcoil | 08B4_08B5 | -0.0227 | 05B5_05B4 | -0.0192 | 08A3_08A2 | -0.0169 |  |
| tqs01.Quench.070309191753.369 |  | 8006 | 0 | -0.0130 | HcoilHcoil | 08B4_08B5 | -0.0154 | 08B3_08B4 | -0.0122 | 05B5_05B4 | -0.0118 |  |
| tqs01.Quench.070309194032.957 |  | 8004 | 0 | -0.0105 | HcoilHcoil | 08B4_08B5 | -0.0126 | 08B3_08B4 | -0.0112 | 05B5_05B4 | -0.0092 |  |
| tqs01.Quench.070309200939.358 |  | 9411 | 0 | -0.0076 | HcoilHcoil | 08B4_08B5 | -0.0098 | 08A6_08A5 | -0.0091 | 08A7_08A6 | -0.0085 |  |
| tqs01.Quench.070309203322.207 |  | 9405 | 0 | -0.0091 | HcoilHcoil | 08B4_08B5 | -0.0126 | 08B3_08B4 | -0.0088 | 05B5_05B4 | -0.0083 |  |
| tqs01.Quench.070309205458.892 |  | 9406 | 0 | -0.0143 | HcoilHcoil | 08B4_08B5 | -0.0168 | 05B5_05B4 | -0.0130 | 08B3_08B4 | -0.0126 |  |
| tqs01.Quench.070312164435.878 | 52 | 9603 | 20 | -0.0060 | HcoilHcoil | 15A6_15A8 | -0.0069 | 15A5_15A6 | -0.0028 | 05B5_05B4 | -0.0015 |  |
| tqs01.Quench.070312170656.263 | 53 | 9359 | 100 | -0.0134 | HcoilHcoil | 15A6_15A8 | -0.0106 | 15A5_15A6 | -0.0042 | V1_TrigCvtB2 | -0.0001 |  |
| tqs01.Quench.070312172903.316 | 54 | 9291 | 122 | -0.0118 | HcoilHcoil | 15A6_15A8 | -0.0113 | 15A5_15A6 | -0.0049 | V1_TrigCvtB2 | -0.0003 |  |
| tqs01.Quench.070312175026.599 | 55 | 9101 | 200 | -0.0125 | HcoilHcoil | 15A6_15A8 | -0.0129 | 15A5_15A6 | -0.0056 | V1_TrigCvtB2 | -0.0003 |  |
| tqs01.Quench.070312181453.187 | 56 | 8411 | 300 | -0.0048 | HcoilHcoil | 05A7_05B6 | -0.0048 | 05A2_05A3 | -0.0036 | 15A2_15A3 | -0.0032 |  |
| tqs01.Quench.070312184626.003 | 57 | 3170 | 352 | -0.1616 | HcoilHcoil | 05A3_05A4 | -0.0148 | 05A2_05A3 | -0.0146 | 05B3_05B2 | -0.0109 |  |
| tqs01.Quench.070312190734.194 | 58 | 8966 | 250 | -0.0147 | HcoilHcoil | 15A6_15A8 | -0.0137 | 05A1_05A2M_2 | -0.0076 | 15A5_15A6 | -0.0063 |  |
| tqs01.Quench.070312192553.589 | 59 | 3225 | 350 | -0.0143 | HcoilHcoil | 05A3_05A4 | -0.0101 | V1_TrigCvtB2 | -0.0003 | HP_HN | 0.0027 |  |
| tqs01.Quench.070312195617.882 | 60 | 8966 | 250 | -0.0134 | HcoilHcoil | 15A6_15A8 | -0.0136 | 05B5_05B4 | -0.0085 | 05A7_05B6 | -0.0084 |  |
| tqs01.Quench.070312202058.433 | 61 | 8978 | 250 | -0.0129 | HcoilHcoil | 15A6_15A8 | -0.0134 | 15A5_15A6 | -0.0064 | 05A7_05B6 | -0.0057 |  |
| tqs01.Quench.070313094326.023 |  | 4 | 0 | -0.0035 | SlWcoil | V1_TrigCvtB2 | -0.0003 | 05A1_05A2M_2 | -0.0001 | HP_HN | 0 |  |
| tqs01.Quench.070313121853.733 | 62 | 9614 | 20 | -0.0063 | HcoilHcoil | 15A6_15A8 | -0.0073 | 15A5_15A6 | -0.0031 | V1_TrigCvtB2 | -0.0001 |  |
| tqs01.Quench.070313123808.269 |  | 0 | 0 | -0.0020 | WcoilGnd | 05B5_05B4 | -0.0001 | 15B5_15B4 | -0.0001 | V1_TrigCvtB2 | -0.0001 |  |
| tqs01.Quench.070313130308.171 | 63 | 9097 | 198 | -0.0123 | HcoilHcoil | 15A6_15A8 | -0.0126 | 15A5_15A6 | -0.0059 | 15A8_15B6 | -0.0032 |  |
| tqs01.Quench.070313134409.170 | 64 | 9611 | 20 | -0.0066 | HcoilHcoil | 15A6_15A8 | -0.0074 | 15A5_15A6 | -0.0029 | Q24P_Q24N | -0.002 |  |
| tqs01.Quench.070313140831.009 | 65 | 8981 | 250 | -0.0127 | HcoilHcoil | 15A6_15A8 | -0.0137 | 15A8_15B6 | -0.0085 | 05A1_05A2 | -0.0076 |  |
| tqs01.Quench.070313152204.724 | 66 | 9615 | 20 | -0.0070 | HcoilHcoil | 15A6_15A8 | -0.0076 | 15A5_15A6 | -0.0036 | 05A2_05A3 | -0.0032 |  |
| tqs01.Quench.070313154137.591 | 67 | 8981 | 250 | -0.0160 | WcoilGnd | 15A6_15A8 | -0.0133 | 08A3_08A2 | -0.0064 | 08A8_08A7 | -0.0064 |  |
| tqs01.Quench.070313161252.035 | 68 | 9617 | 19 | -0.0071 | HcoilHcoil | 15A6_15A8 | -0.0073 | 15A5_15A6 | -0.0038 | V1_TrigCvtB2 | -0.0003 |  |
| tqs01.Quench.070313164459.088 | 69 | 9616 | 20 | -0.0066 | HcoilHcoil | 15A6_15A8 | -0.0076 | 15A8_15B6 | -0.0052 | 15B6_15B5 | -0.0041 |  |
| tqs01.Quench.070313171540.528 | 70 | 9616 | 20 | -0.0064 | HcoilHcoil | 15A6_15A8 | -0.0073 | 15A5_15A6 | -0.0029 | 15B6_15B5 | -0.0017 |  |
| tqs01.Quench.070313174803.661 | 71 | 9632 | 20 | -0.0069 | HcoilHcoil | 15A6_15A8 | -0.0074 | 15A5_15A6 | -0.0039 | 15B6_15B5 | -0.0039 |  |
| tqs01.Quench.070313182743.141 | 72 | 9630 | 19 | -0.0064 | HcoilHcoil | 15A6_15A8 | -0.0074 | 05A3_05A4 | -0.0038 | 08B3_08B4 | -0.0035 |  |
| tqs01.Quench.070313190544.467 | 73 | 9641 | 20 | -0.0073 | HcoilHcoil | 15A6_15A8 | -0.0078 | 15A5_15A6 | -0.0045 | 05A7_05B6 | -0.0018 |  |
| tqs01.Quench.070313194543.628 | 74 | 9612 | 20 | -0.0084 | HcoilHcoil | 15A6_15A8 | -0.0087 | 15A5_15A6 | -0.0041 | 08B5_08A8 | -0.0003 |  |
| tqs01.Quench.070313202919.217 | 75 | 9926 | 20 | -0.0071 | HcoilHcoil | 15A6_15A8 | -0.0077 | 15A5_15A6 | -0.0041 | 05A3_05A4 | -0.0018 |  |
| tqs01.Quench.070313205845.334 | 76 | 9211 | 19 | -0.0101 | HcoilHcoil | 15A6_15A8 | -0.0113 | 15A5_15A6 | -0.0045 | V1_TrigCvtB2 | -0.0003 |  |
| tqs01.Quench.070313212139.437 | 77 | 9927 | 20 | -0.0063 | HcoilHcoil | 15A6_15A8 | -0.0070 | 15A5_15A6 | -0.0029 | 05B3_05B2 | -0.0022 |  |
| tqs01.Quench.070313214428.697 | 78 | 9924 | 20 | -0.0057 | HcoilHcoil | 15A6_15A8 | -0.0066 | 15A5_15A6 | -0.0022 | V1_TrigCvtB2 | -0.0003 |  |
| tqs01.Quench.070314143026.727 |  | 1 | 0 | -0.1945 | WcoilGnd | 05B5_05B4 | -0.0034 | 15B5_15B4 | -0.0034 | 08B1_08B2 | -0.0032 |  |
| tqs01.Quench.070314144411.388 | 79 | 9918 | 19 | -0.0060 | HcoilHcoil | 15A6_15A8 | -0.0064 | 15A5_15A6 | -0.0022 | V1_TrigCvtB2 | -0.0001 |  |
| tqs01.Quench.070314172755.661 | 80 | 9923 | 20 | -0.0062 | HcoilHcoil | 15A6_15A8 | -0.0069 | 15A5_15A6 | -0.0024 | 05B4_05B3 | -0.0018 |  |
| tqs01.Quench.070314181635.332 | 81 | 9703 | 20 | -0.0041 | HcoilHcoil | 15A6_15A8 | -0.0046 | 15A5_15A6 | -0.0035 | 05A2_05A3 | -0.0027 |  |
| tqs01.Quench.070314184853.444 | 82 | 9989 | 20 | -0.2071 | HcoilHcoil | 15A6_15A8 | -0.0069 | V1_TrigCvtB2 | -0.0036 | 15A5_15A6 | -0.0034 |  |
| tqs01.Quench.070314194009.492 | 83 | 9983 | 20 | -0.0035 | HcoilHcoil | 15A6_15A8 | -0.0062 | 15A5_15A6 | -0.0024 | 05A3_05A4 | -0.001 |  |
| tqs01.Quench.070314202926.124 | 84 | 9792 | 20 | -0.0064 | HcoilHcoil | 15A6_15A8 | -0.0067 | 15A5_15A6 | -0.0027 | 05A4_05A5 | -0.0024 |  |
| tqs01.Quench.070314205544.003 | 85 | 9982 | 20 | -0.0046 | HcoilHcoil | 15A6_15A8 | -0.0050 | 15A5_15A6 | -0.0029 | 05B5_05B4 | -0.0013 |  |
| tqs01.Quench.070315115603.030 | 86 | 9977 | 19 | -0.0042 | HcoilHcoil | 15A6_15A8 | -0.0074 | 15A5_15A6 | -0.0053 | 15A4_15A5 | -0.0025 |  |
| tqs01.Quench.070315123423.553 | 87 | 9979 | 20 | -0.0064 | HcoilHcoil | 15A6_15A8 | -0.0074 | 15A5_15A6 | -0.0056 | 05A1_05A2 | -0.0038 |  |
| tqs01.Quench.070315130807.526 | 88 | 9925 | 20 | -0.0091 | HcoilHcoil | 15A6_15A8 | -0.0070 | 15A5_15A6 | -0.0056 | 15A4_15A5 | -0.0025 |  |
| tqs01.Quench.070315135406.786 | 89 | 9935 | 20 | -0.0059 | HcoilHcoil | 15A6_15A8 | -0.0070 | 15A5_15A6 | -0.0057 | 05A7_05B6 | -0.0025 |  |
| tqs01.Quench.070315143047.299 | 90 | 9872 | 20 | -0.0097 | HcoilHcoil | 15A6_15A8 | -0.0098 | 15A5_15A6 | -0.0084 | 07A1_07A2M_2 | -0.005 |  |
| tqs01.Quench.070315153507.444 | 91 | 9770 | 20 | -0.0134 | HcoilHcoil | 15A6_15A8 | -0.0141 | 15A5_15A6 | -0.0123 | 07A1_07A2M_2 | -0.0102 |  |
| tqs01.Quench.070315183145.732 | 92 | 9487 | 20 | -0.0136 | HcoilHcoil | 15A6_15A8 | -0.0147 | 15A5_15A6 | -0.0097 | 08B3_08B4 | -0.0073 |  |
| tqs01.Quench.070315191243.471 | 93 | 8785 | 20 | -0.0245 | HcoilHcoil | 15A6_15A8 | -0.0286 | 15A5_15A6 | -0.0190 | 07B2_07B3 | -0.0147 |  |
| tqs01.Quench.070315193942.342 | 94 | 8814 | 20 | -0.0238 | HcoilHcoil | 15A6_15A8 | -0.0244 | 15A5_15A6 | -0.0169 | 08A3_08A2 | -0.0148 |  |
| tqs01.Quench.070315200356.056 | 95 | 8819 | 20 | -0.0262 | HcoilHcoil | 15A6_15A8 | -0.0270 | 15A5_15A6 | -0.0204 | 08A3_08A2 | -0.0144 |  |
| tqs01.Quench.070315203136.000 | 96 | 8822 | 20 | -0.0241 | HcoilHcoil | 15A6_15A8 | -0.0252 | 15A5_15A6 | -0.0179 | 08B4_08B5 | -0.0134 |  |
| tqs01.Quench.070315205716.269 | 97 | 8822 | 20 | -0.0238 | HcoilHcoil | 15A6_15A8 | -0.0252 | 15A5_15A6 | -0.0176 | 05A5_05A6 | -0.0125 |  |
| tqs01.Quench.070315213106.928 | 98 | 7148 | 20 | -0.0489 | HcoilHcoil | 15A6_15A8 | -0.0501 | 15A5_15A6 | -0.0395 | 08B2_08B3 | -0.0148 |  |
| tqs01.Quench.070316100850.826 | 99 | 7184 | 20 | -0.0442 | HcoilHcoil | 15A6_15A8 | -0.0459 | 15A5_15A6 | -0.0346 | V1_TrigCvtB2 | -0.0001 |  |
| tqs01.Quench.070316103450.084 | 100 | 7200 | 20 | -0.0483 | HcoilHcoil | 15A6_15A8 | -0.0497 | 15A5_15A6 | -0.0396 | Q24P_Q24N | -0.0071 |  |
| tqs01.Quench.070316110436.334 | 101 | 7207 | 20 | -0.0451 | HcoilHcoil | 15A6_15A8 | -0.0469 | 15A5_15A6 | -0.0354 | V1_TrigCvtB2 | -0.0003 |  |

Figure 2.2.  Quench history during training at 4.5K, at 1.9K, and during temperature dependence study. The marker of each quench shows the coil where it started.

- Temperature Dependence

Temperature dependence studies were performed at 20 A/s. All quenches started in coil 15. Results are shown in the following plot.

Fig 3.1  Temperature dependence.

- Ramp Rate Dependence

Ramp rate dependence studies were performed at 4.5 K. Results are shown in the following plot.

Figure 4.1.  Ramp rate dependence of quench current.  The marker of each quench shows the coil where it started.

- Heater studies

Protection heater studies were performed at 4.5 K. Two Heater Firing Units (HFUs) were configured for 4.8mF capacitance, with each connected to two magnet strip heaters in parallel. One HFU was manually fired with the magnet at a constant current to initiate a quench; the second HFU was discharged as a protection heater by the system when the quench was detected. Results for the quench development time are shown in the following plot.

Fig. 5.1  Protection heater delay plus detection time at different current. Different markers show the effect of different capacitor bank voltage.

- MIITs study

A study aimed at evaluating the effects of high MIITs was performed at 4.5K. The spot heater was not operational, therefore spontaneous quenches were used during this study. In the first part of the test, current ramp rate was set to 250 A/s in order to quench around 9000 A, and the dump delay was increased from 5 ms to 200 ms (following these steps: 25, 45, 65, 90, 200 ms). Standard current ramps at 20 A/s with no dump delay were performed after each MIITs deposition in order to asses any change in magnet performance. After quench 67 it was observed that 200 ms after the quench the current was so low that any further increase of the delay was not going to increase the MIITs (6.87).  Therefore the ramp rate was set to 20 A/s for all quenches in the rest of the study.

At 20 A/s the quench current was about 9620 A. The dump delay was increased from 5 to more than 250 ms. With quench 72 we started delaying also to the quench protection heaters following these steps: 7.6, 15.6, 21.2, 27.3 ms. After quench 74 (dump delay: 270 ms, protection heater delay: 21.2 ms, MIITs: 7.95)  the quench current jumped to 9926 A (+3.3%).

After quench 75 (dump delay: 276 ms, protection heater delay: 27.3 ms, MIITs: 8.16) the quench current decreased to 9211 A (-7.2% with respect to the previous quench). A following series of three quenches with standard delays (dump delay: 5 ms, no protection heater delay) found a plateau at 9923 A. Quench 80 (dump delay: 280 ms, protection heater delay: 30.7 ms, MIITs: 8.07) caused a small current decrease (9703 A) followed by a new current record (9989 A) in the two subsequent standard quenches. The current reached in quench 82 was 0.6% higher than the previous plateau, and 4.0% higher than the plateau with 20 A/s ramps before the MIITs study (9602 A).

Quench 83 (dump delay: 289 ms, protection heater delay: 40 ms, MIITs: 7.82) caused another small current decrease (9792 A) followed by a plateau around 9980 A. The following series of quenches with further increases of the protection heater delays (finally removed in quench 90) failed to increase the MIITs. Therefore in quench 90 the detection threshold was increase from 700 mV to 3 V (the AQD was actually around 2 V) generating 7.75 MIITs. In quench 91 (at 9770 A) the detection threshold was increased to 4 V (the AQD was actually around 3 V) and the quench generated 8.08 MIITs causing a current degradation of 2.9% with respect to the previous quench. In quench 92 (at 9487 A) the detection threshold was increased to 7 V and the quench generated 8.7 MIITs causing a current degradation of 7.4% with respect to the previous quench. A series of quenches with standard delays found a plateau at 8820 A. Another quench (97) with 7 V threshold without protection heaters and with 300 ms dump delay generated 9.53 MITTs.  Finally a series of quenches with standard delays found a plateau at 7200 A (-18.4% with respect to the previous plateau, and -25% with respect to the plateau with 20 A/s ramps before the MIITs study). The results are shown in the following plot.

Figure 6.1.  Quench history during MIITs study.  The marker of each quench shows the kind of quench. The numbers close to some quenches at 20 A/s with delays show the MIITs generated during that quench.

- Magnetic Measurements

The field quality magnetic measurements were made with the VMTF vertical drive system and LHC/EMS rotating harmonic coil readout cart. Several data sets were captured:  warm z-scan before cool down, z-scan at 6.5 kA @ 4.5 K, a full measurement program at 1.9 (described below), and finally a z-scan after the magnet warm up.  A 0.1 m long tangential probe, with 2 dipole, 2 quadrupole and 1 tangential windings, was utilized. This probe was specially built for these measurements with a radius of 2.17 cm, optimized to the warm finger ID. The positive direction of the z-axis for the scans is pointing from the magnetic center to the lead end, from which the probe was inserted.  Each measurement (e.g., at one z-position) contains data from at least 25 full rotations of the probe, and z-scans steps were equal to the length of the probe.

The magnetic measurement program at 1.9 K consisted of the following measurements:

  - Z-scans at 12.3 Tm/m (LHC injection, estimated to be 0.583 kA), 100 Tm/m (estimated to be 5.15kA), and 200 Tm/m or just below the maximum quench current, Iqmax– 0.6kA. For the last measurement, the magnet was powered at 10kA due to the quench limitation around 10.5 kA.

  - Z-scan at 4kA for comparison with TQC01

  - Eddy current loops:  20 40 and 80 A/s up to 10 kA with the  probe  positioned in the center of the magnet

  - Dynamic effects measurement, which included a current accelerator profile, similar to the one used in LHC MQXB quads (15 min. duration of the injection plateau and the probe positioned in the center of the magnet).

All magnetic measurement results are presented at 17 mm reference radius, the official radius adopted for LHC.  A detailed magnetic measurements summary is posted at the following URL:

HTTP://tdserver1.fnal.gov/velev/magnets/web/magnets/TQS01/TQS01c_mag_meas.html

Table 7.1 summarizes the quadrupole strength (T*m/m) and transfer function (TF) versus the excitation current, measured when the probe was positioned at the center of the magnet body (z=0 m). The 16% degradation of the TF at high currents is expected due to the iron saturation.

Fig. 7.1 shows the TF versus z coordinate profiles at 0.58, 5.15 and 10 kA. The integral magnetic lengths are calculated to be 0.712, 0.723 and 0.735 m at these currents.

| Requested Current (A) | -10 | 10 | 583 | 4000 | 5155 | 10000 |
| --- | --- | --- | --- | --- | --- | --- |
| Measured Current (A) | -10.81 | 10.80 | 583.84 | 3997.74 | 5152.42E | 9995.80 |
| Field (T*m/m) | 0.2336 | 0.2336 | 12.48 | 83.92 | 104.58 | 184.92 |
| TF (T/kA) | 21.71 | 21.62 | 21.38 | 20.99 | 20.29 | 18.50 |

Table 7.1 Strength and TF at different currents in the body of the magnet

Figure 7.1. The magnet TF versus z coordinate at 0.583, 5.15 and 10.0 kA.

Table 7.2 summarizes the harmonics at injection (0.583 kA) and maximum measured current (10 kA), averaged over the magnet (left) and for the center body position (right). In general, the field harmonics are in the order of several units. The b5 and b6 at injection are observed to be relatively large, ~ 10 units.

Table 7.2. TQS01c body and average harmonics at different currents

|  | Average | Average | Body only | Body only |
| --- | --- | --- | --- | --- |
| Multipole(units) | Injection | 10 kA | Injection | 10kA |
| b_3 | -1.014 | -0.365 | -1.147 | -0.805 |
| b_4 | -3.726 | -0.028 | -3.313 | 0.057 |
| b_5 | -9.054 | 1.636 | -9.263 | 1.481 |
| b_6 | -10.667 | 1.505 | -10.755 | 1.480 |
| b_7 | 0.108 | 0.014 | 0.103 | 0.024 |
| b_8 | 0.080 | -0.012 | 0.076 | 0.000 |
| b_9 | 0.134 | -0.021 | 0.155 | -0.004 |
| b_10 | 0.093 | -0.013 | 0.117 | 0.000 |
| a_3 | 0.085 | 0.298 | 1.358 | 1.560 |
| a_4 | -4.076 | -1.037 | -4.880 | -1.341 |
| a_5 | -4.122 | 0.329 | -4.565 | 0.466 |
| a_6 | 0.422 | 0.041 | 0.119 | -0.126 |
| a_7 | -0.077 | -0.041 | -0.031 | -0.040 |
| a_8 | -0.018 | -0.040 | 0.031 | -0.040 |
| a_9 | 0.014 | -0.007 | 0.038 | -0.003 |
| a_10 | -0.015 | 0.003 | -0.009 | 0.000 |

Figure 7.2 shows the dodecapole versus time. The current profile used in this measurement was derived from the profile of production inner triplet LHC quadrupole (LQXB) measurements. The duration of the injection porch was set to 15 min at 12.8 T, accordingly to the LHC specifications. One can observe that the b6 decay and snapback, which are commonly observed in NbTi magnets, are not present (see the time interval from ~900 to ~1800 s).

Current loops at 20, 40 and 80 A/s for TQS01 quadrupole have been executed. The b6 difference between the ramp rate loops is small, indicating small or negligible eddy current effect on the hysteresis loop. The b6 hysteresis loops are shown in Figure 7.3.

Figure 7.2. Dodecapole (b6, in units) versus time (s) in a modified LHC accelerator current profile.

Figure 7.3. Dodecapole (b6) versus excitation current at different ramp rates: 20 (red), 40 (green) and 80 (blue) A/s.

- Strain gauge results

Coils 5,7,8,15 were used in TQS01c. Each coil had 3 strain gauges: two gauges were located on the island center to measure azimuthal and axial strain and a single axial gauge was placed near the lead end. The gauges where thermally compensated by gauges mounted on stress-free element. Fully compensated strain gauges were also used on the shell and the axial tie rods. Measured strain “ε” in two principal directions “z, θ” (and no shear) was converted into stress “σ” using the relationships below with the Modulus, and Poisson ratio for bronze (islands) and aluminum (shell):

.

A comparison of stress in the structure and coils between the three TQS01 assemblies is shown in the table below.

|  | TQS01 | TQS01b | TQS01c |
| --- | --- | --- | --- |
| Maximum current (A) | 10602 (4.4K) 11019 (3.2K) | 9932 (4.4K) | 9570 (4.4K) 10521(1.9K) 9989 (4.4K) |
| Iss (%) | 87% (4.4K) | 82% (4.4K) | 80-82% (4.4K) 80% (1.9K) |
| Shell cold (MPa) -t | +152 | +158 | +142 |
| Shell cold (MPa) -z | +143 | +140 | +137 |
| Rods cold (MPa) -z | +113 | +116 | +148 |
| Island cold (MPa) -t | -198 | -202 | -162 |
| Island cold (MPa) -z | +34 | +34 | +39 |

A typical measured stress of coil 5 during cool-down is shown in the figure below:

Coils 7 and 8 showed a similar behavior however coil 15 behaved differently. During cool-down coil 15 gained only half the expected pre-stress and during heater studies lost most of its remaining pre-stress. In fact all indications are that the coil ended up in azimuthal tension close to 30MPa at 10kA. The figures below show the stress in all coils during excitation:

Changes in coil 15 island stress during heater studies (see section 6). After the coil generated 8 MIITs it gained 300A with an additional 80A following. Increasing the MIITs level closer to 9 MIITs resulted in coil degradation.

A number of pdf plot files with strain data can be found in:

http://supercon.lbl.gov/caspi/download/TQS01/TQS01c/

The measured strain during the entire test is shown in the following figures:

9. Quench Antenna Data

A quench antenna was used during training at 4.5 and 1.9K. The “KEK/HGQ” quench antenna consists of three stationary coil segments, each 0.35 m long and separated by 0.105 m long couplings. Each coil is made with four windings that are sensitive to normal and skew sextupole and octupole magnetic flux changes, at a radius of 23 mm. The probe was positioned in the bore of the magnet so that the second antenna coil, C2, was centered on the magnet coil center. Data analysis showed that only windings in C2 recorded flux change signals when the magnet started quenching. Figure 9.1 shows for every training quench the difference between the time of the first signal in the quench antenna coils and the time of the quench start according to voltage taps data. This difference is within +3 -2 ms with very few exceptions. Therefore almost all training quenches started in the magnet body and did not propagate to the ends before heater and dump were fired after (usually fast) quench development and detection.

Figure 9.1  Difference between start of signal in quench antenna coils, and in voltage taps during training.

- RRR measurement

Estimates of RRR in TQS01 coil segments have been made using data captured during the initial cool down of the magnet. This was the first attempt to perform a “slow” cool down of VMTF using gaseous helium, to limit temperature variations across the magnet in order to prevent large coil stresses, and the new procedure worked well. The magnet was cooled with helium gas starting from 300 K at about 09:30 on 2/28, reaching 23 K about 1800 on 3/1/07, as shown in Figure RRR-1; the dewar was filled with liquid helium early on 3/2.  No attempt was made to measure coil voltages during warm-up, as has been the usual procedure for VMTF magnet tests.

During the cool down, coil voltages across “fixed” and “configurable” voltage tap segments were monitored by the pentek data loggers, while a current of slowly alternating polarity, +/- 6A, was put through the magnet.  However, in fact, the cool down was begun about two hours prior to starting the voltage tap scans, so temperatures had already fallen somewhat by the time voltage monitoring began: thus, “room temperature” voltage readings are somewhat under-estimated because of this.  The scan configuration was also not completely correct, as debugging of the new configuration tool was taking place at this time: segments that were manually bridged across “open” taps were incorrect, and therefore are not available during for RRR measurements.  At 1800 on 3/1, at 23 K, an attempt was made to correct some of the errors in gain and channel assignments.  No attempt was made to cool below this temperature before filling with liquid helium.  Thus, in this discussion “RRR” of a segment refers to the ratio of voltage at “about 280 K” (12:20 on 2/28) to that at “about 23 K” (about 18:00 on 3/1) – i.e., it is an approximate measure that is not a proper calculation of RRR.  It is possible there were some variations in coil temperatures in the “300 K” data, between inner and outer coils for example. Amplifier gains for the channels studied were correct and stable throughout the measurement.

The best measurements come from the configurable voltage tap (CVT) channels, in which the amplifier gain (or attenuation) is almost continuously adjustable (.001 to 4000) and is therefore optimized for known segment lengths.  Fixed voltage taps (FVT) suffer from the use of older (partially programmable) amplifiers with much coarser gain and attenuation settings: in most of the FVT segments at 23 K the voltage difference (from + to -6A) toggles at the 1 bit resolution limit, so the measurements are not very reliable.  The CVT segments, however, have very good resolution in most cases.

Figure 10.1  Test Stand temperatures during gaseous He cool down of VMTF and TQS01.

Fig. 10.2.  RRR of inner layer, outer layer, and average for each coil (coils 5, 7, 8 and 15)

Figure 10.3.  RRR of segments (numbers correspond to the segments listed in Table 10.1)

|  | Coil 5 | Coil 7 | Coil 8 | Coil 15 |
| --- | --- | --- | --- | --- |
| 1 | 05A2_A3 | 07A3_A2 | 08A3_A2 | 15A2_A3 |
| 2 | 05A3_A4 | 07A5_A3 | 08A4_A3 | 15A3_A4 |
| 3 | 05A4_A5 | 07A6_A5 | 08A5_A4 | 15A4_A5 |
| 4 | 05A5_A6 | 07A7_A6 | 08A6_A5 | 15A5_A6 |
| 5 | 05A6_A7 | 07A8_A7 | 08A7_A6 | 15A6_A8 |
| 6 | 05A7_B6 | 07B6_A8 | 08A8_A7 | 15A8_B6 |
| 7 | 05B6_B5 | 07B5_B6 | 08B5_A8 | 15B6_B5 |
| 8 | 05B5_B4 | 07B4_B5 | 08B4_B5 | 15B5_B4 |
| 9 | 05B4_B3 | 07B3_B4 | 08B3_B4 | 15B4_B3 |
| 10 | 05B3_B2 | 07B2_B3 | 08B2_B3 | 15B3_B2 |

Table 10.1  List of segments with RRR plotted in Fig 10.3 (data not available if segment is read)

- Voltage Spikes

The voltage spike detection system (VSDS) was used to capture half coil voltage signals in a 500 ms window whenever the half coil difference exceeded a threshold of 100-130 mV (depending on the ramp).  This threshold was relatively large compared with our usual setting of about 15-25 mV, due to the level of noise on half coil signals (which may be due to the way in which these were wired and shielded).  These voltage data are available for each training ramp, until the system failed on ramp 26 due to a power supply problem.  Analysis of the spike data is still in progress. A few examples of big spikes are shown in the following.

Figure 11.1.  Voltage spike recorder during ramp 7. It didn’t trigger the quench protection system. Quench detection threshold was 600 mV.

Figure 11.2.  Another big voltage spike, recorder during ramp 7, that didn’t trigger the quench protection system.

Figure 11.3.  Voltage spike, recorder during ramp 10, that triggered the quench protection system. Quench detection threshold was 600 mV

# Text boxes

300 A gain

80 A gain

degradation

Gain of 300 A

Permanent degradation

80 A gain