Package Characteristics:  CABGA LF

| Feature | Value |
| --- | --- |
| Package Length | 10.02 mm |
| Package Width | 10.02 mm |
| Package Thickness | 0.99 mm |
| Solder Ball Diameter | 0.475 mm |
| Die Length | 5.5 mm |
| Die Width | 5.58 mm |
| Die Thickness | 0.26 mm |
| Pitch | 0.8 mm |
| Weight | 0.2420 g |
| CTE | 8.454 ppm/C |
| Width of Solder ball in contact with component pad | 0.395 mm |
| Solderball Alloy (SEM estimation) | Sn4Ag.5Cu |

Top View

Bottom View

Cross-section of solder ball

SEM of solder ball cross-section

X-ray