MSFC PRACA : 2003-02-12 08:41

MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A17536 | In-Flight Anomaly Number -- | Contractor Report Number P-089 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title DOCUMENTATION OF CORRECTIVE ACTION ASSOCIATED WITH USE OF INCORRECT WELDING ROD ON A 21-6-9 LINE |
| EICN# -- | ELEMENT ET | Contractor -- | FSCM# -- | FCRIT 1 |
| HCRIT -- | Sys_Lvl -- | Misc Codes A B C D E F G H ( ) I J K L M N O |
| HARDWARE EIM | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE LRU | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE NCA | NOMENCLATURE PROPULSION LINES | PART# PD 4800XXX-XXX | SER/LOT# VARIOUS | MANUFACTURER ARROWHEAD |
| Test/Operation M - MFG | Prevailing Condtion N - INSPECTION | F / U UC | Fail Mode UC - UNSAT | Cause MAT - MFG-ASY-EQUP |
| System PROPULSION | Defect MT - TYPE W | Material H - WELD | Work Contact W. MATTHEESS | Fail Date 12/16/1999 |
| Received at MSFC 12/22/1999 | Date Isolated 12/17/1999 | FMEA Reference 2.7.1.1 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location ARROWHEAD | Symptom UC - UNSAT | Time Cycle -- |
| Effectivity Text ET-92, 101 AND SUBSEQUENT |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 05/24/2000 | CN RSLV SBMT -- | Defer Date -- | Add Date 12/30/1999 | R/C Codes 2 - MFG -- -- |
| Assignee |
| Design M. BUTLER | Chief Engineer N. OTTE | S & MA R. GLADWIN | Project -- | Project MGR J. SMELSER |
| Approval |
| Design M. BUTLER | Chief Engineer N. OTTE | S & MA R. GLADWIN | Project . | Project MGR J. SMELSER |
| PAC Assignee T. WHITE | PAC Review Complete TLW | MSFC Closure Date 05/03/2000 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description ISSUE #1 (12/16/99): THE INCORRECT WELD ROD WAS USED ON ONE WELD IN A 21-6-9 PRESSLINE. HASTELLOY-W WELD ROD WAS USED INSTEAD OF THE REQUIRED 21-6-9 WELD ROD. ISSUE #2 (1/26/00): INCORRECT WELD FILLER ROD WAS CALLED OUT ON THE PLANNING PAPER. HASTELLOY-W WELD ROD WAS USED INSTEAD OF THE REQUIRED INCONEL 718 WELD ROD. CRITICALITY: THIS CONDITION IS A NON-CONFORMANCE AND DID NOT RESULT IN A FAILURE. * REVISION B DATED 3/30/00 REFER TO ASTERISK (*) FOR CHANGES. ALL TASK ITEMS NOW COMPLETE AND CLOSED THE FOLLOWING PART NUMBERS WERE AFFECTED: P/N ET S/N DESCRIPTION PD4800175-089 92 755 LO2 F/L FWD ELBOW PD4800175-089 93 756 LO2 F/L FWD ELBOW PD4800175-089 INV 757 LO2 F/L FWD ELBOW PD4800175-089 INV 760 LO2 F/L FWD ELBOW PD4800175-090 92 639 LO2 F/L AFT FLEX ASSY PD4800175-090 93 640 LO2 F/L AFT FLEX ASSY PD4800175-099 92 695 LO2 F/L FWD FLEX ASSY PD4800175-099 93 696 LO2 F/L FWD FLEX ASSY PD4800175-099 94 697 LO2 F/L FWD FLEX ASSY PD4800175-500 101 790 LO2 F/L FWD ELBOW PD4800175-500 102 791 LO2 F/L FWD ELBOW PD4800175-500 104 792 LO2 F/L FWD ELBOW PD4800175-500 105 793 LO2 F/L FWD ELBOW PD4800175-500 103 794 LO2 F/L FWD ELBOW PD4800175-500 107 795 LO2 F/L FWD ELBOW PD4800175-500 106 796 LO2 F/L FWD ELBOW PD4800175-500 109 797 LO2 F/L FWD ELBOW PD4800175-500 108 798 LO2 F/L FWD ELBOW PD4800175-500 INV 801 LO2 F/L FWD ELBOW PD4800175-509 101 815 LO2 F/L AFT FLEX ASSY PD4800175-509 102 816 LO2 F/L AFT FLEX ASSY PD4800175-509 103 817 LO2 F/L AFT FLEX ASSY PD4800175-509 104 818 LO2 F/L AFT FLEX ASSY PD4800175-509 105 819 LO2 F/L AFT FLEX ASSY PD4800175-509 107 820 LO2 F/L AFT FLEX ASSY PD4800175-509 106 821 LO2 F/L AFT FLEX ASSY PD4800175-509 108 822 LO2 F/L AFT FLEX ASSY PD4800175-509 109 823 LO2 F/L AFT FLEX ASSY PD4800175-509 INV 826 LO2 F/L AFT FLEX ASSY PD4800175-510 101 840 LO2 F/L FWD FLEX ASSY PD4800175-510 102 841 LO2 F/L FWD FLEX ASSY PD4800175-510 103 842 LO2 F/L FWD FLEX ASSY PD4800175-510 104 843 LO2 F/L FWD FLEX ASSY PD4800175-510 105 844 LO2 F/L FWD FLEX ASSY PD4800175-510 106 845 LO2 F/L FWD FLEX ASSY PD4800175-510 107 846 LO2 F/L FWD FLEX ASSY PD4800175-510 108 847 LO2 F/L FWD FLEX ASSY PD4800175-510 109 848 LO2 F/L FWD FLEX ASSY PD4800175-510 REC 855 LO2 F/L FWD FLEX ASSY PD4800178-020 104 139 LH2 LW RECIRCULATION LINE PD4800178-020 101 140 LH2 LW RECIRCULATION LINE PD4800178-020 102 141 LH2 LW RECIRCULATION LINE PD4800178-020 103 142 LH2 LW RECIRCULATION LINE PD4800178-020 92 143 LH2 LW RECIRCULATION LINE PD4800178-020 105 144 LH2 LW RECIRCULATION LINE PD4800178-020 106 145 LH2 LW RECIRCULATION LINE PD4800178-020 109 146 LH2 LW RECIRCULATION LINE PD4800178-020 107 148 LH2 LW RECIRCULATION LINE PD4800178-020 108 149 LH2 LW RECIRCULATION LINE PD4800178-020 INV 151 LH2 LW RECIRCULATION LINE PD4800178-020 INV 154 LH2 LW RECIRCULATION LINE PD4800178-020 REC 155 LH2 LW RECIRCULATION LINE PD4800180-010 105 1148 GO2 LINE ASSY UPPER LOC 1-6 PD4800180-010 101 1171 GO2 LINE ASSY UPPER LOC 1-6 PD4800180-010 102 1172 GO2 LINE ASSY UPPER LOC 1-6 PD4800180-010 103 1173 GO2 LINE ASSY UPPER LOC 1-6 PD4800180-010 92 1174 GO2 LINE ASSY UPPER LOC 1-6 PD4800180-010 104 1175 GO2 LINE ASSY UPPER LOC 1-6 PD4800180-010 107 1176 GO2 LINE ASSY UPPER LOC 1-6 PD4800180-010 INV 1177 GO2 LINE ASSY UPPER LOC 1-6 PD4800180-010 106 1178 GO2 LINE ASSY UPPER LOC 1-6 PD4800180-010 108 1179 GO2 LINE ASSY UPPER LOC 1-6 PD4800180-010 INV 1180 GO2 LINE ASSY UPPER LOC 1-6 PD4800180-010 INV 1181 GO2 LINE ASSY UPPER LOC 1-6 PD4800180-010 INV 1182 GO2 LINE ASSY UPPER LOC 1-6 PD4800180-010 INV 1183 GO2 LINE ASSY UPPER LOC 1-6 PD4800180-010 INV 1184 GO2 LINE ASSY UPPER LOC 1-6 PD4800180-010 INV 1186 GO2 LINE ASSY UPPER LOC 1-6 PD4800180-010 INV 1187 GO2 LINE ASSY UPPER LOC 1-6 PD4800180-010 INV 1188 GO2 LINE ASSY UPPER LOC 1-6 PD4800180-010 INV 1189 GO2 LINE ASSY UPPER LOC 1-6 PD4800180-010 INV 1190 GO2 LINE ASSY UPPER LOC 1-6 PD4800180-019 102 1208 GO2 LINE ASSY UPPER LOC 7-12 PD4800180-019 101 1230 GO2 LINE ASSY UPPER LOC 7-12 PD4800180-019 103 1231 GO2 LINE ASSY UPPER LOC 7-12 PD4800180-019 92 1232 GO2 LINE ASSY UPPER LOC 7-12 PD4800180-019 104 1233 GO2 LINE ASSY UPPER LOC 7-12 PD4800180-019 105 1234 GO2 LINE ASSY UPPER LOC 7-12 PD4800180-019 107 1235 GO2 LINE ASSY UPPER LOC 7-12 PD4800180-019 106 1236 GO2 LINE ASSY UPPER LOC 7-12 PD4800180-019 108 1237 GO2 LINE ASSY UPPER LOC 7-12 PD4800180-019 INV 1238 GO2 LINE ASSY UPPER LOC 7-12 PD4800180-019 INV 1239 GO2 LINE ASSY UPPER LOC 7-12 PD4800180-019 INV 1240 GO2 LINE ASSY UPPER LOC 7-12 PD4800180-019 INV 1241 GO2 LINE ASSY UPPER LOC 7-12 PD4800180-019 INV 1242 GO2 LINE ASSY UPPER LOC 7-12 PD4800180-019 INV 1243 GO2 LINE ASSY UPPER LOC 7-12 PD4800180-019 INV 1244 GO2 LINE ASSY UPPER LOC 7-12 PD4800180-019 INV 1245 GO2 LINE ASSY UPPER LOC 7-12 PD4800180-019 INV 1246 GO2 LINE ASSY UPPER LOC 7-12 PD4800180-069 102 1291 GO2 LINE ASSY UPPER OGIVE P/L PD4800180-069 103 1292 GO2 LINE ASSY UPPER OGIVE P/L PD4800180-069 104 1294 GO2 LINE ASSY UPPER OGIVE P/L PD4800180-069 105 1295 GO2 LINE ASSY UPPER OGIVE P/L PD4800180-069 107 1296 GO2 LINE ASSY UPPER OGIVE P/L PD4800180-069 106 1297 GO2 LINE ASSY UPPER OGIVE P/L PD4800180-069 108 1298 GO2 LINE ASSY UPPER OGIVE P/L PD4800180-069 INV 1299 GO2 LINE ASSY UPPER OGIVE P/L PD4800180-069 INV 1300 GO2 LINE ASSY UPPER OGIVE P/L PD4800180-069 INV 1301 GO2 LINE ASSY UPPER OGIVE P/L PD4800180-069 INV 1302 GO2 LINE ASSY UPPER OGIVE P/L PD4800180-069 101 1290 GO2 LINE ASSY UPPER OGIVE P/L PD4800180-069 92 1293 GO2 LINE ASSY UPPER OGIVE P/L PD4800180-080 101 1350 GO2 LINE ASSY MID INTERTANK P/L GO UMB JNT H PD4800180-080 102 1351 GO2 LINE ASSY MID INTERTANK P/L GO UMB JNT H PD4800180-080 103 1352 GO2 LINE ASSY MID INTERTANK P/L GO UMB JNT H PD4800180-080 104 1354 GO2 LINE ASSY MID INTERTANK P/L GO UMB JNT H PD4800180-080 105 1355 GO2 LINE ASSY MID INTERTANK P/L GO UMB JNT H PD4800180-080 107 1356 GO2 LINE ASSY MID INTERTANK P/L GO UMB JNT H PD4800180-080 106 1357 GO2 LINE ASSY MID INTERTANK P/L GO UMB JNT H PD4800180-080 108 1358 GO2 LINE ASSY MID INTERTANK P/L GO UMB JNT H PD4800180-080 INV 1359 GO2 LINE ASSY MID INTERTANK P/L GO UMB JNT H PD4800180-080 INV 1360 GO2 LINE ASSY MID INTERTANK P/L GO UMB JNT H PD4800180-080 INV 1361 GO2 LINE ASSY MID INTERTANK P/L GO UMB JNT H PD4800180-080 REC 1362 GO2 LINE ASSY MID INTERTANK P/L GO UMB JNT H PD4800180-080 92 1353 GO2 LINE ASSY MID INTERTANK PD4800180-089 102 1473 GO2 LINE ASSY MID LOC 31-33 JNT G-H PD4800180-089 102 1499 GO2 LINE ASSY MID LOC 23-26 JNT E-F PD4800180-089 101 1521 GO2 LINE ASSY MID LOC 31-33 JNT G-H PD4800180-089 101 1522 GO2 LINE ASSY MID LOC 23-26 JNT E-F PD4800180-089 101 1523 GO2 LINE ASSY MID LOC 20-22 JNT D-E PD4800180-089 101 1524 GO2 LINE ASSY MID LOC 27-30 JNT F-G PD4800180-089 103 1526 GO2 LINE ASSY MID LOC 31-33 JNT G-H PD4800180-089 103 1527 GO2 LINE ASSY MID LOC 23-26 JNT E-F PD4800180-089 103 1528 GO2 LINE ASSY MID LOC 20-22 JNT D-E PD4800180-089 103 1529 GO2 LINE ASSY MID LOC 27-30 JNT F-G PD4800180-089 92 1530 GO2 LINE ASSY MID LOC 31-33 JNT G-H PD4800180-089 92 1531 GO2 LINE ASSY MID LOC 20-22 JNT D-E PD4800180-089 92 1532 GO2 LINE ASSY MID LOC 23-26 JNT E-F PD4800180-089 92 1533 GO2 LINE ASSY MID LOC 27-30 JNT F-G PD4800180-089 104 1534 GO2 LINE ASSY MID LOC 23-26 JNT E-F PD4800180-089 104 1535 GO2 LINE ASSY MID LOC 27-30 JNT F-G PD4800180-089 104 1536 GO2 LINE ASSY MID LOC 31-33 JNT G-H PD4800180-089 104 1537 GO2 LINE ASSY MID LOC 20-22 JNT D-E PD4800180-089 107 1538 GO2 LINE ASSY MID LOC 31-33 JNT G-H PD4800180-089 105 1539 GO2 LINE ASSY MID LOC 31-33 JNT G-H PD4800180-089 107 1540 GO2 LINE ASSY MID LOC 27-30 JNT F-G PD4800180-089 107 1541 GO2 LINE ASSY MID LOC 20-22 JNT D-E PD4800180-089 105 1542 GO2 LINE ASSY MID LOC 23-26 JNT E-F PD4800180-089 105 1543 GO2 LINE ASSY MID LOC 20-22 JNT D-E PD4800180-089 105 1544 GO2 LINE ASSY MID LOC 27-30 JNT F-G PD4800180-089 107 1545 GO2 LINE ASSY MID LOC 23-26 JNT E-F PD4800180-089 102 1546 GO2 LINE ASSY MID LOC 20-22 JNT D-E PD4800180-089 102 1547 GO2 LINE ASSY MID LOC 27-30 JNT F-G PD4800180-089 106 1548 GO2 LINE ASSY MID LOC 20-22 JNT D-E PD4800180-089 106 1549 GO2 LINE ASSY MID LOC 27-30 JNT F-G PD4800180-089 106 1550 GO2 LINE ASSY MID LOC 23-26 JNT E-F PD4800180-089 106 1551 GO2 LINE ASSY MID LOC 31-33 JNT G-H PD4800180-089 108 1552 GO2 LINE ASSY MID LOC 31-33 JNT G-H PD4800180-089 108 1553 GO2 LINE ASSY MID LOC 20-22 JNT D-E PD4800180-089 108 1554 GO2 LINE ASSY MID LOC 23-26 JNT E-F PD4800180-089 108 1555 GO2 LINE ASSY MID LOC 27-30 JNT F-G PD4800180-089 INV 1556 GO2 LINE ASSY MID LOC 31-33 JNT G-H PD4800180-089 INV 1557 GO2 LINE ASSY MID LOC 31-33 JNT G-H PD4800180-089 INV 1558 GO2 LINE ASSY MID LOC 31-33 JNT G-H PD4800180-089 INV 1559 GO2 LINE ASSY MID LOC 20-22 JNT D-E PD4800180-089 INV 1560 GO2 LINE ASSY MID LOC 31-33 JNT G-H PD4800180-089 INV 1561 GO2 LINE ASSY MID LOC 20-22 JNT D-E PD4800180-089 INV 1562 GO2 LINE ASSY MID LOC 20-22 JNT D-E PD4800180-089 INV 1563 GO2 LINE ASSY MID LOC 20-22 JNT D-E PD4800180-089 INV 1564 GO2 LINE ASSY MID LOC 23-26 JNT E-F PD4800180-089 INV 1565 GO2 LINE ASSY MID LOC 23-26 JNT E-F PD4800180-089 INV 1568 GO2 LINE ASSY MID LOC 23-26 JNT E-F PD4800180-089 INV 1569 GO2 LINE ASSY MID LOC 23-26 JNT E-F PD4800180-089 INV 1572 GO2 LINE ASSY MID LOC 27-30 JNT F-G PD4800180-089 INV 1573 GO2 LINE ASSY MID LOC 27-30 JNT F-G PD4800180-089 INV 1574 GO2 LINE ASSY MID LOC 27-30 JNT F-G PD4800180-089 INV 1581 GO2 LINE ASSY MID LOC 27-30 JNT F-G PD4800180-089 INV 1583 GO2 LINE ASSY MID LOC 31-33 JNT G-H PD4800180-089 INV 1584 GO2 LINE ASSY MID LOC 20-22 JNT D-E PD4800180-089 INV 1585 GO2 LINE ASSY MID LOC 23-26 JNT E-F PD4800180-089 INV 1586 GO2 LINE ASSY MID LOC 27-30 JNT F-G PD4800180-090 INV 1645 GO2 LINE ASSY MID LOC 13-19 PD4800180-090 92 1644 GO2 LINE ASSY MID LOC 13-19 PD4800180-520 102 1697 GO2 LINE ASSY MID LOC 13-19 PD4800180-520 103 1698 GO2 LINE ASSY MID LOC 13-19 PD4800180-520 105 1699 GO2 LINE ASSY MID LOC 13-19 PD4800180-520 104 1700 GO2 LINE ASSY MID LOC 13-19 PD4800180-520 106 1702 GO2 LINE ASSY MID LOC 13-19 PD4800180-520 107 1703 GO2 LINE ASSY MID LOC 13-19 PD4800180-520 INV 1705 GO2 LINE ASSY MID LOC 13-19 PD4800180-520 108 1707 GO2 LINE ASSY MID LOC 13-19 PD4800180-520 INV 1708 GO2 LINE ASSY MID LOC 13-19 PD4800180-520 101 1695 GO2 LINE ASSY MID LOC 13-19 PD4800184-039 101 180 LH2 L/H FEEDLINE PD4800184-039 102 181 LH2 L/H FEEDLINE PD4800184-039 92 182 LH2 L/H FEEDLINE PD4800184-039 103 183 LH2 L/H FEEDLINE PD4800184-039 104 184 LH2 L/H FEEDLINE PD4800184-039 105 185 LH2 L/H FEEDLINE PD4800184-039 106 186 LH2 L/H FEEDLINE PD4800184-039 107 187 LH2 L/H FEEDLINE PD4800184-039 108 188 LH2 L/H FEEDLINE PD4800184-039 109 189 LH2 L/H FEEDLINE PD4800184-039 INV 195 LH2 L/H FEEDLINE PD4800205-009 92 482 GH2 LINE FWD FLEX ASSY PD4800205-009 INV 483 GH2 LINE FWD FLEX ASSY PD4800205-019 101 607 GH2 LINE ASSY MID STGHTLOC 23-26 JNT K-L PD4800205-019 102 608 GH2 LINE ASSY MID STGHTLOC 23-26 JNT K-L PD4800205-019 103 609 GH2 LINE ASSY MID STGHTLOC 23-26 JNT K-L PD4800205-019 92 610 GH2 LINE ASSY MID STGHTLOC 23-26 JNT K-L PD4800205-019 104 611 GH2 LINE ASSY MID STGHTLOC 23-26 JNT K-L PD4800205-019 105 612 GH2 LINE ASSY MID STGHTLOC 23-26 JNT K-L PD4800205-019 107 613 GH2 LINE ASSY MID STGHTLOC 23-26 JNT K-L PD4800205-019 106 614 GH2 LINE ASSY MID STGHTLOC 23-26 JNT K-L PD4800205-019 108 615 GH2 LINE ASSY MID STGHTLOC 23-26 JNT K-L PD4800205-019 INV 616 GH2 LINE ASSY MID STGHTLOC 23-26 JNT K-L PD4800205-019 INV 617 GH2 LINE ASSY MID STGHTLOC 23-26 JNT K-L PD4800205-019 INV 618 GH2 LINE ASSY MID STGHTLOC 23-26 JNT K-L PD4800205-019 INV 619 GH2 LINE ASSY MID STGHTLOC 23-26 JNT K-L PD4800205-019 INV 620 GH2 LINE ASSY MID STGHTLOC 23-26 JNT K-L PD4800205-019 INV 622 GH2 LINE ASSY MID STGHTLOC 23-26 JNT K-L PD4800205-029 92 721 GH2 LINE ELBOW FLEX ASSY P/L JNT X-N PD4800205-029 101 728 GH2 LINE ELBOW FLEX ASSY P/L JNT X-N PD4800205-029 102 729 GH2 LINE ELBOW FLEX ASSY P/L JNT X-N PD4800205-029 103 730 GH2 LINE ELBOW FLEX ASSY P/L JNT X-N PD4800205-029 104 731 GH2 LINE ELBOW FLEX ASSY P/L JNT X-N PD4800205-029 105 732 GH2 LINE ELBOW FLEX ASSY P/L JNT X-N PD4800205-029 107 733 GH2 LINE ELBOW FLEX ASSY P/L JNT X-N PD4800205-029 106 734 GH2 LINE ELBOW FLEX ASSY P/L JNT X-N PD4800205-029 INV 735 GH2 LINE ELBOW FLEX ASSY P/L JNT X-N PD4800205-029 108 736 GH2 LINE ELBOW FLEX ASSY P/L JNT X-N PD4800205-029 INV 737 GH2 LINE ELBOW FLEX ASSY P/L JNT X-N PD4800205-029 REC 738 GH2 LINE ELBOW FLEX ASSY P/L JNT X-N PD4800205-029 REC 739 GH2 LINE ELBOW FLEX ASSY P/L JNT X-N PD4800205-029 REC 740 GH2 LINE ELBOW FLEX ASSY P/L JNT X-N PD4800205-060 101 901 GH2 LINE AFT FLEX ASSY P/L GH UMB JNT PD4800205-060 102 908 GH2 LINE AFT FLEX ASSY P/L GH UMB JNT PD4800205-060 103 909 GH2 LINE AFT FLEX ASSY P/L GH UMB JNT PD4800205-060 92 910 GH2 LINE AFT FLEX ASSY P/L GH UMB JNT PD4800205-060 104 911 GH2 LINE AFT FLEX ASSY P/L GH UMB JNT PD4800205-060 105 912 GH2 LINE AFT FLEX ASSY P/L GH UMB JNT PD4800205-060 107 913 GH2 LINE AFT FLEX ASSY P/L GH UMB JNT PD4800205-060 106 914 GH2 LINE AFT FLEX ASSY P/L GH UMB JNT PD4800205-060 108 915 GH2 LINE AFT FLEX ASSY P/L GH UMB JNT PD4800205-060 INV 916 GH2 LINE AFT FLEX ASSY P/L GH UMB JNT PD4800205-060 INV 917 GH2 LINE AFT FLEX ASSY P/L GH UMB JNT PD4800205-060 INV 918 GH2 LINE AFT FLEX ASSY P/L GH UMB JNT PD4800205-060 INV 919 GH2 LINE AFT FLEX ASSY P/L GH UMB JNT PD4800205-060 INV 920 GH2 LINE AFT FLEX ASSY P/L GH UMB JNT PD4800205-079 101 547 GH2 LINE FWD STGHT ASSY LOC 20-22 JNT J-K PD4800205-079 102 548 GH2 LINE FWD STGHT ASSY LOC 20-22 JNT J-K PD4800205-079 103 549 GH2 LINE FWD STGHT ASSY LOC 20-22 JNT J-K PD4800205-079 92 550 GH2 LINE FWD STGHT ASSY LOC 20-22 JNT J-K PD4800205-079 104 551 GH2 LINE FWD STGHT ASSY LOC 20-22 JNT J-K PD4800205-079 105 552 GH2 LINE FWD STGHT ASSY LOC 20-22 JNT J-K PD4800205-079 107 553 GH2 LINE FWD STGHT ASSY LOC 20-22 JNT J-K PD4800205-079 106 554 GH2 LINE FWD STGHT ASSY LOC 20-22 JNT J-K PD4800205-079 108 555 GH2 LINE FWD STGHT ASSY LOC 20-22 JNT J-K PD4800205-079 INV 556 GH2 LINE FWD STGHT ASSY LOC 20-22 JNT J-K PD4800205-079 INV 557 GH2 LINE FWD STGHT ASSY LOC 20-22 JNT J-K PD4800205-079 INV 559 GH2 LINE FWD STGHT ASSY LOC 20-22 JNT J-K PD4800205-079 INV 560 GH2 LINE FWD STGHT ASSY LOC 20-22 JNT J-K PD4800205-079 INV 561 GH2 LINE FWD STGHT ASSY LOC 20-22 JNT J-K PD4800205-079 INV 562 GH2 LINE FWD STGHT ASSY LOC 20-22 JNT J-K PD4800205-079 INV 563 GH2 LINE FWD STGHT ASSY LOC 20-22 JNT J-K PD4800205-079 INV 564 GH2 LINE FWD STGHT ASSY LOC 20-22 JNT J-K PD4800205-080 101 667 GH2 LINE MID FIXED ASSY LOC 27-29 JNT L-M PD4800205-080 102 668 GH2 LINE MID FIXED ASSY LOC 27-29 JNT L-M PD4800205-080 103 669 GH2 LINE MID FIXED ASSY LOC 27-29 JNT L-M PD4800205-080 92 670 GH2 LINE MID FIXED ASSY LOC 27-29 JNT L-M PD4800205-080 104 671 GH2 LINE MID FIXED ASSY LOC 27-29 JNT L-M PD4800205-080 105 672 GH2 LINE MID FIXED ASSY LOC 27-29 JNT L-M PD4800205-080 107 673 GH2 LINE MID FIXED ASSY LOC 27-29 JNT L-M PD4800205-080 108 674 GH2 LINE MID FIXED ASSY LOC 27-29 JNT L-M PD4800205-080 INV 675 GH2 LINE MID FIXED ASSY LOC 27-29 JNT L-M PD4800205-080 INV 676 GH2 LINE MID FIXED ASSY LOC 27-29 JNT L-M PD4800205-080 INV 677 GH2 LINE MID FIXED ASSY LOC 27-29 JNT L-M PD4800205-080 INV 678 GH2 LINE MID FIXED ASSY LOC 27-29 JNT L-M PD4800205-080 106 679 GH2 LINE MID FIXED ASSY LOC 27-29 JNT L-M PD4800205-080 INV 680 GH2 LINE MID FIXED ASSY LOC 27-29 JNT L-M PD4800205-080 INV 681 GH2 LINE MID FIXED ASSY LOC 27-29 JNT L-M PD4800205-080 REC 682 GH2 LINE MID FIXED ASSY LOC 27-29 JNT L-M PD4800205-089 101 787 GH2 LINE AFT STGHT ASSY P/L JNT Y-X PD4800205-089 102 788 GH2 LINE AFT STGHT ASSY P/L JNT Y-X PD4800205-089 103 789 GH2 LINE AFT STGHT ASSY P/L JNT Y-X PD4800205-089 92 790 GH2 LINE AFT STGHT ASSY P/L JNT Y-X PD4800205-089 104 791 GH2 LINE AFT STGHT ASSY P/L JNT Y-X PD4800205-089 105 792 GH2 LINE AFT STGHT ASSY P/L JNT Y-X PD4800205-089 107 793 GH2 LINE AFT STGHT ASSY P/L JNT Y-X PD4800205-089 106 794 GH2 LINE AFT STGHT ASSY P/L JNT Y-X PD4800205-089 108 795 GH2 LINE AFT STGHT ASSY P/L JNT Y-X PD4800205-089 INV 796 GH2 LINE AFT STGHT ASSY P/L JNT Y-X PD4800205-089 INV 797 GH2 LINE AFT STGHT ASSY P/L JNT Y-X PD4800205-089 INV 798 GH2 LINE AFT STGHT ASSY P/L JNT Y-X PD4800205-089 INV 799 GH2 LINE AFT STGHT ASSY P/L JNT Y-X PD4800205-089 INV 800 GH2 LINE AFT STGHT ASSY P/L JNT Y-X PD4800205-089 INV 801 GH2 LINE AFT STGHT ASSY P/L JNT Y-X PD4800205-089 INV 802 GH2 LINE AFT STGHT ASSY P/L JNT Y-X PD4800205-089 INV 803 GH2 LINE AFT STGHT ASSY P/L JNT Y-X PD4800205-089 INV 804 GH2 LINE AFT STGHT ASSY P/L JNT Y-X PD4800205-089 INV 805 GH2 LINE AFT STGHT ASSY P/L JNT Y-X PD4800205-089 INV 806 GH2 LINE AFT STGHT ASSY P/L JNT Y-X PD4800205-089 INV 807 GH2 LINE AFT STGHT ASSY P/L JNT Y-X PD4800205-089 INV 808 GH2 LINE AFT STGHT ASSY P/L JNT Y-X PD4800205-090 107 822 GH2 LINE AFT STGHT ASSY LOC 30-32 JNT M-N PD4800205-090 101 848 GH2 LINE AFT STGHT ASSY LOC 30-32 JNT M-N PD4800205-090 102 849 GH2 LINE AFT STGHT ASSY LOC 30-32 JNT M-N PD4800205-090 103 850 GH2 LINE AFT STGHT ASSY LOC 30-32 JNT M-N PD4800205-090 92 851 GH2 LINE AFT STGHT ASSY LOC 30-32 JNT M-N PD4800205-090 104 852 GH2 LINE AFT STGHT ASSY LOC 30-32 JNT M-N PD4800205-090 105 853 GH2 LINE AFT STGHT ASSY LOC 30-32 JNT M-N PD4800205-090 106 854 GH2 LINE AFT STGHT ASSY LOC 30-32 JNT M-N PD4800205-090 108 855 GH2 LINE AFT STGHT ASSY LOC 30-32 JNT M-N PD4800205-090 INV 857 GH2 LINE AFT STGHT ASSY LOC 30-32 JNT M-N PD4800205-090 INV 858 GH2 LINE AFT STGHT ASSY LOC 30-32 JNT M-N PD4800205-090 INV 859 GH2 LINE AFT STGHT ASSY LOC 30-32 JNT M-N PD4800205-090 INV 860 GH2 LINE AFT STGHT ASSY LOC 30-32 JNT M-N PD4800205-090 INV 861 GH2 LINE AFT STGHT ASSY LOC 30-32 JNT M-N PD4800205-090 INV 862 GH2 LINE AFT STGHT ASSY LOC 30-32 JNT M-N PD4800205-090 INV 863 GH2 LINE AFT STGHT ASSY LOC 30-32 JNT M-N PD4800205-090 INV 1184 GH2 LINE AFT STGHT ASSY LOC 30-32 JNT M-N PD4800205-509 103 1163 GH2 LINE FWD FLEX ASSY PD4800205-509 102 1164 GH2 LINE FWD FLEX ASSY PD4800205-509 104 1165 GH2 LINE FWD FLEX ASSY PD4800205-509 105 1166 GH2 LINE FWD FLEX ASSY PD4800205-509 107 1167 GH2 LINE FWD FLEX ASSY PD4800205-509 108 1168 GH2 LINE FWD FLEX ASSY PD4800205-509 106 1169 GH2 LINE FWD FLEX ASSY PD4800205-509 INV 1170 GH2 LINE FWD FLEX ASSY PD4800205-509 INV 1171 GH2 LINE FWD FLEX ASSY PD4800205-509 101 1162 GH2 LINE FWD FLEX ASSY |
| Contractor Investigation/Resolution PROBLEM DESCRIPTION: ISSUE #1: ARROWHEAD IDENTIFIED A WELD THROUGH X-RAY ANALYSIS THAT MAY HAVE BEEN WELDED WITH THE WRONG WELD ROD. MMA LABORATORIES, INC.,AN INDEPENDENT LAB, INITIALLY IDENTIFIED AND REPORTED ON 12/10/99 THROUGH PORTABLE CHEMICAL ANALYSIS THAT THE WELD ROD MATERIAL WAS STAINLESS 316 ALLOY INSTEAD OF 21-6-9. THE WELD IN QUESTION WAS A GH2 FORWARD FLEX PRESSLINE SECTION, PD4800205-509. LMMSS WAS NOTIFIED ON 12-14-99 OF THIS ISSUE. INVESTIGATION FOLLOWED: - TESTING ON SOME OF THE OTHER WELDS ON THE SAME PRESSLINE INDICATED THAT THE CORRECT 21-6-9 ROD MATERIAL WAS PRESENT. - THE REMAINDER OF THE 21-6-9 WELD RODS FROM THE SAME LOT, 24903, WERE TESTED AND FOUND TO BE ACCEPTABLE. - CONFIRMATION OF MMA LABORATORIES, INC.'S FINDINGS OF STAINLESS 316 WELD ROD MATERIAL TYPE WAS REQUESTED BY MAF. ARROWHEAD SENT SAMPLES TO ATLAS, ANOTHER OUTSIDE TESTING LAB AND THE MAF TECHNICAL LAB. BOTH LABS AGREED THE MATERIAL WAS HASTELLOY-W, NOT STAINLESS 316. - ARROWHEAD IDENTIFIED THEY PURCHASE ALL THEIR WELD WIRE AND ROD FROM BOB MARTIN CO. - ARROWHEAD IDENTIFIED THE ONLY WELD ROD MATERIAL THEY USE IS 308 ECL, 347, 21-6-9, HASTELLOY-W AND INCONEL 718. - ARROWHEAD IDENTIFIED THAT ONLY MANUAL WELDS WERE SUSPECT. THE AUTOMATED AND/OR MACHINE WELDS USING WELD WIRE SPOOLS AND REQUIRE EDDY CURRENT INSPECTION PERFORMED ON THE MATERIAL PRIOR TO AND AFTER EACH WELD IS PERFORMED. - A COMPLETE REVIEW OF BOTH ARROWHEAD AND BOB MARTIN CO.'S PROCESSES WERE ACCOMPLISHED TO IDENTIFY THE MOST PROBABLE CAUSE OF THE MIXED WELD ROD MATERIAL. - BOB MARTIN CO. (WELD ROD SUPPLIER) PERFORMS ALL ETM64-119 FLOW DOWN REQUIREMENTS FOR ALLOY VERIFICATION OF EACH WELD ROD AS WELL AS REQUIRED CHEMICAL ANALYSIS PRIOR TO DELIVERY. - ALL ET-101 SINGLE ALLOY MANUAL WELD X-RAYS WERE REVIEWED BY LMMSS, AHP, AND SAMPLED BY NASA AND MSFC X-RAY INTERPRETERS/ENGINEERS TO IDENTIFY IF SIMILAR BI-METAL INDICATIONS WERE PRESENT. ALL WERE FOUND ACCEPTABLE. ISSUE #2: DURING A REVIEW OF WELD ROD CALLED OUT WITHIN THE ARROWHEAD PLANNING AGAINST THE DESIGN REQUIREMENTS ON THE DRAWING (AS A RESULT OF ISSUE #1), AN ARROWHEAD INSPECTOR DISCOVERED THAT FOR PD4800180-520, SN 0001706, (GO2 MID PRESSLINE) WELD #9 THE WRONG WELD ROD WAS CALLED OUT. THE ENGINEERING REQUIREMENT IS FOR INCONEL 718, HOWEVER HASTELLOY-W FILLER ROD WAS IDENTIFIED IN THE BUILD PAPER. WELD # 9 IS A CLOSE OUT WELD AND REQUIRES A DOUBLE EXPOSURE X-RAY FILM BECAUSE THE X-RAY IS SHOT ON AN ANGLE THROUGH MULTIPLE PIECES OF METAL. TASK I FAILURE/PROBLEM INVESTIGATION ISSUE #1: A. COMPLETE THE MATERIAL ANALYSIS ON THE SAMPLE OF WELD CONTAINING THE INCORRECT WELD ROD. CLOSURE STATEMENT: ANALYSIS BY AN OUTSIDE TESTING LAB, ATLAS, CONFIRMS THE MATERIAL IS HASTELLOY-W. THE MAF TECHNICAL LAB HAS ALSO CONFIRMED THE MATERIAL TO BE HASTELLOY-W. REF. LAB REPORT 99A204. RESPONSIBILITY: R. LEBOEUF -4643 R. PONTIFF -4320 ECD: 12/23/99 COMPLETE: 1/8/2000 B. IDENTIFY AND LOCATE ALL ET LINES WELDED BY ARROWHEAD AT MAF. CLOSURE STATEMENT: ALL LINES HAVE BEEN IDENTIFIED AND ARE ON ATTACHMENT 1.0. RESPONSIBILITY: W. MATTHEESSEN -3741 D. WESTPHAL -3740 ECD: 12-23-99 COMPLETE: 12-23-1999 C. PROVIDE DEFECT HISTORY (WELD REPAIRS) ON LINES IDENTIFIED ON ATTACHMENT 1.0 FROM ISSUE 1, ACTION B. PRIORITIES ARE ET-106, 92, THEN ET 102 AND UP. CLOSURE STATEMENT: ET-92, 101, 106, 102, & 103 WELD REPAIRS HAVE BEEN IDENTIFIED. BASED ON ENGINEERING ANALYSIS (REF,: 1, ACTION L) THIS TASK HAS BEEN RE- SCOPED, REQUIRING NO ADDITIONAL DATA TO BE PROVIDED. THIS TASK IS CLOSED RESPONSIBILITY: D. BALES -3840 W. SCHRIEFFER - 3840 M. ROHLINGER - 3761 S. PARIKH - 3760 ECD: 12-21-1999 - ET92 ECD: 1-4-2000 - REST OF LINES COMPLETE: 1-11-2000 D. PROVIDE DETAILED (PAPER & ELECTRONIC) LIST OF PARTS THAT ARE MANUAL MONO-METAL WELDS WHICH BY X-RAY REVIEW COULD DETERMINE A BI-METAL WELD. THIS LIST SHALL INCLUDE PD PART NUMBER, VENDOR PART NUMBER, DETAIL SUB-ASSEMBLY PART NUMBER AND WELD NUMBER. CLOSURE STATEMENT: LIST HAS BEEN GENERATED. X-RAY FILM DATA PACKAGES AND ENGINEERING DESIGN PACKAGES HAVE BEEN RECONCILED. REF: E-MAIL FROM J. SHELLY DATED 3/24/2000 REFERENCES COMPLETION OF TASK. RESPONSIBILITY: J. SHELLY - 4110 W. SIGUR - 4100 ECD: 12-20-1999 COMPLETE: 1-6-2000 E. REVIEW X-RAYS FOR THE CRITICAL MONO-METAL WELDS FOR HARDWARE AT MAF, IDENTIFIED ON ATTACHMENT 1.0 FROM ISSUE 1, ACTION B, C, & D. PRIORITIES ARE ET-101, 106, 92, THEN ET 102 AND UP. CLOSURE STATEMENT: ET-92, 101,& 106 ALL REQUIRED WELDS HAVE BEEN COMPLETED. THERE IS NO INDICATION OF INCORRECT WELD ROD BEING USED. BASED ON ENGINEERING ANALYSIS (ISSUE 1, ACTION L) THIS ACTION HAS BEEN RE-SCOPED. THIS ACTION IS CLOSED. REF.: EMAIL FROM S. JONES FOR G. COPELAND 1/10/2000. RESPONSIBILITY: S. MCEVOY -3742 D. WESTPHAL -3740 ECD: 2-25-2000 CANCELED: 1-11-2000 *F. DOCUMENT ALL INVESTIGATIVE ACTIVITY PERFORMED BY ARROWHEAD AND LOCKHEED MARTIN PERSONNEL AT ARROWHEAD & BOB MARTIN CO.. CLOSURE STATEMENT: INVESTIGATION WAS CONDUCTED AT BOTH ARROWHEAD PRODUCTS & BOB MARTIN (ARROWHEAD'S WELD ROD SUPPLIER) BY A JOINT LOCKHEED MARTIN & ARROWHEAD TEAM. THE BOB MARTIN REVIEW STARTED AT THE ORDER ENTRY POINT AND CONTINUED ON TO THE SHIP POINT. THE INVESTIGATION SHOWED CLEAR FLOWS WITH ADEQUATE CHECKS IN PLACE. CONTROLS ARE IN PLACE TO ASSURE NO MIXING OCCURS DURING SHIPMENT. BOB MARTIN COMPANY WAS EXONERATED AS A SOURCE OF SUSPICION FOR MIXED ALLOY, BASED ON THE SUSPECT ALLOY BEING IDENTIFIED AS HASTELLOY W (AVAILABLE AT ARROWHEAD), AND THROUGH THE AUDIT PERFORMED BY THE JOINT TEAM. A PRACTITIONER WELD BOOTH WAS IDENTIFIED AS THE LOCATION OF THE ALLOY MIX-UP. BASED ON INTERVIEWS WITH INSPECTORS, THE PRACTITIONER HAD PREVIOUSLY RECEIVED VERBAL WARNINGS FOR HAVING MULTIPLE ALLOY WELD RODS IN THE WORK AREA, AND AT THAT TIME ALL WELD RODS WERE CONFISCATED. HAVING MULTIPLE ALLOY WELD RODS IN THE WORK AREA IS A VIOLATION OF THE COMPANY POLICY. A REVIEW OF THE DAILY LABOR REPORTS SHOW, THAT ALL JOBS PERFORMED BY THE EMPLOYEE THE DAY PRIOR TO THIS INCIDENT REQUIRED THE USE OF HASTELLOY W. IN ADDITION, A 100% SCREENING OF ALL ROD IN THE CONTROLLED FLOOR STOCK DID NOT IDENTIFY ANY MIXED ALLOY. REF.: EMAIL DATED 2-15-2000 & FAX DATED 12-15-1999 FROM A. MEAD (ARROWHEAD VP QA) RESPONSIBILITY: D. BALES -3840 W. SCHRIEFFER - 3840 M. ROHLINGER - 3761 S. PARIKH - 3760 ECD: 12-23-1999 ECD: 2-11-2000 COMPLETE: 2-16-200 *G. EXPLAIN THE DIFFERENCE BETWEEN THE ORIGINAL CHEMISTRY REPORT (MMA LABORATORIES, 316) AND THE LATER REPORT (ATLAS & MAF, HASTELLOY-W). CLOSURE STATEMENT: THE LATTER CHEMICAL ANALYSIS USED PROVEN TECHNIQUES (SEM WITH EDX) AFTER CUTTING THE WELD OUT OF THE PART. ARROWHEAD PRODUCTS RECOMMENDED THE FIRST TEST AS A NONDESTRUCTIVE TECHNIQUE. ARROWHEAD AND LOCKHEED MARTIN QA PERSONNEL WITNESSED THE TEST AND APPROPRIATE CONTROLS WERE USED. A SAMPLE COUPON OF 316 WAS TESTED AND THE CHEMISTRY OF THE WELD MATCHED COMPLETELY. THE LAB CONFIRMED THAT THEY HAD USED THE TECHNIQUE FOR ROD VERIFICATION BEFORE. AFTER THE SECOND TEST CONFIRMED THE MATERIAL AS HASTELLOY W, THE LAB WAS CONTACTED AND QUESTIONED ON THE CAUSE OF THE MISIDENTIFICATION. IT WAS FOUND THAT ALL THE WELDS TESTED BY THIS TECHNIQUE BEFORE HAD BEEN SIGNIFICANTLY THICKER (CONSTRUCTION) WELDS, RESULTING IN CLEAR SAMPLING OF THE FILLER ALLOY ONLY. WITH LESS WELD WIDTH ON THE ARROWHEAD PART TOO MUCH OF THE PARENT (21-6-9) MATERIAL WAS PICKED UP AND AVERAGED INTO THE FILLER ROD, MASKING THE HIGH NICKEL CONTENT AND RESULTING IN THE IDENTIFICATION OF 300 SERIES STAINLESS WITH A MOLY CONTENT MATCHING 316. REF.: EMAIL DATED 2-15-2000 & FAX DATED 12-15-1999 FROM A. MEAD (ARROWHEAD VP QA) RESPONSIBILITY: D. BALES -3840 W. SCHRIEFFER - 3840 M. ROHLINGER - 3761 S. PARIKH - 3760 ECD: 12-23-1999 ECD: 2-11-2000 COMPLETE: 2-16-2000 *H. IDENTIFY ALL SUPPLIERS THAT WELD OR BRAZE ET HARDWARE AND AUDIT THEIR WELD WIRE/ROD CONTROL PROCESS. CLOSURE STATEMENT: AN AUDIT OF THE 15 SUPPLIERS THAT PERFORM EITHER WELDING OR BRAZING WAS COMPLETED. OF THE 15, TWO DID NOT REQUIRE AUDIT AS THEY DO NOT USE EITHER FILLER METAL OR BRAZING ROD IN THEIR PROCESS. ONE OTHER SUPPLIER (ARROWHEAD) WAS NOT AUDITED, SINCE IMPLEMENTATION OF CORRECTIVE ACTIONS IS NOT COMPLETE. OF THE 12 AUDITED SUPPLIERS, 6 HAD VARIOUS VIOLATIONS OF THE GOVERNING SPECIFICATIONS. IT WAS DETERMINED THAT NO FLIGHT HARDWARE IS AFFECTED. HOWEVER, 2 PIECES OF GROUND SERVICE EQUIPMENT (GSE) SUPPLIED BY SENIOR FLEXRONICS (SSP) IS AFFECTED. NCD N041803 WAS GENERATED TO ADDRESS THE GSE (82629021030- 009 S/NS 12 & 13). REF.: EMAIL FROM M. ROHLINGER 3-2-2000 & 3-9-2000. RESPONSIBILITY: D. BALES -3840 W. SCHRIEFFER - 3840 M. ROHLINGER - 3761 S. PARIKH - 3760 ECD: 1-16-2000 ECD: 2-29-2000 COMPLETE: 3-2-2000 I. ARROWHEAD TO PROVIDE WRITTEN CAUSE. CLOSURE STATEMENT: EMPLOYEE ERROR - WELDER VIOLATED COMPANY POLICY BY KEEPING MULTIPLE TYPES OF WELD ROD ALLOY IN WORK AREA. REF.: SPAR 99006-MA-AHP RESPONSIBILITY: D. BALES -3840 W. SCHRIEFFER - 3840 M. ROHLINGER - 3761 S. PARIKH - 3760 ECD: 1-18-2000 COMPLETE: 1-12-2000 *J. ARROWHEAD TO PROVIDE WRITTEN CORRECTIVE ACTIONS. CLOSURE STATEMENT: WELD ROD WILL NOW BE ISSUED BY QUALITY PERSONNEL INSTEAD OF THE AREA FOREMAN. THE PROCEDURE WAS REVISED TO REQUIRE THE WELDER TO DISPOSE OF ALL EXCESS WELD RODS IN A SECURE CONTAINER. ALL SHUTTLE PROGRAM WIRE WILL BE REPAINTED TO SHOW ALLOY COMPOSITION OF WELD. IN ADDITION, WEEKLY SURVEILLANCE BY QUALITY OF THE WELD WORK AREAS WILL BE CONDUCTED TO ASSURE COMPLIANCE. REF.: SPAR 99006-MA-AHP RESPONSIBILITY: D. BALES -3840 W. SCHRIEFFER - 3840 M. ROHLINGER - 3761 S. PARIKH - 3760 ECD: 1-18-2000 COMPLETE: 1-12-2000 K. ARROWHEAD TO CLEAR ALL LINES AND ASSEMBLES ON THEIR FACILITIES. LINES SHALL NOT BE SHIPPED WITHOUT SHOWING OBJECTIVE EVIDENCE THAT THIS HAS OCCURRED. CLOSURE STATEMENT: REVIEW OF ALL CRITICAL MONO-METAL WELDS ARE COMPLETE WITH NO SUSPECT WELDS NOTED. REF.: M. ROHLINGER EMAIL 2-24-2000. RESPONSIBILITY: D. BALES -3840 W. SCHRIEFFER - 3840 M. ROHLINGER - 3761 S. PARIKH - 3760 ECD: 2-25-2000 COMPLETE: 2-24-2000 L. BASED ON X-RAY REVIEW HISTORY & STRESS ANALYSIS REEVALUATE THE REQUIREMENT TO PERFORM 100% X-RAY REVIEWS OF MONO-METAL WELDS. CLOSURE STATEMENT: LIST HAS BEEN GENERATED, REVIEWED AND PAST ON TO ALL PARTIES. THIS LIST CONSISTS OF ALL WELDS ON LINES THAT HAVE LOW OR NEGATIVE MARGINS WHEN ANALYZED USING THE PROPERTIES OF 300 SERIES WIRE AND ARE MONO- METAL WELDS. REF. EMAIL DATED 1-10-2000 FROM G. COPELAND. RESPONSIBILITY: G. COPELAND - 3000 ECD: 1-12-2000 COMPLETE: 1-11-2000 *M. BASED ON THE REVISED LIST OF X-RAYS, REVIEW THE APPROPRIATE X-RAYS. CLOSURE STATEMENT: ALL LINES HAVE BEEN INSPECTED. ALL HAVE BEEN CLEARED. (ET-104; REFERENCE AR M00005 & M00005M3) RESPONSIBILITY: S. MCEVOY -3742 D. WESTPHAL - 3740 ECD: 2-25-2000 COMPLETE: 2-1-2000 ISSUE #2: *A. REVIEW ALL PROCESS PLANS WHICH BUILD ET FLIGHT HARDWARE TO DETERMINE THOSE PLANS WHICH ARE INCORRECT. THIS SHOULD START WITH ET-92. CLOSURE STATEMENT: 1. ET-92, 102 THRU 109 & INVENTORY REVIEW IS COMPLETE AND ALL PLANS WERE CORRECT, EXCEPT AS NOTED BELOW. 2. PART NUMBER PD4800180-520 REVIEW IS COMPLETE AND SERIAL NUMBERS / ETS ARE SHOWN BELOW. LOCATION / ET # PART SERIAL # CLEARANCE RATIONALE 104 0001700 N037963 N/A 0001701 PROPERTY LOST REPORT 106 0001702 N037963 107 0001703 N037963 109 0001705 N046504 STORES 0001704 & 0001708 N046506 ARROWHEAD 0001706 INITIAL DEFECT 108 0001707 ACCEPTABLE AS BUILT REF. M. ROHLINGER EMAILS DATED 2-15-2000 (ET-107, 109, & INVENTORY) (102 THRU 107 & ET-92) RESPONSIBILITY: D. BALES -3840 W. SCHRIEFFER - 3840 M. ROHLINGER - 3761 S. PARIKH - 3760 ECD: 2-4-2000 COMPLETE: 2-15-2000 *B. ARROWHEAD TO PROVIDE WRITTEN ROOT CAUSE AND CORRECTIVE ACTIONS. CLOSURE STATEMENT: CAUSE ISSUE #1: EMPLOYEE ERROR - WELDER VIOLATED COMPANY POLICY BY KEEPING MULTIPLE TYPES OF WELD ROD ALLOY IN WORK AREA. CAUSE * ISSUE #2: EMPLOYEE ERROR - INCORRECT WELD ROD SPECIFIED ON PLANNING AND INADEQUATE CHANGE DESCRIPTION ON THE PLANNING CHANGE RECORD CAUSED THE ERROR TO GO UNNOTICED DURING ARROWHEAD AND LMMSS REVIEW AND APPROVAL. OVERALL CAUSE: THE MANUFACTURING PLANNING SPECIFIED THE INCORRECT WELD ROD. WELD ROD VERIFICATION WAS PERFORMED TO THE PLANNING REQUIREMENT, INSTEAD OF TO BOTH DRAWING AND PLANNING REQUIREMENTS. THE INCORRECT ALLOY WAS INADVERTENTLY SPECIFIED DURING A REVISION TO THE PLANNING WHERE WELD ALLOYS WERE MOVED FROM A GENERAL NOTES FIELD TO A SPECIFICATION FIELD. THE PLANNING CHANGE RECORD IDENTIFIED THE CHANGE AS AN UPGRADE TO CURRENT [PLANNING] STANDARDS, WITHOUT SPECIFICALLY IDENTIFYING THE OPERATION CHANGED OR THE NATURE OF THE CHANGE. ROOT CAUSE: INADEQUATE CHANGE DESCRIPTION ON THE PLANNING CHANGE RECORD CAUSED THE ERROR TO GO UNNOTICED DURING ARROWHEAD AND LMMSS REVIEW AND APPROVAL. CORRECTIVE ACTION: 1. QS-210 REVISION L, WHICH DEFINES WELD ROD CONTROL REQUIREMENTS, REQUIRES ALLOY VERIFICATION BY DRAWING AND PLANNING. THIS POLICY HAS BEEN IMPLEMENTED AND CONTRIBUTED TO THE IDENTIFICATION OF THE ERROR. 2. QUALITY BULLETIN 00-03 (ON FILE) HAS BEEN ISSUED TO DEFINE THE REQUIREMENTS FOR PLANNING CHANGE DESCRIPTION. REF.: SCAR 00-012 TASK II CORRECTIVE ACTIONS ISSUE #1: - WELD ROD WILL NOW BE ISSUED BY QUALITY PERSONNEL INSTEAD OF THE AREA FOREMAN. - PROCEDURE REVISED TO REQUIRE WELDER TO DISPOSE OF ALL EXCESS WELD ROD IN SECURE CONTAINER. - ALL SHUTTLE PROGRAM WIRE TO BE REPAINTED TO SHOW ALLOY COMPOSITION OF WELD. - IN ADDITION WEEKLY SURVEILLANCE BY QUALITY OF THE WELD WORK AREAS TO ASSURE COMPLIANCE. REF.: SPAR 99006-MA-AHP * ISSUE #2: - QS-210 REVISION L, WHICH DEFINES WELD ROD CONTROL REQUIREMENTS, REQUIRES ALLOY VERIFICATION BY DRAWING AND PLANNING. THIS POLICY HAS BEEN IMPLEMENTED AND CONTRIBUTED TO THE IDENTIFICATION OF THE ERROR. - QUALITY BULLETIN 00-03 (ON FILE) HAS BEEN ISSUED TO DEFINE THE REQUIREMENTS FOR PLANNING CHANGE DESCRIPTION. REF.: SCAR 00-012 RESPONSIBILITY: D. BALES -3840 W. SCHRIEFFER - 3840 M. ROHLINGER - 3761 S. PARIKH - 3760 ECD: 2-11-2000 COMPLETE: 2-15-2000 TASK III CLEARANCE OF EFFECTIVITIES ISSUE #1: ET-92, 101 & 106 CLEARED BASED ON THE FOLLOWING: A. AUTOMATED AND MACHINE WELDS HAVE WELD WIRE ID INSPECTION GATES (EDDY CURRENT) BEFORE AND AFTER EACH WELD B. MANUAL WELDED MONO-METAL WELDS WERE CLEARED THROUGH 100% X- RAY ANALYSIS, WHICH WOULD IDENTIFY ANY BI-METAL CONDITIONS. C. MANUAL WELDED BI-METAL WELDS WERE CLEARED USING STRESS ANALYSIS ON ALL WELDS USING WORST CASE INCORRECT WELD WIRE MATERIAL. THE GO2 PRESSLINE WAS IDENTIFIED AS THE ONLY BI- METALLIC WELDED JOINT WITH REDUCED STRUCTURAL FS USING AISI 308 WELD MATERIAL. D. MOST WELDS MEET DESIGN REQUIREMENTS THROUGH DEMONSTRATED PROOF TEST TO GREATER THAN 100% OF DESIGN LIMIT LOADS REF.: ET-101 FRR CHARTS * ET-102, 103, 104 (EXCEPT FOR FORWARD GO2 PRESSLINE), 105 & 107 THRU 109 & ALL UNINSTALLED LINES AT MAF ARE CLEARED: BASED ON X-RAY REVIEW CRITERIA IDENTIFIED IN ISSUE #1 ACTION M, AND THE ISSUE #1 CRITERIA IDENTIFIED ABOVE EXCEPT FOR B. * ET-104 (FORWARD GO2 PRESSLINE: - ANALYSIS SHOWED THAT MATERIAL IS HASTELLOY-W - TESTING OF 718 PANELS WELDED WITH HASTELLOY-W SHOWED MARGIN OF SAFETY IS UNAFFECTED. ISSUE #2: - ET-92, 102 THRU 109 & INVENTORY REVIEW IS COMPLETE AND ALL PLANS WERE CORRECT, EXCEPT AS NOTED BELOW. - PART NUMBER PD4800180-520 REVIEW IS COMPLETE AND SERIAL NUMBERS / ETS ARE SHOWN BELOW. LOCATION / ET # PART SERIAL # CLEARANCE RATIONALE 104 0001700 N037963 N/A 0001701 PROPERTY LOST REPORT 106 0001702 N037963 107 0001703 N037963 109 0001705 N046504 STORES 0001704 & 0001708 N046506 ARROWHEAD 0001706 INITIAL DEFECT 108 0001707 ACCEPTABLE AS BUILT PD4800180-520 (SLWT) ET-101 THRU 103, 105 - BUILT PRIOR TO PLANNING CHANGE REFERENCE ISSUE 2 ACTION A. * TASK IV CAPS CLOSURE SUMMARY THERE WERE TWO ISSUES FOUND AT ARROWHEAD. THE FIRST ISSUE WAS FOUND ON 12/16/99 CONCERNING THE USE OF INCORRECT WELD ROD ON ONE WELD IN A 21-6-9 PRESSLINE. HASTELLOY-W WELD ROD WAS USED INSTEAD OF THE REQUIRED 21-6-9 WELD ROD. THE SECOND ISSUE WAS FOUND ON 1/26/00 AND CONCERNS INCORRECT WELD FILLER ROD THAT WAS CALLED OUT ON THE PLANNING PAPER. HASTELLOY-W WELD ROD WAS USED INSTEAD OF THE REQUIRED INCONEL 718 WELD ROD. AN EXTENSIVE REVIEW WAS CONDUCTED TO DETERMINE THE CAUSE OF THE FIRST ISSUE. IT WAS FINALLY TRACED TO AN EMPLOYEE KEEPING WELD ROD IN THE WORK AREA AFTER COMPLETING A JOB. THIS WAS IN VIOLATION OF COMPANY POLICY. IN ADDITION, EXTENSIVE TESTING WAS PERFORMED TO DETERMINE WHAT THE DISCREPANT WELD ROD MATERIAL WAS THAT WAS USED. FOR CORRECTIVE ACTION, ARROWHEAD CHANGED THE ISSUANCE OF WELD ROD FROM FOREMAN TO QUALITY PERSONEL. THE PROCEDURE WAS ALSO REVISED TO REQUIRE THE WELDER TO DISPOSE OF ALL EXCESS WELD ROD IN A SECURE CONTAINER. ALL SHUTTLE PROGRAM WIRE TO BE REPAINTED TO SHOW ALLOY COMPOSITION OF WELD. IN ADDITION, WEEKLY SURVEILLANCE BY QUALITY OF THE WELD WORK AREAS WILL BE CONDUCTED TO ASSURE COMPLIANCE. THE CAUSE OF THE SECOND ISSUE WAS THAT THE MANUFACTURING PLANNING SPECIFIED THE INCORRECT WELD ROD. WELD ROD VERIFICATION WAS PERFORMED TO THE PLANNING REQUIREMENT, INSTEAD OF TO BOTH DRAWING AND PLANNING REQUIREMENTS. THE INCORRECT ALLOY WAS INADVERTENTLY SPECIFIED DURING A REVISION TO THE PLANNING WHERE WELD ALLOYS WERE MOVED FROM A GENERAL NOTES FIELD TO A SPECIFICATION FIELD. THE PLANNING CHANGE RECORD IDENTIFIED THE CHANGE AS AN UPGRADE TO CURRENT [PLANNING] STANDARDS, WITHOUT SPECIFICALLY IDENTIFYING THE OPERATION CHANGED, OR THE NATURE OF THE CHANGE. THE ROOT CAUSE WAS INADEQUATE CHANGE DESCRIPTION ON THE PLANNING CHANGE RECORD THAT CAUSED THE ERROR TO GO UNNOTICED DURING ARROWHEAD AND LMMSS REVIEW AND APPROVAL. THE CORRECTIVE ACTIONS INCLUDED QS-210 REVISION L, WHICH DEFINES WELD ROD CONTROL REQUIREMENTS, REQUIRES ALLOY VERIFICATION BY DRAWING AND PLANNING. THIS POLICY HAS BEEN IMPLEMENTED AND CONTRIBUTED TO THE IDENTIFICATION OF THE ERROR. THE SECOND CORRECTIVE ACTION WAS THE ISSUANCE OF QUALITY BULLETIN 00-03 TO DEFINE THE REQUIREMENTS FOR PLANNING CHANGE DESCRIPTION. 3/31/00 TASK I - ISSUE #1 F, G, H, M, CLOSED OUT ISSUE #2 A & B, ALSO CLOSED OUT TASK II - ISSUE #2 CORRECTIVE ACTIONS ADDED TASK III - ADDED CLEARANCE OF EFFECTIVITIES FOR ISSUE #1 ET 102 THRU 105, 107 THRU 109 & INVENTORY - ISSUE #2 ET-92, 102 THRU 109 & INVENTORY TASK IV - CLOSED THIS CAPS IS CLOSED |
| MSFC Response/Concurrence 5/23/2000 - BOARD ACCEPTED PROBLEM CLOSURE RATIONALE. SIGNATURES ARE ON FILE IN THE PAC. THIS PROBLEM IS OFFICIALLY CLOSED. |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A17536 | IFA# -- | Contractor RPT# P-089 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# PD4800XXX-XXX | Asmnt Part Name PROPULSIONS LINES | Asmnt Serial/Lot# VARIOUS |
| HCRIT CD 1 | FCRIT CD 3 | CAUSE CD MAT - MFG-ASY-EQUP | FAIL MODE UC - UNSAT |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |