Package Characteristics: CABGA Sn63

| Feature | Value |
| --- | --- |
| Package Length | 10.01 mm |
| Package Width | 10.01 mm |
| Package Thickness | 0.99 mm |
| Solder ball diameter | 0.471 mm |
| Die Length | 5.5 mm |
| Die Width | 5.55 mm |
| Die Thickness | 0.26 mm |
| Pitch | 0.80 mm |
| Weight | 0.2458 g |
| CTE | 8.329 ppm/C |
| Width of Solder ball in contact with component pad | 0.399 mm |
| Solderball Alloy (SEM estimation) | Sn63Pb37 |

Top View

Bottom View

Cross-section of solder ball

SEM of solder ball x-section

X-ray