MSFC PRACA : 2003-02-12 08:41

MSFC Problem Reporting and Corrective Action (PRACA) System

WHOLE RECORD REPORT( + ADDENDUM)

| MSFC Record # A17340 | In-Flight Anomaly Number -- | Contractor Report Number P-086 | JSC# -- | KSC# -- |
| --- | --- | --- | --- | --- |
| Problem Title LH2 FEEDLINE JOINT 2 LEAKAGE |
| EICN# -- | ELEMENT ET | Contractor LMMSS | FSCM# -- | FCRIT 1 |
| HCRIT -- | Sys_Lvl -- | Misc Codes A B C D E F G H I J K L M N O |
| HARDWARE EIM | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE LRU | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| HARDWARE NCA | NOMENCLATURE -- | PART# -- | SER/LOT# -- | MANUFACTURER -- |
| Test/Operation AS - ATS | Prevailing Condtion F - FUNCTIONAL | F / U -- | Fail Mode UC - UNSAT | Cause M - MANUFG |
| System PROPULSION | Defect -- | Material -- | Work Contact E. ALDAHIR | Fail Date 11/13/1998 |
| Received at MSFC 11/17/1998 | Date Isolated 11/13/1998 | FMEA Reference 2.5.8.1 | IFA: Mission Phase -- | Mission Elapsed Time -- |
| Location MAF | Symptom MV - EXT LEAK | Time Cycle -- |
| Effectivity Text ET102 |
| Vehicle Effectivity Codes |
| Vehicle 1 -- | Vehicle 2 -- | Vehicle 3 -- | Vehicle 4 -- | Vehicle 5 -- |
| Mission Effectivity Codes |
| Mssn 1 -- | Mssn 2 -- | Mssn 3 -- | Mssn 4 -- | Mssn 5 -- |
| Estimated Completion Dates |
| MSFC Approved Defer Until Date -- | Contractor Req Defer Until Date -- | LVL 3 Close -- | Remark / Action -- |
| Investigation / Resolution Summary |
| Last MSFC Update 11/25/1998 | CN RSLV SBMT 11/18/1998 | Defer Date -- | Add Date 11/17/1998 | R/C Codes -- -- -- |
| Assignee |
| Design J. SANFORD | Chief Engineer J. LUSK | S & MA M. SMILES | Project -- | Project MGR P. COUNTS |
| Approval |
| Design J. SANFORD | Chief Engineer J. LUSK | S & MA J. GREEN | Project -- | Project MGR J. SINGER |
| PAC Assignee R. TUCKER | PAC Review Complete -- | MSFC Closure Date 11/25/1998 | Status C - CLOSED | F/A Completion -- |
| Problem Type -- | SEV -- | Program Name -- | REVL -- | OPRINC -- |
| FUNC MOD -- | Software Effectivity -- -- -- -- -- | Software Fail CD -- | SUBTYPE -- | Software Closure CD -- |
| RES PERSON L2 -- | Approval Signature L3 -- |
| Related Document Type -- | Related Document ID N036182 |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Related Document Type -- | Related Document ID -- |
| Related Document Title -- |
| Contractor Status Summary |
| Reliability/Quality Assurance Concerns, Recommendations: |
| Problem Description THE LH2 FEEDLINE AT JOINT 2 (FEEDLINE TO UMBILICAL DISCONNECT) HAD A LEAK RATE OF 218.0 SCCM AT 6 PSIG DURING THE PERFORMANCE OF LEAK TEST TP-8C101-FA IN THE MAF FINAL ASSEMBLY AREA. THE MAXIMUM ALLOWABLE LEAK RATE IS 20 SCCM CRITICALITY: THE FAILURE IS A CRIT. 1; FMEA ITEM CODE 2.5.8.1; "LEAKAGE." |
| Contractor Investigation/Resolution GENERAL DURING THE DUAL SEAL CAVITY LEAK CHECK OF JOINT TWO (LH2 EXTERNAL FEEDLINE TO LH2 DISCONNECT), A 218.0 SCCM LEAK WAS DETECTED. THE ALLOWABLE LEAKAGE IS 20 SCCM MAXIMUM AT 6.0 +/- .5 PSIG GHE, AS TESTED PER TP-8C101-FA. THIS JOINT USES A GFP SUPPLIED NAFLEX SEAL MULTIPLE VISUAL DEFECTS WERE DETECTED ON THE PRIMARY SEALING SURFACE OF GFP NAFLEX SEAL AFTER REMOVAL TASK I. FAILURE INVESTIGATION A. EVALUATE SEAL CONDITION FOR CONFORMANCE TO ENGINEERING REQUIREMENTS RESPONSIBILITY: W. MATTHEESSEN-3741/D.WESTPHAL-3740 ECD: 11-16-1998 COMPLETE: 11-16-1998 CLOSURE STATEMENT: A VISUAL INVESTIGATION WAS PERFORMED AND MULTIPLE AREAS OF BARE METAL WERE DETECTED. A FURTHER INSPECTION WAS CONDUCTED AT 10X MULTIPLE DEFECTS WERE FOUND ON THE PRIMARY SEALING SURFACE. THEY INCLUDED: 1. A LONG GREEN TEFLON DEFECT (TEAR) ON THE FLOW DIVERTER SIDE OF THE PRIMARY SEALING SURFACE 2. NUMEROUS CLUSTERS OF "BURST" BUBBLES WERE FOUND ON THE PRIMARY SEALING SURFACE. THESE WERE SCATTERED OVER THE CIRCUMFERENCE OF THE PRIMARY SEALING SURFACE. MANY OF THESE "BURST " BUBBLES UPON FURTHER EXAMINATION OF THE TEFLON SHOWED NO EVIDENCE OF THE REQUIRED BLACK TEFLON PRIMER ON EITHER THE METALLIC SUBSTRATE OR THE GREEN TEFLON FINAL COAT 3. SEVERAL AREAS BLACK TEFLON PRIMER SHOWING THROUGH THE GREEN TEFLON FINISH COAT 4. SEVERAL AREAS OF INTACT BUT PARTIALLY COLLAPSED BUBBLES THE CAUSE OF THE LEAKAGE WAS MANUFACTURING DEFECTS THAT WERE NOT DETECTABLE BY NORMAL UNAIDED VISUAL INSPECTION. THESE PRE-EXISTING DEFECTS UPON INSTALLATION AND TORQUEING CAUSED MULTIPLE LEAK PATHS ACROSS THE PRIMARY SEALING SURFACE CAUSE: 1. MANUFACTURING DEFECT ON GFP NAFLEX SEAL TASK II. CORRECTIVE ACTION A. GFP NAFLEX SEAL NONE, GFP HARDWARE. GFP SEAL RETURNED TO BOEING NORTH AMERICAN FOR INVESTIGATION PER CONTRACT DIRECTION. THIS WILL BE TRACKED BY STANDARD MSFC TRACKING SYSTEM FOR GFP PROBLEMS TASK III. CLEARANCE OF EFFECTIVITIES ALL ET'S CLEARED. THE PURPOSE OF LEAK TESTING IS TO FILTER OUT SUCH DISCREPANCIES. ALL INSTALLED JOINTS PASSED TM04 REQUIRED LEAK TEST TASK IV. CAPS CLOSURE SUMMARY DURING THE STANDARD SEAL CAVITY LEAK TEST PROCEDURE TP-8C101-FA ON JOINT 2 OF THE LH2 UMBILICAL DISCONNECT LINE, A 218.0 SCCM HELIUM LEAK WAS DETECTED (6.0 +/- .5 PSIG APPLIED PRESSURE). THIS EXCEEDS THE ALLOWABLE LEAKAGE RATE OF 20 SCCM AFTER INVESTIGATION IT WAS DETERMINED THAT THE MOST PROBABLE CAUSE FOR THE LEAK WAS THE MULTIPLE MANUFACTURING DEFECTS FOUND ON THE GFP SEAL PRIMARY SEALING SURFACE. THE GFP SEAL HAS BEEN RETURNED TO BOEING NORTH AMERICAN FOR INVESTIGATION PER CONTRACTS DIRECTION THIS CAPS IS CLOSED. NO FURTHER ACTION IS REQUIRED |
| MSFC Response/Concurrence 11/25/98 - MSFC APPROVES CLOSURE OF THIS PR |

MSFC Problem Reporting and Corrective Action (PRACA) System

ASSESSMENT ADDENDUM REPORT

| MSFC Report# A17340 | IFA# -- | Contractor RPT# P-086 | JSC# -- | KSC# -- | EICN# -- |
| --- | --- | --- | --- | --- | --- |
| Asmnt Part# 0600-500 | Asmnt Part Name LH2 FEEDLINE | Asmnt Serial/Lot# -- |
| HCRIT CD -- | FCRIT CD 1 | CAUSE CD M - MANUFG | FAIL MODE UC - UNSAT |
| Asmnt FMEA 2.5.8 | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM 1 | FMEA CSE -- | FMEA SCSE -- |
| Asmnt FMEA -- | Asmnt FM -- | FMEA CSE -- | FMEA SCSE -- |
| Correlated Part# -- | Correlated Part# -- | Correlated Part# -- |
| Associated LRU# -- | Associated LRU# -- | Associated LRU# -- |
| MAJOR DESIGN CHANGES |
| APRV DATE -- | DESCRIPTION OF CHANGES -- |
| ASSESSMENT TEXT |