UNITED STATES DEPARTMENT OF AGRICULTURE

NATURAL RESOURCES CONSERVATION SERVICE

OREGON

MATERIAL SPECIFICATION

MS-211  BEDDING

1.	SCOPE

This specification governs the quality of bedding material used in the foundation of pipelines, conduits and structures.

2.	QUALITY

Soil material, fine gravel or coarse gravel specified as bedding material shall be durable, non-compressible and be within the grading limits of the Unified Soil Classification System, USCS.  The ASTM specifications for classifying soils are:  ASTM D-2487, Classification of Soils for Engineering Purposes, and ASTM D-2488, Standard Practice for Description and Identification of Soils (Visual Manual Procedure).

3.	GRADATION

The following table lists some general properties of materials suitable for bedding.  Gradation is unique for each soil in the USCS.  The bedding requirements are site specific and shall be shown on the drawings using an identification symbol of the USCS.

|  |  | S.G. | Size |
| --- | --- | --- | --- |
| Material | USCS | (Min.) | (Max.) |
| Soil | SW,SP,SM,SC,ML,CL | 1.75 | #10 Sieve |
| Fine Gravel | SW,SP,SM,SC | 2.00 | 3/4-inch |
| Coarse Gravel | GW,GP,GM,GC | 2.40 | 3-inch |
|  | SW,SP,SM,SC |  |  |