PRODUCTION COST ISSUES FOR COSINE THETA AND COMMON COIL MAGNETS

Peter Wanderer, BNL

Vlhc MAGNET WORKSHOP

FERMILAB — MAY, 2000

Compare cosine theta, common coil:

processes

components

( new ideas for cost-reduction r&d?

| SUPERCONDUCTOR PROPERTIES | NbTi | Nb3Sn or HTS (prereacted) |
| --- | --- | --- |
| Cost | Cheap | Expensive |
| Cable shape (precise) | Keystoned | Rectangular |
| Minimum bend radius | < 1 cm | ~ 3 cm |
| Winding tension | Medium to high | Medium |
| Turn-to-turn insulation | Kapton – 1 mil delicate & robust to ~ 140 MPa | Glass cloth—delicate and robust |
| Apply turn-to-turn insulation | Barberpole wrap | Sock, weave, or barberpole wrap |

Cost:  New Nb3Sn R&D effort (multilab, multivendor)

## Separate copper stabilizer from superconducting wire

Bend radius:  common coil magnets

| COIL DESIGN | Cosine Theta | Common Coil Racetrack |
| --- | --- | --- |
| Peak Field/Central Field | Highest | Similar in optimized design |
| Field Quality (systematic) | 2D wedges, thick 3D end spacers | 2D rectangles, thick 2D end spacers (+ auxiliary coils?) |

Field quality: Start with large 2D coils.

Study tradeoffs:

complexity of auxiliary coils,

separate trim coils,

accelerator physics systematic f.q. tolerances

| COIL MANUFACTURE | Cosine Theta (3D) | Racetrack (2D) |
| --- | --- | --- |
| Coil Winder (automatic) | 3D (rotates winding mandrel) | 2D |
| Straight section (precise wedges) | Trapezoidal wedges | Rectangular wedges |
| Ends | Many 3D separators, inserted by hand | A few 2D separators |
| Leads | Solder to NbTi expansion loop | Different solder to NbTi expansion loop |

| COIL MFGR. (cont.) | Cosine Theta (3D) | Racetrack (2D) |
| --- | --- | --- |
| Coil sizing fixture | 3D 70 MPa precise heated complex insert | 2D 0.1 MPa precise vacuum impreg. 2D insert |
| Conductor position random variation | ~ 25 (m to 50 (m | Little data |

** Common coil conductor position:  make multiple (short) coils and magnets, nominally identical, measure field quality

| COIL ASSEMBLY | Cosine Theta | Common coil |
| --- | --- | --- |
| “Degree of difficulty” | 6 | 3 |
| Field Quality focus | Top-bottom coil matching | Left-right coil matching (little data) |
| Preload in straight section | Preload ( Lorentz force | Low appears to be ok |
| Axial preload | Thick endplates | Nominal |

Field Quality:  left-right matching calculations, trial assemblies

Preload: R&D fixturing that allows preload to be varied cheaply.

| COIL ASSEMBLY (cont.) | Cosine Theta | Common coil |
| --- | --- | --- |
| Assembly press | Massive, precise dimensions | Nominal (precise) |
| Coil contact parts (laminations) | Precise, complex collars (die cost) | Precise support plates (laminated?) |
| Ground plane insulation | Folded kapton | Kapton with many fewer folds |

Coil contact parts:

laminated vs. nonlaminated designs for common coil.

| YOKE (laminated) | Cosine Theta | Common coil |
| --- | --- | --- |
| Shape | Approximately round interior, exterior | Racetrack interior, round or rectangular exterior |
| Amount of material | Lots, especially 1-in-1 | Less |
| Configuration | 1-in-1 vs 2-in-1 | 2-in-1 |